17 CUTTING TOOL TECHNOLOGY

# Review Questions

- What are the two principal aspects of cutting-tool technology?

- Answer. The two principal aspects of cutting tool technology are (1) tool material and (2) tool geometry.

- Name the three modes of tool failure in machining.

- Answer. The three tool failure modes are (1) fracture failure, (2) temperature failure, and (3) gradual wear.

- What are the two principal locations on a cutting tool where tool wear occurs?

- Answer. Wear occurs on the top face of the cutting tool as crater wear and on the side or flank of the tool, called flank wear. Portions of flank wear are often identified separately as notch wear, corresponding to the surface of the work; and nose radius wear, corresponding to the tool point.

- Identify the mechanisms by which cutting tools wear during machining.

- Answer. The important tool wear mechanisms are (1) abrasion, (2) adhesion, (3) diffusion, and (4) plastic deformation of the cutting edge.

- What is the physical interpretation of the parameter C in the Taylor tool life equation?

- Answer. The parameter C is the cutting speed corresponding to a one-minute tool life. C is the speed-axis intercept on the log-log plot of the tool life data.

- What are some of the tool life criteria used in production machining operations?

- Answer. As identified in the text, tool life criteria used in production include (1) visual observation of flank or crater wear, (2) degradation of finish, (3) workpiece count, and (4) length of cutting time for the tool.

- Identify three desirable properties of a cutting-tool material.

- Answer. Three desirable properties are (1) toughness to resist fracture failure, (2) hot hardness to resist temperature failure, and (3) wear resistance to prolong the life of the tool during gradual wear.

- What are the principal alloying ingredients in high-speed steel?

- Answer. Principal alloying ingredients in HSS are (1) either tungsten or a combination of tungsten and molybdenum, (2) chromium, (3) vanadium, and (4) carbon. Some grades of HSS also contain cobalt.

- What is the difference in ingredients between steel cutting grades and nonsteel-cutting grades of cemented carbides?

- Answer. In general, non-steel cutting grades contain only WC and Co. Steel cutting grades contain TiC and/or TaC in addition to WC-Co.

- Identify some of the common compounds that form the thin coatings on the surface of coated carbide inserts.

- Answer. The common coatings are: TiN, TiC, and Al2O3.

- Name the seven elements of tool geometry for a single point cutting tool.

- Answer. The seven elements of single-point tool geometry are (1) back rake angle, (2) side rake angle, (3) end relief angle, (4) side relief angle, (5) end cutting edge angle, (6) side cutting edge angle, and (7) nose radius.

- Identify the alternative ways by which a cutting tool is held in place during machining.

- Answer. There are three principal ways: (1) solid shank, in which the cutting edge is an integral part of the tool shank, an example being high speed steel tooling; (2) brazed inserts, used for some cemented carbides; and (3) mechanically clamped inserts, used for most hard tool materials including cemented carbides, coated carbides, cermets, ceramics, SPD, and CBN.

- Name the two main categories of cutting fluid according to function.

- Answer. The two functional categories of cutting fluids are: (1) coolants and (2) lubricants.

- Name the four categories of cutting fluid according to chemistry.

- Answer. The four categories of cutting fluids according to chemistry are (1) cutting oils, (2) emulsified oils, (3) chemical fluids, and (4) semi-chemical fluids.

- What are the methods by which cutting fluids are applied in a machining operation?

- Answer. The most common method of application is flooding, in which a steady stream of fluid is direct at the operation.  Other methods include mist application, fluid-hole delivery through the tool, and manual application (e.g., using a paint brush).

- Dry machining is being considered by machine shops because of certain problems inherent in the use of cutting fluids. What are those problems associated with the use of cutting fluids?

Answer. Cutting fluids become contaminated over time with a variety of contaminants, including tramp oil, garbage, small chips, molds, fungi, and bacteria. In addition to causing odors and health hazards, contaminated cutting fluids do not perform their lubricating function as well as when they are fresh and clean.

- What are some of the new problems introduced by machining dry?

Answer. Problems with dry machining include (1) overheating the tool, (2) operating at lower cutting speeds and production rates to prolong tool life, and (3) absence of chip removal benefits that are provided by cutting fluids in grinding and milling.

- Define machinability.

- Answer. Machinability can be defined as the relative ease with which a material can be machined using an appropriate cutting tool under appropriate cutting conditions.

- What are the criteria by which machinability is commonly assessed in a production machining operation?

- Answer. The machinability criteria include (1) tool wear and tool life, (2) forces and power, (3) surface finish, and (4) ease of chip disposal.

- What are the factors on which the selection of feed in a machining operation should be based?

- Answer. The factors are (1) type of tooling (e.g., a cemented carbide tool should be used at a lower feed than a high-speed steel tool), (2) whether the operation is roughing or finishing (e.g., higher feeds are used in roughing operations), (3) cutting forces limitations that would require lower feeds, and (4) surface roughness requirements.

- The unit cost in a machining operation is the sum of four cost terms.  The first three terms are: (1) part load/unload cost, (2) cost of time the tool is actually cutting the work, and (3) cost of the time to change the tool. What is the fourth term?

- Answer. The fourth term is the cost of the tool itself (purchasing the tool and grinding it, if applicable).

- Which cutting speed is always lower for a given machining operation, cutting speed for minimum cost or cutting speed for maximum production rate? Why?

Answer. Cutting speed for minimum cost is always lower because of the fourth term in the unit cost equation, which deals with the actual cost of the cutting edge. This term tends to push the U-shaped function toward a lower value in the case of cutting speed for minimum cost.

# Problems

- Flank wear data were collected in a series of turning tests using a coated carbide tool on hardened alloy steel at a feed of 0.30 mm/rev and a depth of 4.0 mm. At a speed of 125 m/min, flank wear = 0.12 mm at 1 min, 0.27 mm at 5 min, 0.45 mm at 11 min, 0.58 mm at 15 min, 0.73 at 20 min, and 0.97 mm at 25 min. At a speed of 165 m/min, flank wear = 0.22 mm at 1 min, 0.47 mm at 5 min, 0.70 mm at 9 min, 0.80 mm at 11 min, and 0.99 mm at 13 min. The last value in each case is when final tool failure occurred. (a) On a single piece of linear graph paper, plot flank wear as a function of time for both speeds. Using 0.75 mm of flank wear as the criterion of tool failure, determine the tool lives for the two cutting speeds. (b) On a piece of natural log-log paper, plot your results determined in the previous part. From the plot, determine the values of n and C in the Taylor Tool Life Equation. (c) As a comparison, calculate the values of n and C in the Taylor equation solving simultaneous equations. Are the resulting n and C values the same?

Solution: (a) and (b) Student exercises. For part (a), at v1 = 125 m/min, T1 = 20.4 min using criterion FW = 0.75 mm, and at v2 = 165 m/min, T2 = 10.0 min using criterion FW = 0.75 mm. In part (b), values of C and n may vary due to variations in the plots. The values should be approximately the same as those obtained in part (c) below.

(c) Two equations: (1) 125(20.4)n = C, and (2) 165(10.0)n = C

(1) and (2) 125(20.4)n = 165(10.0)n

ln 125 + n ln 20.4 = ln 165 + n ln 10.0

4.8283 + 3.0155 n = 5.1059 + 2.3026 n

0.7129 n = 0.2776				n = 0.3894

(1) C = 125(20.4)0.3894 = 404.46

(2) C = 165(10.0)0.3894 = 404.46			C = 404.46

- Solve Problem 17.1 except that the tool life criterion is 0.50 mm of flank land wear rather than 0.75 mm.

- Solution: (a) and (b) Student exercises. For part (a), at v1 = 125 m/min, T1 = 13.0 min using criterion FW = 0.50 mm, and at v2 = 165 m/min, T2 = 5.6 min using criterion FW = 0.50 mm. In part (b), values of C and n may vary due to variations in the plots. The values should be approximately the same as those obtained in part (c) below.

- (c) Two equations: (1) 125(13.0)n = C, and (2) 165(5.6)n = C

- (1) and (2) 125(13.0)n = 165(5.6)n

- ln 125 + n ln 13.0 = ln 165 + n ln 5.6

- 4.8283 + 2.5649 n = 5.1059 + 1.7228 n

- 0.8421 n = 0.2776				n = 0.3296

- (1) C = 125(13.0)0.3894 = 291.14

- (2) C = 165(5.6)0.3894 = 291.15			C = 291.15

- Tool life tests on a lathe have resulted in the following data: (1) at a cutting speed of 375 ft/min, the tool life was 5.5 min; (2) at a cutting speed of 275 ft/min, the tool life was 53 min. (a) Determine the parameters n and C in the Taylor tool life equation. (b) Based on the n and C values, what is the likely tool material used in this operation? (c) Using your equation, compute the tool life that corresponds to a cutting speed of 300 ft/min. (d) Compute the cutting speed that corresponds to a tool life T = 10 min.

- Solution: (a) VTn = C; Two equations: (1) 375(5.5)n = C  and (2) 275(53)n = C

- 375(5.5)n = 275(53)n

- 375/275 = (53/5.5)n

- 1.364 = (9.636)n

- ln 1.364 = n ln 9.636

- 0.3102 = 2.2655 n			n = 0.137

- C = 375(5.5)0.137  = 375(1.2629) 		C = 474

- Check: C = 275(53)0.137 = 275(1.7221) = 474

- (b) Comparing these values of n and C with those in Table 17.2, the likely tool material is high speed steel.

- (c) At v = 300 ft/min, T = (C/v)1/n = (474/300)1/0.137  = (1.579)7.305  = 28.1 min

- (d) For T = 10 min, v = C/Tn = 474/100.137 = 474/1.371 = 346 ft/min

- Tool life tests in turning yield the following data: (1) when cutting speed is 100 m/min, tool life is 10 min; (2) when cutting speed is 75 m/min, tool life is 30 min. (a) Determine the n and C values in the Taylor tool life equation. Based on your equation, compute (b) the tool life for a speed of 110 m/min, and (c) the speed corresponding to a tool life of 15 min.

- Solution: (a) Two equations: (1) 120(7)n = C  and (2) 80(28)n = C.

- 120(7)n = 80(28)n

- ln 120 + n ln 7 = ln 80 + n ln 28

- 4.7875 + 1.9459 n = 4.3820 + 3.3322 n

- 4.7875 - 4.3820 = (3.3322 – 1.9459) n

- 0.4055 = 1.3863 n			n = 0.2925

- C = 120(7)0.2925 = 120(1.7668) 		C = 212.0

- Check: C = 80(28)0.2925 = 80(2.6503) = 212.0

- (b) 110 T0.2925 = 212.0

- T0.2925 = 212.0/110 = 1.927

- T = 1.9271/0.2925 = 1.9273.419 = 9.42 min

- (c) v (15)0.2925 = 212.0

- v = 212.0/(15)0.2925 = 212.0/2.2080 = 96.0 m/min

- Turning tests have resulted in 1-min tool life at a cutting speed = 4.0 m/s and a 20-min tool life at a speed = 2.0 m/s. (a) Find the n and C values in the Taylor tool life equation. (b) Project how long the tool would last at a speed of 1.0 m/s.

- Solution: (a) For data (1) T = 1.0 min, then C =  4.0 m/s = 240 m/min

- For data (2) v = 2 m/s = 120 m/min

- 120(20)n = 240

- 20n = 240/120 = 2.0

- n ln 20 = ln 2.0

- 2.9957 n = 0.6931			n = 0.2314

- (b) At v = 1.0 m/s = 60 m/min

- 60(T)0.2314 = 240

- (T)0.2314 = 240/60 = 4.0

- T = (4.0)1/0.2314 = (4)4.3215 = 400 min

- In a production turning operation, the workpart is 125 mm in diameter and 300 mm long. A feed of 0.225 mm/rev is used in the operation. If cutting speed = 3.0 m/s, the tool must be changed every 5 workparts; but if cutting speed = 2.0 m/s, the tool can be used to produce 25 pieces between tool changes. Determine the Taylor tool life equation for this job.

- Solution: (1) Tm = (125 mm)(0.3 m)/(3.0 m/s)(0.225 mm) = 174.53 s = 2.909 min

- T = 5(2.909) = 14.54 min

- (2) Tm = (125 mm)(0.3 m)/(2.0 m/s)(0.225 mm) = 261.80s = 4.363 min

- T = 25(4.363) = 109.08 min

- (1) v = 3 m/s = 180 m/min

- (2) v = 2 m/s = 120 m/min

- (1) 180(14.54)n = C

- (2) 120(109.08)n = C

- 180(14.54)n = 120(109.08)n

- ln 180 + n ln(14.54) = ln 120 + n ln(109.08)

- 5.1929 + 2.677 n = 4.7875 + 4.692 n

- 5.1929 - 4.7875 = (4.692 - 2.677) n

- 0.4054 = 2.0151 n			n = 0.2012

- C = 180 (14.54)0.2012 			C = 308.43

- For the tool life plot of Figure 17.4, show that the middle data point (v = 130 m/min, T = 12 min) is consistent with the Taylor equation determined in Example Problem 17.1.

- Solution: Taylor equation calculated in Example 17.1 is: vT0.223 = 229. Consistency would be demonstrated by using the values from the middle data point (T = 12 min at v = 130 ft/min) in the equation and obtaining the same value of C as above (C = 229).

- 130(12)0.223 = 130(1.7404) = 226.3

- This represents a difference of less than 1.2%, which is close enough and well within expected random variation in typical tool life data.

- In the tool wear plots of Figure 17.3, complete failure of the cutting tool is indicated by the end of each wear curve. Using complete failure as the criterion of tool life instead of 0.50 mm flank wear, the resulting data are: (1) v = 160 m/min, T = 5.75 min; (2) v = 130 m/min, T = 14.25 min; and (3) v = 100 m/min, T = 47 min. Determine the parameters n and C in the Taylor tool life equation for this data.

- Solution: Let us use the two extreme data points to calculate the values of n and C, then check the resulting equation against the middle data point.

- (1) 160(5.75)n = C  and (3) 100(47)n = C

- 160(5.75)n = 100(47)n

- ln 160 + n ln 5.75 = ln 100 + n ln 47

- 5.0752 + 1.7492 n = 4.6052 + 3.8501 n

- 0.4700 = 2.1009 n				n = 0.224

- (1) C = 160(5.75)0.224 = 236.7

- (3) C = 100(47)0.224 = 236.9		use average: C = 236.8

- Check against data set (2): 130(14.25)0.224 = 235.7. This represents a difference of less than 0.5%, which would be considered good agreement for experimental data. Better results on determining the Taylor equation would be obtained by using regression analysis on all three data sets to smooth the variations in the tool life data. Note that the n value is very close to the value obtained in Example 17.1 (n = 0.224 here vs. n = 0.223 in Example 17.1), and that the C value is higher here (C = 236.8 here vs. C = 229 in Example 17.1). The higher C value here reflects the higher wear level used to define tool life (complete failure of cutting edge here vs. a flank wear level of 0.50 mm in Example 17.1).

- A series of turning tests are performed to determine the parameters n, m, and K in the expanded version of the Taylor equation, Eq. (17.4). The following data were obtained during the tests: (1) cutting speed = 1.9 m/s, feed = 0.22 mm/rev, tool life = 10 min; (2) cutting speed = 1.3 m/s, feed = 0.22 mm/rev, tool life = 47 min; and (3) cutting speed = 1.9 m/s, feed = 0.32 mm/rev, tool life = 8 min. (a) Determine n, m, and K. (b) Using your equation, compute the tool life when the cutting speed is 1.5 m/s and the feed is 0.28 mm/rev.

- Solution: Three equations to be solved simultaneously:

- (1) (1.9 x 60)(10)n(0.22)m = K

- (2) (1.3 x 60)(47)n(0.22)m = K

- (3) (1.9 x 60)(8)n(0.32)m = K

- (1) and (2): ln 114 + n ln 10 + m ln 0.22 = ln 78 + n ln 47 + m ln 0.22

- ln 114 + n ln 10 = ln 78 + n ln 47

- 4.7362 + 2.3026 n = 4.3567 + 3.8501 n

- 0.3795 = 1.548 n				n = 0.245

- (1) and (3): ln 114 + 0.245 ln 10 + m ln 0.22 = ln 114 + 0.245 ln 8 + m ln 0.32

- 0.5646 + m (-1.5141) = 0.5099 + m (-1.1394)

- -0.3747 m = -0.0547			m = 0.146

- (1) K = 114(10)0..245(0.22)0.146 =114(1.7588)(0.8016) = K = 160.7

- (b) v = 1.5 m/s, f = 0.28 mm/rev

- (1.5 x 60)(T)0.245(0.28)0.146 = 160.7

- 90(T)0.245(0.8304) = 160.7

- (T)0.245 = 2.151

- T = 2.1511/0.245 = 22.7 min

- A drilling operation is performed in which 0.5 in diameter holes are drilled through cast iron plates that are 1.0 in thick. Sample holes have been drilled to determine the tool life at two cutting speeds. At 80 surface ft/min, the tool lasted for exactly 50 holes. At 120 surface ft/min, the tool lasted for exactly 5 holes. The feed of the drill was 0.003 in/rev. (Ignore effects of drill entrance and exit from the hole. Consider the depth of cut to be exactly 1.00 in, corresponding to the plate thickness.) Determine the values of n and C in the Taylor tool life equation for the above sample data, where cutting speed v is expressed in ft/min, and tool life T is expressed in min.

- Solution: (1) v = 80 ft/min, N = (80)/(0.5/12) = 611 rev/min

- feed rate fr = (0.003)(611) = 1.833 in/min

- time per hole Tm = 1.0 in/(1.833 in/min) = 0.545 min

- for 50 holes, T = 50(0.545 min) = 27.25 min

- Formulating the data as vTn = C, we have: 80(27.25)n = C

- (2) v = 120 ft/min, N = (120)/(.5/12) = 917 rev/min

- feed rate fr = (0.003)(917) = 2.75 in/min

- time per hole Tm = 1.0 in/(2.75 in/min) = 0.364 min

- for 5 holes, T = 5(0.364 min) = 1.82 min

- Formulating the data as vTn = C, we have: 120(1.82)n = C

- Setting (1) = (2): 80(27.25)n = 120(1.82)n

- ln 80 + n ln 27.25 = ln 120 + n ln 1.82

- 4.382 + 3.3051 n = 4.7875 + 0.5978 n

- 2.7073 n = 0.4055				n = 0.15

- C = 80(27.25)0.15 = 80(1.6417) = 131.34

- C = 120(1.82)0.15 = 120(1.094) = 131.29		C = 131.32

- The outside diameter of a cylinder made of titanium alloy is to be turned. The starting diameter is 400 mm and the length is 1100 mm. The feed is 0.35 mm/rev and the depth of cut is 2.5 mm. The cut will be made with a cemented carbide cutting tool whose Taylor tool life parameters are: n = 0.24 and C = 450. Units for the Taylor equation are min for tool life and m/min for cutting speed. Compute the cutting speed that will allow the tool life to be just equal to the cutting time for this part.

- Solution: In this problem we want Tm = T, where Tm = machining time per piece and T = tool life. Both of these times must be expressed in terms of cutting speed.

- Tm = DL/fv and T = (C/v)1/n

- Tm = (400)(1100)(10-6)/0.35(10-3)v = 3949/v = 3949 (v)-1

- T = (450/v)1/.24 = (450/v)4.1667 = 4504.1667(v)-4.1667 = 1135(108)(v)-4.1667

- Setting Tm = T: 3949 v-1 = 1135(108)(v)-4.1667

- v3.1667 = 0.2874(108)

- v = {0.2874(108)}1/3.1667 = {0.2874(108)}0.3158 = 226.6 m/min

- Check: Tm = 3949 (226.6)-1 = 17.4 min

- T = (450/226.6)1/.24 = (450/226.6)4.1667 = 17.4 min

- The workpart in a turning operation is 88 mm in diameter and 400 mm long. A feed of 0.25 mm/rev is used in the operation. If cutting speed = 3.5 m/s, the tool must be changed every 3 workparts; but if cutting speed = 2.5 m/s, the tool can be used to produce 20 pieces between tool changes. Determine the cutting speed that will allow the tool to be used for 50 parts between tool changes.

- Solution: (1) v = 3.5 m/s = 210 m/min

- Tm = (0.088 m)(0.4 m)/(210 m/min)(0.00025 m) = 2.106 min

- T = 3(2.106) = 6.32 min

- (2) v = 2.5 m/s = 150 m/min

- Tm = (0.088 m)(0.4 m)/(150 m/min)(0.00025 mm) = 2.949 min

- T = 20(2.949) = 58.98 min

- (1) 210(6.32)n = C

- (2) 150(58.98)n = C

- 210(6.32)n = 150(58.98)n

- ln 210 + n ln(6.32) = ln 150 + n ln(58.98)

- 5.347 + 1.844 n = 5.011 + 4.077 n

- 5.347 – 5.011 = (4.077 – 1.844) n

- 0.336 = 2.233 n			n = 0.150

- C = 210 (6.32)0.150 			C = 277.15

- Check: 150(58.98)0.150 = 277.03 ) Close enough. use C = 277.1

- Set T = 50 Tm

- vT0.15 = 277.1, T0.15 = 277.1/v, T = (277.1/v)1/0.15 = (277.1/v)6.646 = 1.711415(10)16/v6.646

- Tm = (0.088)(0.4)/0.00025 v = 442.34/v

- 1.711415(10)16/v6.646 = 50(442.34/v) = 22116.8/v

- 1.711415(10)16/v5.646 = 22116.8

- v5.646 = 1.711415(10)16/22116.8= 7.738075(10)11 = 773,807,500,000

- v = (773,807,500,000)1/5.646 = (773,807,500,000)0.177122 = 127.57 m/min

- Check: Tm = 442.34/127.57 = 3.468 min, 50 Tm = 173.4 min

- T = (277.1/127.57)6.646 = (2.172)6.646 = 173.3 min (Close enough!)

- The outside diameter of a cylinder made of a steel alloy is to be turned. The starting diameter is 300 mm and the length is 625 mm. The feed is 0.35 mm/rev and the depth of cut is 2.5 mm. The cut will be made with a cemented carbide cutting tool whose Taylor tool life parameters are: n = 0.24 and C = 450. Units for the Taylor equation are min for tool life and m/min for cutting speed. Compute the cutting speed that will allow the tool life to be just equal to the cutting time for three of these parts.

- Solution: In this problem we want 3Tm = T, where Tm = machining time per piece and T = tool life. Both of these times must be expressed in terms of cutting speed.

- Tm = DL/fv and T = (C/v)1/n

- Tm = (300)(625)(10-6)/0.35(10-3)v = 1683/v = 1683 (v)-1

- 3Tm = 3(1683 (v)-1) = 5049(v)-1

- T = (450/v)1/.24 = (450/v)4.1667 = 4504.1667(v)-4.1667 = 1135(108)(v)-4.1667

- Setting 3Tm = T: 5049v-1 = 1135(108)(v)-4.1667

- v3.1667 = 0.2248(108)

- v = {0.2248(108)}1/3.1667 = {0.2248(108)}0.3158 = 209.747 m/min

- Check: 3Tm = 5049 (209.747)-1 = 24.07 min

- T = (450/209.747)1/.24 = (450/209.747)4.1667 = 24.06 min (close enough)

- In a turning operation using high-speed steel tooling, cutting speed = 110 m/min. The Taylor tool life equation has parameters n = 0.140 and C = 150 (m/min) when the operation is conducted dry. When a coolant is used in the operation, the value of C is increased by 15%. Determine the percent increase in tool life that results if the cutting speed is maintained at 110 m/min.

- Solution: Dry: 110(T)0.14 = 150

- T = (150/110)1/.14 = (1.364)7.143 = 9.18 min

- With coolant: 110(T)0.14 = 150(1 + 15%) = 150(1.15) = 172.5

- T = (172.5/110)1/.14 = (1.568)7.143 = 24.85 min

- Increase = (24.85 – 9.18)/9.18 = 1.71 = 171%

- A production turning operation on a steel workpiece normally operates at a cutting speed of 125 ft/min using high-speed steel tooling with no cutting fluid. The appropriate n and C values in the Taylor equation are given in Table 17.2 in the text. It has been found that the use of a coolant type cutting fluid will allow an increase of 25 ft/min in the speed without any effect on tool life. If it can be assumed that the effect of the cutting fluid is simply to increase the constant C by 25, what would be the increase in tool life if the original cutting speed of 125 ft/min were used in the operation?

- Solution: From Table 17.2, n = 0.125 and C = 200 for dry cutting.

- With cutting fluid, C = 200 + 25 = 225.

- Dry: at v = 125 ft/min, T = (200/125)1/.125 = (1.6)8 = 42.95 min

- With cutting fluid: at v = 125 ft/min, T = (225/125)1/.125 = (1.8)8 = 110.2 min

- Increase = (110.2 - 42.95) = 67.25 min = 156.6%

- A machinability rating is to be determined for a new work material using the cutting speed for a 60-min tool life as the basis of comparison. For the base material (B1112 steel), test data resulted in Taylor equation parameter values of n = 0.29 and C = 500, where speed is in m/min and tool life is min. For the new material, the parameter values were n = 0.21 and C = 400. These results were obtained using cemented carbide tooling. (a) Compute a machinability rating for the new material. (b) Suppose the machinability criterion were the cutting speed for a 10-min tool life rather than the present criterion. Compute the machinability rating for this case. (c) What do the results of the two calculations show about the difficulties in machinability measurement?

- Solution: (a) Base material: v60 = 500/600.29 = 152.5 m/min

- New material: v60 = 400/600.21 = 169.3 m/min

- MR = 169.3/152.5 = 1.11 = 111%

- (b) Base material: v10 = 500/100.29 = 256.4 m/min

- New material: v10 = 400/100.21 = 246.6 m/min

- MR = 246.6/256.4 = 0.96 = 96%

- (c) Different test conditions often result in different machinability results.

- A machinability rating is to be determined for a new work material. For the base material (B1112), test data resulted in a Taylor equation with parameters n = 0.29 and C = 490. For the new material, the Taylor parameters were n = 0.23 and C = 430. Units in both cases are: speed in m/min and tool life in min. These results were obtained using cemented carbide tooling. (a) Compute a machinability rating for the new material using cutting speed for a 30-min tool life as the basis of comparison. (b) If the machinability criterion were tool life for a cutting speed of 150 m/min, what is the machinability rating for the new material?

- Solution: (a) Base material: v30 = 490/30.29 = 182.7 m/min

- New material: v30 = 430/30.23 = 196.7 m/min

- MR = 196.7/182.7 = 1.08 = 108%

- (b) Base material: T150 = (490/150)1/.29 = (3.27)3.448= 59.3 min

- New material: v10 = (430/150)1/.23 = (2.87)4.348 = 97.4 min

- MR = 97.4/59.3 = 1.64 = 164%

- A high-speed steel tool is used to turn a steel workpart that is 300 mm long and 80 mm in diameter. The parameters in the Taylor equation are: n = 0.13 and C = 75 (m/min) for a feed of 0.4 mm/rev. The operator and machine tool rate = $30.00/hr, and the tooling cost per cutting edge = $4.00. It takes 2.0 min to load and unload the workpart and 3.50 min to change tools. Determine (a) cutting speed for maximum production rate, (b) tool life in min of cutting, and (c) cycle time and cost per unit of product.

- Solution: (a) Co = $30/hr = $0.50/min

- vmax = 75/[(1/0.13 - 1)(3.5)].13 = 75/[6.692 x 3.5].27 = 49.8 m/min

- (b) Tmax = (75/49.8)1/.13 = (1.506)7.692 = 23.42 min

- (c) Tm = DL/fv = (80)(300)/(.4 x 49.8 x 103) = 3.787 min

- np = 23.42/3.787 = 6.184 pc/tool life		Use np = 6 pc/tool life

- Tc = Th + Tm + Tt/np = 2.0 + 3.787 + 3.5/6 = 6.37 min/pc.

- Cc = 0.50(6.37) + 4.00/6 = $3.85/pc

- Solve Problem 17.18 except that in part (a), determine cutting speed for minimum cost.

- Solution: (a) Co = $30/hr = $0.50/min

- vmin = 75[0.50/((1/0.13 - 1)(.50 x 3.5 + 4.00))].13 = 75[.50/(6.692 x 5.75)].13 = 42.6 m/min

- (b) Tmin = (75/42.6)1/.13 = (1.76)7.692 = 76.96 min

- (c) Tm = DL/fv = (80)(300)/(.4 x 42.6 x 103) = 4.42 min/pc.

- np = 76.96/4.42 = 17.41 pc/tool life		Use np = 17 pc/tool life

- Tc = Th + Tm + Tt/np = 2.0 + 4.42 + 3.5/17 = 6.63 min/pc.

- Cc = 0.50(6.63) + 4.0/17 = $3.55/pc

- A cemented carbide tool is used to turn a part with a length of 14.0 in and diameter = 4.0 in. The parameters in the Taylor equation are: n = 0.25 and C = 1000 (ft/min). The rate for the operator and machine tool = $45.00/hr, and the tooling cost per cutting edge = $2.50. It takes 2.5 min to load and unload the workpart and 1.50 min to change tools. The feed = 0.015 in/rev. Determine (a) cutting speed for maximum production rate, (b) tool life in min of cutting, and (c) cycle time and cost per unit of product.

- Solution: (a) vmax = C/((1/n-1)Tt)n = 1000/[(1/0.25 - 1)(1.5)].25

- = 1000/[(4.0-1) x 1.5].25 = 687 ft/min

- (b) Tmax = (1000/687)1/.25 = (1.456)4.0 = 4.5 min or (1/n -1) Tt = (4-1)1.5 = 4.5 min

- (c) Tm = DL/fv = (4)(14)/(.015 x 687 x 12) = 1.42 min

- np = 4.5/1.42 = 3.17 pc/tool		Use np = 3 pc/tool life

- Tc = Th + Tm + Tt/np = 2.5 + 1.42 + 1.5/3 = 4.42 min/pc.

- Co = $45/hr = $0.75/min

- Cc = Co (Th + Tm + Tt/np) + Ct/np = 0.75(4.42 ) + 2.5/3 = $4.15/pc

- Solve Problem 17.20 except that in part (a), determine cutting speed for minimum cost.

- Solution: (a) Co = $45/hr = $0.75/min

- vmin = C[(n/(1-n))(Co/(CoTt + Ct))]n = 1000[(0.25/(1-0.25))(0.75/(0.75(1.5) + 2.5))]0.25 =

- 1000[.3333*0.75/(1.125+2.5)].25 = 1000[ .333*0.75/3.625]0.25 = 1000 [ 0.06897]0.25 =  512 ft/min

- (b) Tmin = (1000/512)1/.25 = (1.953)4.0 = 14.55 min

- (c) Tm = DL/fv = (4)(14)/(0.015 x 512 x 12) = 1.91 min

- np = 14.55/1.91 = 7.62 pc/tool		Use np = 7 pc/tool life

- Tc = Th + Tm + Tt/np = 2.5 + 1.91 + 1.5/7 = 4.62 min/pc.

- Cc = Co (Th + Tm + Tt/np) + Ct/np = 0.75(4.62) + 2.5/7 = $3.83/pc

- Disposable and regrindable tooling are to be compared. The same grade of cemented carbide tooling is available in two forms for turning operations in a certain machine shop: disposable inserts and brazed inserts. The parameters in the Taylor equation for this grade are: n = 0.25 and C = 300 (m/min) under the cutting conditions considered here. For the disposable inserts, price of each insert = $6.00, there are four cutting edges per insert, and the tool change time = 1.0 min (this is an average of the time to index the insert and the time to replace it when all edges have been used). For the brazed insert, the price of the tool = $30.00 and it is estimated that it can be used a total of 15 times before it must be scrapped. The tool change time for the regrindable tooling = 3.0 min. The standard time to grind or regrind the cutting edge is 5.0 min, and the grinder is paid at a rate = $20.00/hr. Machine time on the lathe costs $24.00/hr. The workpart to be used in the comparison is 375 mm long and 62.5 mm in diameter, and it takes 2.0 min to load and unload the work. The feed = 0.30 mm/rev. For the two tooling cases, compare (a) cutting speeds for minimum cost, (b) tool lives, (c) cycle time and cost per unit of production. Which tool would you recommend?

- Solution: Disposable inserts: (a) Co = $24/hr = $0.40/min, Ct = $6/4 = $1.50/edge

- vmin = 300[0.40/((1/0.25 - 1)(0.40 x 1.0 + 1.50))].25 = 300[0.40/(3 x 1.9)].25 = 154.4 m/min

- (b) Tmin = (1/0.25 - 1)(0.4 + 1.5)/0.4 = 3(1.9/0.4) = 14.25 min

- (c) Tm = (62.5)(375)/(0.30)(10-3)(154.4) = 1.59 min/pc

- np = 14.25/1.59 = 8.96 pc/tool life	Use np = 8 pc/tool

- Tc = 2.0 + 1.59 + 1.0/8 = 3.72 min/pc.

- Cc = 0.40(3.72) + 1.50/8 = $1.674/pc

- Regrindable tooling: (a) Co = $24/hr = $0.40/min, Ct = $30/15 + 5($20/60) = $3.67/edge

- vmin = 300[0.40/((1/0.25 - 1)(0.40 x 3.0 + 3.67))].25 = 300[0.40/(3 x 4.87)].25 = 122.0 m/min

- (b) Tmin = (1/0.25 - 1)(0.4 x 3 + 3.67)/0.4 = 3(4.87/0.4) = 36.5 min

- (c) Tm = (62.5)(375)/(0.30)(10-3)(122) = 2.01 min/pc

- np = 36.5/2.01 = 18.16 pc/tool life	Use np = 18 pc/tool

- Tc = 2.0 + 2.01 + 3.0/18 = 4.18 min/pc

- Cc = 0.40(4.18) + 3.67/18 = $1.876/pc

- Disposable inserts are recommended. Cycle time and cost per piece are less.

- Solve Problem 17.22 except that in part (a), determine the cutting speeds for maximum production rate.

- Solution: Disposable inserts: (a) Co = $24/hr = $0.40/min, Ct = $6/4 = $1.50/edge

- vmax = 300[1.0/((1/0.25 - 1)(1.0)].25 = 300[1.0/(3 x 1.0)].25 = 228.0 m/min

- (b) Tmax = (1/0.25 - 1)(1.0) = 3(1.0) = 3.0 min

- (c) Tm = (62.5)(375)/(0.30)(10-3)(228) = 1.08 min/pc

- np = 3.0/1.08 = 2.78 pc/tool life		Use np = 2 pc/tool

- Tc = 2.0 + 1.08 + 1.0/2 = 3.58 min/pc.

- Cc = 0.40(3.58) + 1.50/2 = $2.182/pc

- Regrindable tooling: (a) Co = $24/hr = $0.40/min, Ct = $30/15 + 5($20/60) = $3.67/edge

- vmax = 300[1.0/((1/0.25 - 1)(3.0))].25 = 300[1.0/(3 x 3.0)].25 = 173.2 m/min

- (b) Tmax = (1/0.25 - 1)(3) = 3(3.0) = 9.0 min

- (c) Tm = (62.5)(375)/(0.30)(10-3)(173.2) = 1.42 min/pc

- np = 9.0/1.42 = 6.34 pc/tool life		Use np = 6 pc/tool

- Tc = 2.0 + 1.42 + 3.0/6 = 3.92 min/pc.

- Cc = 0.40(3.92) + 3.67/6 = $2.180/pc

- Disposable inserts are recommended. Cycle time and cost per piece are less. Comparing the results in this problem with those of the previous problem, note that with the maximum production rate objective in the current problem, cycle times are less, but that unit costs are less in the previous problem where the objective is minimum cost per piece.

- Three tool materials are to be compared for the same finish turning operation on a batch of 150 steel parts: high-speed steel, cemented carbide, and ceramic. For the high-speed steel tool, the Taylor equation parameters are: n = 0.130 and C = 80 (m/min). The price of the HSS tool is $20.00 and it is estimated that it can be ground and reground 15 times at a cost of $2.00 per grind. Tool change time is 3 min. Both carbide and ceramic tools are in insert form and can be held in the same mechanical toolholder. The Taylor equation parameters for the cemented carbide are: n = 0.30 and C = 650 (m/min); and for the ceramic: n = 0.6 and C = 3,500 (m/min). The cost per insert for the carbide is $8.00 and for the ceramic is $10.00. There are 6 cutting edges per insert in both cases. Tool change time is 1.0 min for both tools. The time to change a part is 2.5 min. The feed is 0.30 mm/rev, and depth of cut is 3.5 mm. The cost of machine time is $40/hr. The part is 73.0 mm in diameter and 250 mm in length. Setup time for the batch is 2.0 hr. For the three tooling cases, compare: (a) cutting speeds for minimum cost, (b) tool lives, (c) cycle time, (d) cost per production unit, (e) total time to complete the batch and production rate. (f) What is the proportion of time spent actually cutting metal for each tooling? Use of a spreadsheet calculator is recommended.

- Solution: HSS tooling: (a) Ct = $20/15 + 2.00 = $3.33/edge. Co = $40/hr = $0.667/min

- vmin = 80[0.667/((1/.13 - 1)(0.667 x 3.0 + 3.33))].130 =  47.7 m/min

- (b) Tmin = (1/.13 - 1)(0.667 x 3 + 3.33)/0.667 = 6.69(5.33/.667) = 53.4 min

- (c) Tm = (73)(250(10-6))/(0.30(10-3)47.7) = 4.01min/pc

- np = 53.4/4.01 = 13.3 pc/tool life		Use np = 13 pc/tool life

- Tc = 2.5 + 4.01 + 3.0/13 = 6.74 min/pc.

- (d) Cc = 0.667(6.74) + 3.33/13 = $4.75/pc

- (e) Time to complete batch = 2.5(60) + 150(6.74) = 1161 min = 19.35 hr.

- Production rate Rp = 100 pc/13.8 hr = 7.75 pc/hr.

- (f) Proportion of time spent cutting = 100(4.81)/828 = 0.518 = 51.8%

- Cemented carbide tooling: (a) Ct = $8/6 = $1.33/edge. Co = $40/hr = $0.667/min

- vmin = 650[0.667/((1/.30 - 1)(0.667 x 1.0 + 1.333))].30 =  363 m/min

- (b) Tmin = (1/.30 - 1)(0.667 x 1 + 1.333)/0.667 = 2.333(2.0/0.667) = 7 min

- (c) Tm = (73)(250(10-6))/(0.30(10-3)363) = 0.53 min/pc

- np = 7/0.53 = 13.2 pc/tool life		Use np = 13 pc/tool life

- Tc = 2.5 + 0.53 + 1.0/13 = 3.11 min/pc.

- (d) Cc = 0.667(3.11) + 1.333/13 = $2.18/pc

- (e) Time to complete batch = 2.5(60) + 150(3.11) = 616.5 min = 10.28 hr.

- Production rate Rp = 150 pc/10.28 hr = 14.59 pc/hr.

- (f) Proportion of time spent cutting = 150(0.53)/616.5 = 0.129 = 12.9%

- Ceramic tooling: (a) Ct = $10/6 = $1.67/edge. Co = $40/hr = $0.667/min

- vmin = 3,500[0.667/((1/.6 - 1)(0.667 x 1.0 + 1.67))].6 = 2105 m/min

- (b) Tmin = (1/0.6 - 1)(0.667 x 1 + 1.67)/0.667 = 0.667(2.33/0.667) = 2.33 min

- (c) Tm = (73)(250(10-6))/(0.30(10-3)2105) = 0.091 min/pc

- np = 2.33/0.091 = 25.6 pc/tool life	Use np = 25 pc/tool life

- Tc = 2.5 + 0.091 + 1.0/25 = 2.63 min/pc.

- (d) Cc = 0.667(2.63) + 1.67/25 = $1.82/pc

- (e) Time to complete batch = 2.5(60) + 150(2.63) = 544 min = 9.08 hr.

- Production rate Rp = 150 pc/9.08 hr = 16.52 pc/hr.

- (f) Proportion of time spent cutting = 150(0.091)/544 = 0.025 = 2.5%

- Comment: One might conclude that such a low proportion of time spent cutting would argue against the use of the calculated cutting speed for ceramic tooling. However, note that ceramic tooling provides a significant advantage in terms of unit cost, batch time, and production rate compared to HSS tooling and even carbide tooling. The very small cutting time Tm and resulting low proportion of time spent cutting for ceramic tooling focuses attention on the nonproductive work elements in the batch time, specifically, setup time and workpart handling time; and puts pressure on management to seek ways to reduce these nonproductive elements.

- Solve Problem 17.24 except that in parts (a) and (b), determine the cutting speeds and tool lives for maximum production rate. Use of a spreadsheet calculator is recommended.

- Solution: HSS tooling: (a) Ct = $20/15 + 2.00 = $3.33/edge. Co = $40/hr = $0.667/min

- vmax = 80/[(1/.13 - 1)(3.0)].130 = 80/[6.69 x 3)].130 = 54 m/min

- (b) Tmax = (1/0.13 - 1)(3) = 6.69(3) = 20.0 min

- (c) Tm = (73)(250(10-6))/(0.30(10-3)54) = 3.53 min/pc

- np = 20.0/3.53 = 5.66 pc/tool life		Use np = 5 pc/tool life

- Tc = 2.5 + 3.53 + 3.0/5 = 6.63 min/pc.

- (d) Cc = 0.667(6.63) + 3.33/5 = $5.09/pc

- (e) Time to complete batch = 2.5(60) + 150(6.63) = 1144.5 min = 19.08 hr.

- Production rate Rp = 150 pc/19.08 hr = 7.86 pc/hr.

- (f) Proportion of time spent cutting = 150(3.53)/1144.5 = 0.463 = 46.3%

- Cemented carbide tooling: (a) Ct = $8/6 = $1.33/edge. Co = $40/hr = $0.667/min

- vmax = 650/[(1/.30 - 1)(1.0)].30 = 650/[(2.33 x 1.0)].30 = 504 m/min

- (b) Tmax = (1/0.30 - 1)(1.0) = 2.33(1.0) = 2.33 min

- (c) Tm = (73)(250(10-6))/(0.30(10-3)504) = 0.38 min/pc

- np = 2.33/0.38 = 6.13 pc/tool life		Use np = 6 pc/tool life

- Tc = 2.5 + 0.38 + 1.0/6 = 3.05 min/pc.

- (d) Cc = 0.667(3.05) + 1.33/6 = $2.25/pc

- (e) Time to complete batch = 2.5(60) + 150(3.05) = 607 min = 10.12 hr.

- Production rate Rp = 150 pc/10.12 hr = 14.82 pc/hr.

- (f) Proportion of time spent cutting = 150(0.38)/607 = 0.094 = 9.4%

- Ceramic tooling: (a) Ct = $10/6 = $1.67/edge. Co = $40/hr = $0.667/min

- vmax = 3,500/[(1/.6 - 1)(1.0)].6 = 3,500/[.667 x 1.0].6 = 4464 m/min

- (b) Tmax = (1/0.6 - 1)(1) = 0.667(1) = .667 min

- (c) Tm = (73)(250(10-6))/(0.30(10-3)4464) = 0.043 min/pc

- np = 0.667/0.043 = 15.58 pc/tool life	Use np = 15 pc/tool life

- Tc = 2.5 + 0.043 + 1.0/15 = 2.61 min/pc.

- (d) Cc = 0.667(2.61) + 1.67/15 = $1.85/pc

- (e) Time to complete batch = 2.5(60) + 150(2.61) = 541 min = 9.02 hr.

- Production rate Rp = 150 pc/9.02 hr = 16.63 pc/hr.

- (f) Proportion of time spent cutting = 150(0.043)/541 = 0.012 = 1.2%

- Comment: One might conclude that such a low proportion of time spent cutting would argue against the use of the calculated cutting speed for ceramic tooling. However, note that ceramic tooling provides a significant advantage in terms of unit cost, batch time, and production rate compared to HSS tooling and even carbide tooling. The very small cutting time Tm and resulting low proportion of time spent cutting for ceramic tooling focuses attention on the nonproductive work elements in the batch time, specifically, setup time and workpart handling time; and puts pressure on management to seek ways to reduce these nonproductive elements.

- A vertical boring mill is used to bore the inside diameter of a large batch of tube-shaped parts. The diameter = 28.0 in and the length of the bore = 14.0 in. Current cutting conditions are: speed = 200 ft/min, feed = 0.015 in/rev, and depth = 0.125 in. The parameters of the Taylor equation for the cutting tool in the operation are: n = 0.23 and C = 850 (ft/min). Tool change time = 3.0 min, and tooling cost = $3.50 per cutting edge. The time required to load and unload the parts = 12.0 min, and the cost of machine time on this boring mill = $42.00/hr. Management has decreed that the production rate must be increased by 25%. Is that possible? Assume that feed must remain unchanged in order to achieve the required surface finish. What is the current production rate and the maximum possible production rate for this job?

- Solution: At the current operating speed v = 200 ft/min:

- T = (850/200)1/.23 = 540 min

- Tm = (28)(14)/(200 x 12 x 0.015) = 34.2 min/pc

- np = 540/34.2 = 15 pc/tool life

- Tc = 12 + 34.2 + 3/15 = 46.4 min

- Rc = 60/46.4 = 1.293 pc/hr

- Find vmax to compare with current operating speed.

- vmax = 850/[(1/.23 - 1)(3.0)].23 = 850/[(3.348 x 3.0)].23 = 500 ft/min

- Tmax = (1/.23 - 1)(3.0) = 3.348(3.0) = 10.0 min

- Tm = (28)(14)/(500 x 12 x 0.015) = 13.7 min/pc

- np = 10/13.7 = 0.73 pc/tool life

- Tc = 12 + 13.7 + 3/.73 = 29.8 min

- Rc = 60/29.8 = 2.01 pc/hr

- This is a 56% increase in production rate relative to the 200 ft/min cutting speed.

- As indicated in Section 17.4, the effect of a cutting fluid is to increase the value of C in the Taylor tool life equation. In a certain machining situation using HSS tooling, the C value is increased from C = 200 to C = 225 due to the use of the cutting fluid. The n value is the same with or without fluid at n = 0.125. Cutting speed used in the operation is v = 125 ft/min. Feed = 0.010 in/rev and depth = 0.100 in. The effect of the cutting fluid can be to either increase cutting speed (at the same tool life) or increase tool life (at the same cutting speed). (a) What is the cutting speed that would result from using the cutting fluid if tool life remains the same as with no fluid? (b) What is the tool life that would result if the cutting speed remained at 125 ft/min? (c) Economically, which effect is better, given that tooling cost = $2.00 per cutting edge, tool change time = 2.5 min, and operator and machine rate = $30/hr? Justify you answer with calculations, using cost per cubic in of metal machined as the criterion of comparison. Ignore effects of workpart handling time.

- Solution: Cutting dry, the Taylor tool life equation parameters are n = 0.125 and C = 200.

- At v = 125 ft/min, tool life T = (200/125)1/.125 = (1.6)8 = 43 min

- With a cutting fluid, the Taylor tool life equation parameters are n = 0.125 and C = 225.

- The corresponding cutting speed for a 43 min tool life v = 225/430.125 = 140.6 ft/min

- (b) Cutting at v = 125 ft/min with a cutting fluid gives a tool life T = (225/125)8.0 = 110 min

- (c) Which is better, (1) cutting at a speed of 140.6 ft/min to give a 43 min tool life, or (2) cutting at 125 ft/min to give a 110 min tool life. Use 1.0 in3 of metal cut as the basis of comparison, with cost and time parameters as follows: Ct = $2.00/cutting edge, Tt = 2.5 min, and Co = $30/hr = $0.50/min

- (1) At v =140.6 ft/min, Tm = 1.0 in3/RMR = 1.0/(140.6 x 12 x 0.010 x 0.100) = 0.5927 min

- For T = 43 min, volume cut per tool life = 43/0.5927 = 72.5 in3 between tool changes.

- Ignoring work handling time, cost/in3 = 0.50(.5927) + (0.50 x 2.5 + 2.00)/72.5 = $0.341/in3.

- (2) At 125 ft/min, Tm = 1.0 in3/RMR = 1.0/(125 x 12 x 0.010 x 0.100) = 0.6667 min

- For T = 110 min, volume cut per tool life = 110/0.6667 = 164.9 in3 between tool changes.

- Ignoring work handling time, cost/in3 = 0.50(.6667) + (0.50 x 2.5 + 2.00)/164.9 = $0.353/in3.

- Conclusion: it is better to take the benefit of a cutting fluid in the form of increased cutting speed.