23 WELDING PROCESSES

# Review Questions

- Name the principal groups of processes included in fusion welding.

- Answer. The principal groups of processes included in fusion welding are (1) arc welding, (2) resistance welding, (3) oxyfuel welding, and (4) other. The “other” category includes EBW, LBW, thermit welding, and others.

- What is the fundamental feature that distinguishes fusion welding from solid-state welding?

- Answer. In fusion welding, melting occurs at the faying surfaces; in solid state welding, no melting occurs.

- Define what an electrical arc is.

- Answer. An electrical arc is a discharge across a gap in a circuit. In arc welding, the arc is sustained by a thermally ionized column of gas through which the current flows.

- What do the terms arc-on time and arc time mean?

- Answer. The two terms mean the same thing: the proportion of the total time in a shift that the arc is actually on, indicating that welding is occurring.

- Electrodes in arc welding are divided into two categories. Name and define the two types.

- Answer. The two categories are consumable and nonconsumable. The consumable type, in addition to being the electrode for the process, also provides filler metal for the welding joint. The nonconsumable type is made of materials that resist melting, such as tungsten or carbon.

- What are the two basic methods of arc shielding?

- Answer. (1) Shielding gas, such as argon and helium; and (2) flux, which covers the welding operation and protects the molten pool from the atmosphere.

- Why is the heat transfer factor in arc-welding processes that utilize consumable electrodes greater than in those that use nonconsumable electrodes?

- Answer. Because molten metal from the electrode is transferred across the arc and contributes to the heating of the molten weld pool in arc-welding processes that utilize consumable electrodes.

- Describe the shielded metal arc-welding (SMAW) process.

- Answer. SMAW is an arc-welding process that uses a consumable electrode consisting of a filler metal rod coated with chemicals that provide flux and shielding.

- Why is the shielded metal arc-welding (SMAW) process difficult to automate?

- Answer. Because the stick electrodes used in SMAW must be changed frequently, which would be difficult to do automatically. It is much easier to automate the feeding of continuous filler wire, such as in GMAW, FCAW, SAW, or GTAW.

- Describe submerged arc welding (SAW).

- Answer. SAW is an arc-welding process that uses a continuous, consumable bare wire electrode, and arc shielding is provided by a cover of granular flux.

- Why are the temperatures much higher in plasma arc welding than in other AW processes?

- Answer. Because the arc is restricted in diameter, thus concentrating the energy into a smaller area, resulting in much higher power densities.

- Define resistance welding.

- Answer. RW consists of a group of fusion welding processes that utilize a combination of heat and pressure to accomplish coalescence of the two faying surfaces. Most prominent in the group is resistance spot welding.

- Describe the sequence of steps in the cycle of a resistance spot-welding operation.

- Answer. The steps are (1) insert parts between electrodes, (2) squeeze parts between the electrodes, (3) weld, in which the current is switched on for a brief duration (0.1 to 0.4 sec), (4) hold, during which the weld nugget solidifies, and (5) open electrodes and remove parts.

- What is resistance-projection welding?

- Answer. RPW is a resistance welding process in which coalescence occurs at one or more relatively small points on the parts; the contact points are designed into the geometry of the parts as embossments or projections.

- Describe cross-wire welding.

- Answer. Cross-wire welding is a form of resistance projection welding used to fabricate welded wire products such as shopping carts and stove grills.

- Why is the oxyacetylene welding process favored over the other oxyfuel welding processes?

- Answer. Because acetylene and oxygen burn hotter than other oxyfuels.

- Electron-beam welding has a significant disadvantage in high-production applications. What is that disadvantage?

- Answer. EBW is usually carried out in a vacuum for a high quality weld. The time to draw the vacuum adds significantly to the production cycle time.

- Laser-beam welding and electron-beam welding are often compared because they both produce very high power densities. LBW has certain advantages over EBW. What are they?

- Answer. Advantages of LBW over EBW are (1) no vacuum chamber is required in LBM, (2) no x-rays are emitted in LBM; and (3) the laser beam can be focused and directed with conventional optical mirrors and lenses.

- There are several modern-day variations of forge welding, the original welding process. Name them.

- Answer. Variations of forge welding are (1) cold welding, (2) roll welding, (3) and hot pressure welding.

- What is friction stir welding (FSW), and how is it different from friction welding?

- Answer. Friction stir welding (FSW) is a solid state welding process in which a rotating tool is fed along the joint line between two workpieces, generating friction heat and mechanically stirring the metal to form the weld seam. FSW is distinguished from conventional friction welding (FRW) by the fact that friction heat is generated by a separate wear-resistant tool rather than by the parts themselves.

- What is a sonotrode in ultrasonic welding?

- Answer. It is the actuator which is attached to one of the two parts to be welded with USW and which provides the oscillatory motion that results in coalescence of the two surfaces. It is analogous to an electrode in resistance welding.

- Distortion (warping) is a serious problem in fusion welding, particularly arc welding. What are some of the techniques that can be taken to reduce the incidence and extent of distortion?

Answer. The following techniques can be used to reduce warping in arc welding: (1) Welding fixtures can be used to physically restrain movement of the parts during welding. (2) Heat sinks can be used to rapidly remove heat from sections of the welded parts to reduce distortion. (3) Tack welding at multiple points along the joint can create a rigid structure prior to continuous seam welding. (4) Welding conditions (speed, amount of filler metal used, etc.) can be selected to reduce warping. (5) The base parts can be preheated to reduce the level of thermal stresses experienced by the parts. (6) Stress relief heat treatment can be performed on the welded assembly, either in a furnace for small weldments, or using methods that can be used in the field for large structures. (7) Proper design of the weldment itself can reduce the degree of warping.

- What are some of the important welding defects?

- Answer. Some of the important welding defects are (1) cracks, (2) cavities, (3) solid inclusions, (4) incomplete fusion, and (5) imperfect shape or contour of weld cross section.

- What are the three basic categories of inspection and testing techniques used for weldments?  Name some typical inspections and/or tests in each category.

- Answer. The three categories are: (1) visual inspection, which includes dimensional checks and inspection for warping, cracks, and other visible defects; (2) nondestructive evaluation, which includes dye-penetrant, magnetic particle, ultrasonic, and radiographic tests; and (3) destructive tests, which includes conventional mechanical and metallurgical tests adapted to weld joints.

- What are some of the design guidelines for weldments that are fabricated by arc welding?

Answer. The guidelines for weldments by arc welding include (1) Good fit-up of parts to be welded is important to maintain dimensional control and minimize distortion. Machining is sometimes required to achieve satisfactory fit-up. (2) The design of the assembly must provide access room to allow the welding gun to reach the welding area. (3) Whenever possible, design of the assembly should allow flat welding to be performed, as opposed to horizontal, vertical, or overhead arc welding positions.

# Problems

- A shielded metal arc-welding operation is performed on steel at a voltage = 30 volts and a current = 225 amps. The heat transfer factor = 0.90 and melting factor = 0.75. The unit melting energy for steel = 10.2 J/mm3. Determine (a) the rate of heat generation at the weld and (b) the volume rate of metal welded.

- Solution: (a) RHW = f1f2EI = (0.90)(0.75)(30)(225) = 4556 W

- (b) RWV = (4556 W)/(10.2 J/mm3) = 447 mm3/sec.

- A GTAW operation is performed on low carbon steel, whose unit melting energy is 10.3 J/mm3. The welding voltage is 22 volts and the current is 135 amps. The heat transfer factor is 0.7 and the melting factor is 0.65. If filler metal wire of 3.5 mm diameter is added to the operation, the final weld bead is composed of 60% volume of filler and 40% volume base metal. If the travel speed in the operation is 5 mm/sec, determine (a) cross-sectional area of the weld bead, and (b) the feed rate (mm/sec) at which the filler wire must be supplied.

- Solution: (a) RHW = f1f2EI = UmAwv

- Aw = f1f2EI/(Umv) = 0.7(0.65)(22)(135)/(10.3x5.0) = 26.24 mm2

- (b) Volume of weld = Awv = 26.24(5.0) = 131.2 mm3/s

- Filler wire A = D2/4 = (3.5)2/4 = 9.62 mm2

- At 60% filler metal, feed rate of filler wire = 131.2(0.60)/9.62 = 8.18 mm/s

- A flux-cored arc-welding operation is performed to butt weld two austenitic stainless steel plates together. The welding voltage is 21 volts and the current is 185 amps. The cross-sectional area of the weld seam = 75 mm2 and the melting factor of the stainless steel is assumed to be 0.60. Using tabular data and equations given in this and the preceding chapter, determine the likely value for travel speed v in the operation.

- Solution: From Table 23.1, f1 = 0.9 for FCAW.

From Table 22.2, Tm = 1670K for austenitic stainless steel.

Um = 3.33 x 10-6 (1670)2 = 9.29 J/mm3

f1f2EI = UmAwv

v = f1f2EI/UmAw = 0.9(0.6)(21)(185)/(9.29 x 75) = 3.01 mm/s

- A gas metal arc-welding test is performed to determine the value of melting factor f2 for a certain metal and operation. The welding voltage = 25 volts, current = 125 amps, and heat transfer factor is assumed to be = 0.90, a typical value for GMAW. The rate at which the filler metal is added to the weld is 0.50 in3 per minute, and measurements indicate that the final weld bead consists of 57% filler metal and 43% base metal. The unit melting energy for the metal is known to be 75 Btu/in3. (a) Find the melting factor. (b) What is the travel speed if the cross-sectional area of the weld bead = 0.05 in2?

- Solution: (a) f1f2EI = UmAwv

- Awv = welding volume rate = RWV = (0.50 in3/min)/0.57 = 0.877 in3/min = 0.01462 in3/sec.

- Therefore, f1f2EI = Um(RWV)

- 1 Btu/sec = 1055 J/s = 1055 W, so 75 Btu/sec = 79,125 W

- f2 = Um(RWV)/f1EI = 79,125(0.01462)/(0.9 x 25 x 125) = 0.41

- (b) Given that Aw = 0.05 in2, v = (RWV)/Aw = 0.877/0.05 = 17.54 in/min

- A continuous weld is to be made around the circumference of a round steel tube of diameter = 6.0 ft, using a submerged arc welding operation under automatic control at a voltage of 25 volts and current of 300 amps. The tube is slowly rotated under a stationary welding head. The heat transfer factor for SAW is = 0.95 and the assumed melting factor = 0.7. The cross-sectional area of the weld bead is 0.12 in2. If the unit melting energy for the steel = 150 Btu/in3, determine (a) the rotational speed of the tube and (b) the time required to complete the weld.

Solution: (a) f1f2EI = UmAwv

v = f1f2EI/UmAw

1 Btu/sec = 1055 J/s = 1055 W, so 150 Btu/sec = 158,250 W

v = 0.95(0.7)(25)(300)/(158,250 x 0.120) = 0.263 in/sec = 15.76 in/min

Circumference C = D = 12 x 6 = 226.2 in/rev.

Rotational speed N = (15.76 in/min)/(226.2 in/rev) = 0.06967 rev/min

(b) Time to weld around circumference = C/v = (226.2 in/rev)/(15.76 in/min) = 14.35 min

- An RSW operation is used to make a series of spot welds between two pieces of aluminum, each 2.0 mm thick. The unit melting energy for aluminum = 2.90 J/mm3. Welding current = 6,000 amps, and time duration = 0.15 sec. Assume that the resistance = 75 micro-ohms. The resulting weld nugget measures 5.0 mm in diameter by 2.5 mm thick. How much of the total energy generated is used to form the weld nugget?

- Solution: H = I2Rt = (6000)2(75 x 10-6)(0.15) = 405 W-sec = 405 J

- Weld nugget volume V = D2d/4 = (5)2(2.5)/4 = 49.1 mm3

- Heat required for melting = UmV = (2.9 J/mm3)(49.1 mm3) = 142.4 J

- Proportion of heat for welding =142.4/405 = 0.351 = 35.1%

- The unit melting energy for a certain sheet metal is 9.5 J/mm3. Thickness of each of the two sheets to be spot welded is 3.5 mm. To achieve required strength, it is desired to form a weld nugget that is 5.5 mm in diameter and 5.0 mm thick. The weld duration will be set at 0.3 sec. If it is assumed that the electrical resistance between the surfaces is 140 micro-ohms, and that only one-third of the electrical energy generated will be used to form the weld nugget (the rest being dissipated), determine the minimum current level required in this operation.

- Solution: Hm = UmV

- V = D2d/4 = (5.5)2(5.0)/4 = 118.8 mm3

- Hw = 9.5(118.8) = 1129 J

- Required heat for the RSW operation H = 1129/(1/3) = 3386 J

- H = I2Rt = I2(140 x 10-6)(0.3) = 42 x 10-6 I2 = 3386 J

- I2 = 3386/(42 x 10-6) = 80.6 x 106 A2

- I = 8.98 x 103 = 8,980 A

- A resistance spot-welding operation is performed on two pieces of 0.040 in thick sheet steel (low carbon). The unit melting energy for steel = 150 Btu/in3. Current = 9500 A and time duration = 0.17 sec. This results in a weld nugget of diameter = 0.19 in and thickness = 0.060 in. Assume the resistance = 100 micro-ohms. Determine (a) the average power density in the interface area defined by the weld nugget, and (b) the proportion of energy generated that went into formation of the weld nugget.

- Solution: (a) PD = I2R/A

- A = D2/4 = (0.19)2/4 = 0.02835 in2

- I2R = (9500)2 (100 x 10-6) = 9025 W

- 1 Btu/sec = 1055 W, so 9025 W = 8.554 Btu/sec

- PD = 8.554/0.02835 = 302 Btu/sec-in2

- (b) H = I2Rt = (9500)2 (100 x 10-6)(0.17) = 1534 W-sec = 1.454 Btu

- Weld nugget volume V = D2d/4 = (0.19)2(0.060)/4 = 0.0017 in3

- Heat required for melting = UmV = (150 Btu/in3)(0.0017) = 0.255 Btu

- Proportion of heat for welding = 0.255/1.454 = 0.175 = 17.5%

- A resistance seam-welding operation is performed on two pieces of 2.5-mm-thick austenitic stainless steel to fabricate a container. The weld current in the operation is 10,000 amps, the weld duration = 0.3 sec, and the resistance at the interface is 75 micro-ohms. Continuous motion welding is used, with 200-mm-diameter electrode wheels. The individual weld nuggets formed in this RSEW operation have diameter = 6 mm and thickness = 3 mm (assume the weld nuggets are disc-shaped). These weld nuggets must be contiguous to form a sealed seam. The power unit driving the process requires an off-time between spot welds of 1.0 s. Given these conditions, determine (a) the unit melting energy of stainless steel using the methods of the previous chapter, (b) the proportion of energy generated that goes into the formation of each weld nugget, and (c) the rotational speed of the electrode wheels.

- Solution: (a) From Table 29.2, Tm = 1670K for austenitic stainless steel.

- Um = 3.33 x 10-6 (1670)2 = 9.29 J/mm3.

- (b) Hw = UmV

- V = D2d/4 = (6.0)2(3.0)/4 = 84.82 mm3

- Hw = (9.29 J/mm3)(84.82 mm3) = 788 J

- H = I2Rt = (10,000)2(75 x 10-6)(0.3) = 2225 J

- Proportion of heat for welding =788/2225= 0.354 = 35.4%

- (c) Total cycle time per weld Tc = 0.3 + 1.0 = 1.3 sec.

- Distance moved per spot weld in order to have contiguous spot welds for the seam = D = 0.6 mm.

- Therefore, surface speed of electrode wheel v = 6.00 mm/1.3 sec = 4.61 mm/s = 276.9 mm/min.

- N = v/D = (276.9 mm/min)/(200 mm/rev) = 0.441 rev/min

- The voltage in an EBW operation is 45 kV. The beam current is 60 milliamp. The electron beam is focused on a circular area that is 0.25 mm in diameter. The heat transfer factor is 0.87. Calculate the average power density in the area in watt/mm2.

- Solution: Power density PD = f1EI/A

- Power P = f1EI = 0.87(45 x 103)(60 x 10-3) = 2349 W

- Area A = D2/4 = (0.25)2/4 = 0.0491 mm3

- PD = 2349/0.0491 = 47,853 W/mm2

- An electron-beam welding operation is to be accomplished to butt weld two sheet-metal parts that are 3.0 mm thick. The unit melting energy = 5.0 J/mm3. The weld joint is to be 0.35 mm wide, so that the cross section of the fused metal is 0.35 mm by 3.0 mm. If accelerating voltage = 25 kV, beam current = 30 milliamp, heat transfer factor f1 = 0.85, and melting factor f2 = 0.75, determine the travel speed at which this weld can be made along the seam.

- Solution: Available heat for welding RHW = f1f2EI = UmAwv

- Travel velocity v = f1f2EI/UmAw

- Cross sectional area of weld seam Aw = (0.35)(3.0) = 1.05 mm2

- v = 0.85(0.75)(25 x 103)(30 x 10-3)/(5.0 x 1.05) = 91.05 mm/s

- An electron-beam welding operation uses the following process parameters: accelerating voltage = 25 kV, beam current = 100 milliamp, and the circular area on which the beam is focused has a diameter = 0.020 in. If the heat transfer factor = 90%, determine the average power density in the area in Btu/sec in2.

Solution: Power density PD = f1EI/A

Area in which beam is focused A = D2/4 = (0.020)2/4 = 0.000314 in3

Power P = 0.90(25 x 103)(100 x 10-3)/1055 = 2.133 Btu/sec

PD = 2.133/0.000314 = 6792 Btu/sec-in2