12 FUNDAMENTALS OF METAL FORMING

# Review Questions

- What are the differences between bulk deformation processes and sheet metal processes?

- Answer. In bulk deformation, the shape changes are significant, and the workparts have a low area-to-volume ratio. In sheet metal processes, the area-to-volume ratio is high.

- Extrusion is a fundamental shaping process. Describe it.

- Answer. Extrusion is a compression process in which the work material is forced to flow through a die orifice, thereby forcing its cross section to assume the profile of the orifice.

- Why is the term pressworking often used for sheet metal processes?

- Answer. The term pressworking is used because most sheet metal operations are performed on presses.

- What is the difference between deep drawing and bar drawing?

- Answer. Deep drawing is a sheet metal forming process used to fabricate cup-shaped parts; bar drawing is a bulk deformation process used to reduce the diameter of a cylindrical workpart.

- Indicate the mathematical equation for the flow curve.

- Answer. The flow curve is defined in Eq. (12.1) as Yf = Kn.

- How does increasing temperature affect the parameters in the flow curve equation?

- Answer. Increasing temperature decreases both K and n in the flow curve equation.

- Indicate some of the advantages of cold working relative to warm and hot working.

- Answer. Advantages of cold working are (1) better accuracy, (2) better surface finish, (3) increased strength due to work hardening, (4) possible directional properties due to grain flow, and (5) no heating of work required.

- What is isothermal forming?

- Answer. An isothermal forming operation is performed in such a way as to eliminate surface cooling and thermal gradients in the workpart. This is accomplished by preheating the forming tools that contact the workpart.

- Why is friction generally undesirable in metal forming operations?

- Answer. Reasons why friction is undesirable in metal forming include the following: (1) it inhibits metal flow during deformation, causing residual stresses and product defects; (2) it increases forces and power required; and (3) it increases wearing of the tools.

- What is sticking friction in metalworking?

Answer. Sticking friction is when the work surface adheres to the surface of the tool rather than slides against it; it occurs when the friction stress is greater than the shear flow stress of the metal.

Problems

- The strength coefficient = 550 MPa and strain-hardening exponent = 0.22 for a certain metal. During a forming operation, the final true strain that the metal experiences = 0.85. Determine the flow stress at this strain and the average flow stress that the metal experienced during the operation.

- Solution: Flow stress Yf = 550(0.85)0.22 = 531 MPa.

- Average flow stress Yf= 550(0.85)0.22/1.22 = 435 MPa.

- A metal has a flow curve with strength coefficient = 850 MPa and strain-hardening exponent = 0.30. A tensile specimen of the metal with gage length = 100 mm is stretched to a length = 157 mm. Determine the flow stress at the new length and the average flow stress that the metal has been subjected to during the deformation.

- Solution:  = ln (157/100) = ln 1.57 = 0.451

- Flow stress Yf = 850(0.451)0.30 = 669.4 MPa.

- Average flow stress Yf= 850(0.451)0.30/1.30 = 514.9 MPa.

- A particular metal has a flow curve with strength coefficient = 35,000 lb/in2 and strain-hardening exponent = 0.26. A tensile specimen of the metal with gage length = 2.0 in is stretched to a length = 3.3 in. Determine the flow stress at this new length and the average flow stress that the metal has been subjected to during deformation.

- Solution:  = ln (3.3/2.0) = ln 1.65 = 0.501

- Flow stress Yf = 35,000(0.501)0.26 = 29,240 lb/in2.

- Average flow stress Yf= 35,000(0.501)0.26/1.26 = 23,206 lb/in2.

- The strength coefficient and strain-hardening exponent of a certain test metal are 40,000 lb/in2 and 0.19, respectively. A cylindrical specimen of the metal with starting diameter = 2.5 in and length = 3.0 in is compressed to a length of 1.5 in. Determine the flow stress at this compressed length and the average flow stress that the metal has experienced during deformation.

- Solution:  = ln (1.5/3.0) = ln 0.5 = -0.69315

- Flow stress Yf = 40,000(0.69315)0.19 = 37,309 lb/in2.

- Average flow stress Yf = 40,000(0.69315)0.19/1.19 = 31,352 lb/in2.

- For a certain metal, the strength coefficient = 700 MPa and strain-hardening exponent = 0.27. Determine the average flow stress that the metal experiences if it is subjected to a stress that is equal to its strength coefficient K.

- Solution: Yf = K = 700 = Kn = 700.27

-  must be equal to 1.0.

- Yf= 700(1.0).27/1.27 = 700/1.27 = 551.2 MPa

- Determine the value of the strain-hardening exponent for a metal that will cause the average flow stress to be 3/4 of the final flow stress after deformation.

- Solution: Yf= 0.75 Yf

- Kn/(1+n) = 0.75 Kn

- 1/(1+n) = 0.75

- 1 = 0.75(1+n) = 0.75 + 0.75n

- 0.25 = 0.75n		n = 0.333

- The strength coefficient = 35,000 lb/in2 and strain-hardening exponent = 0.40 for a metal used in a forming operation in which the workpart is reduced in cross-sectional area by stretching. If the average flow stress on the part is 20,000 lb/in2, determine the amount of reduction in cross-sectional area experienced by the part.

Solution: Yf= Kn/(1+n)

20,000 = 35,000 .4/(1.4)

1.4(20,000) = 35,000 .4

28,000/35,000 = 0.8 = .4

0.4 ln  = ln (0.8) = -0.22314

ln  = -0.22314/0.4 = -0.55786

 = 0.5724

 = ln(Ao/Af) = 0.5724

Ao/Af = 1.7726

Af = Ao/1.7726 = 0.564Ao

The cross-sectional area has been reduced to 56.4% of its original area. That is a reduction of 43.6%.

- In a tensile test, two pairs of values of stress and strain were measured for the specimen metal after it had yielded: (1) true stress = 217 MPa and true strain = 0.35, and (2) true stress = 259 MPa and true strain = 0.68. Based on these data points, determine the strength coefficient and strain-hardening exponent.

Solution: Solve two equations, two unknowns: ln K = ln  - n ln ε

- ln K = ln 217 – n ln 0.35

- ln K = ln 259 – n ln 0.68

- ln K = 5.3799 – (-1.0498)n = 5.3799 + 1.0498 n

- ln K = 5.5568 – (-0.3857)n = 5.5568 + 0.3857 n

5.3799 + 1.0498 n = 5.5568 + 0.3857 n

1.0498 n – 0.3857 n = 5.5568 – 5.3799

0.6641 n = 0.1769		n = 0.2664

ln K = 5.3799 + 1.0498 (0.2664) = 5.6596		K = 287 MPa

- The following stress and strain values were measured in the plastic region during a tensile test carried out on a new experimental metal: (1) true stress = 43,608 lb/in2 and true strain = 0.27 in/in, and (2) true stress = 52,048 lb/in2 and true strain = 0.85 in/in. Based on these data points, determine the strength coefficient and strain-hardening exponent.

Solution: Solve two equations, two unknowns: ln K = ln  - n ln ε

- ln K = ln 43,608 – n ln 0.27

- ln K = ln 52,048 – n ln 0.85

- ln K = 10.6830 – (-1.3093)n = 10.6830 + 1.3093 n

- ln K = 10.8600 – (-0.1625)n = 10.8600 + 0.1625 n

- 10.6830 + 1.3093 n = 10.8600 + 0.1625 n

1.3093 n – 0.1625 n = 10.8600 – 10.6830

1.1468 n = 0.1769		n = 0.1543

ln K = 10.6830 + 1.3093 (0.1543) = 10.885		K = 53,374 lb/in2