13 BULK DEFORMATION PROCESSES IN METALWORKING

# Review Questions

- What are the reasons why the bulk deformation processes are important commercially and technologically?

- Answer. Reasons why the bulk deformation processes are important include the following: (1) they are capable of significant shape change when hot working is used, (2) they have a positive effect on part strength when cold working is used, and (3) most of the processes produce little material waste; some are net shape processes.

- Name the four basic bulk deformation processes.

- Answer. The four basic bulk deformation processes are (a) rolling, (2) forging, (3) extrusion, and (4) wire and bar drawing.

- What is rolling in the context of the bulk deformation processes?

- Answer. Rolling is a deformation process in which the thickness of the workpiece is reduced by compressive forces exerted by two opposing rolls. The rolls rotate, thus pulling and simultaneously squeezing the workpiece between them.

- List some of the products produced on a rolling mill.

- Answer. Rolled products include flat sheet and plate stock, round bar and rod stock, rails, structural shapes such as I-beams and channels.

- What is draft in a rolling operation?

- Answer. Draft is the difference between the starting thickness and the final thickness as the workpiece passes between the two opposing rolls.

- What is sticking in a hot rolling operation?

- Answer. Sticking is a condition in hot rolling in which the surface of the workpiece adheres to the rolls as the piece passes between the rolls, causing severe deformation of the metal below the surface in order to allow passage through the roll gap.

- Identify some of the ways in which force in flat rolling can be reduced.

- Answer. Ways to reduce force in flat rolling include (1) use hot rolling, (2) reduce draft in each pass, and (3) use smaller diameter rolls.

- What is a two-high rolling mill?

- Answer. A two-high rolling mill consists of two opposing rolls between which the work is compressed.

- What is a reversing mill in rolling?

- Answer. A reversing mill is a two-high rolling mill in which the direction of rotation of the rolls can be reversed to allow the work to pass through from either side.

- What is forging?

- Answer. Forging is a deformation process in which the workpiece is compressed between two dies, using impact or gradual pressure to form the part.

- One way to classify forging operations is by the degree to which the work is constrained in the die. By this classification, name the three basic types.

- Answer. The three basic types are (1) open die forging, (2) impression die forging, and (3) flashless forging.

- Why is flash desirable in impression die forging?

- Answer. Because its presence constrains the metal in the die so that it fills the details of the die cavity.

- What is a trimming operation in the context of impression die forging?

- Answer. Trimming is a shearing operation used to remove the flash on the workpiece after impression die forging.

- What are the two basic types of forging equipment?

- Answer. The two types of forging machines are hammers, which impact the workpart, and presses, which apply a gradual pressure to the work.

- What is isothermal forging?

- Answer. Isothermal forging is a hot forging operation in which the die surfaces are heated to reduce heat transfer from the work into the tooling.

- What is extrusion?

- Answer. Extrusion is a compression forming operation in which a workpiece is forced to flow through a die opening, thus taking the cross-sectional shape of the die opening.

- Distinguish between direct and indirect extrusion.

- Answer. In direct extrusion, also known as forward extrusion, a metal billet is loaded into a container, and a ram compresses the material, forcing it to flow through a die opening at the opposite end of the container. In indirect extrusion, also known as backward extrusion, the die is incorporated into the ram, and as the ram compresses into the metal billet, the metal is forced to flow through the die opening in a direction that is opposite (backwards) of the ram motion.

- Name some products that are produced by extrusion.

- Answer. Products produced by continuous extrusion include structural shapes (window frames, shower stalls, channels), tubes and pipes, and rods of various cross sections. Products made by discrete extrusion include toothpaste tubes, aluminum beverage cans, and battery cases.

- Why is friction a factor in determining the ram force in direct extrusion but not a factor in indirect extrusion?

- Answer. Friction is a factor in direct extrusion because the work billet is squeezed against the walls of the container so that friction resists the movement of the billet toward the die opening. In indirect extrusion, the billet does not move relative to the container walls, and thus there is no friction.

- What are wire drawing and bar drawing?

- Answer. Wire and bar drawing are bulk deformation processes in which the cross section of a wire or bar is reduced by pulling (drawing) it through a die opening.

- Although the workpiece in a wire drawing operation is obviously subjected to tensile stresses, how do compressive stresses also play a role in the process?

- Answer. Compressive stresses are present in wire drawing because the starting metal is compressed as it is forced through the approach of the die opening.

- In a wire drawing operation, why must the drawing stress never exceed the yield strength of the work metal?

Answer. Because if the drawing stress exceeded the yield strength, the metal on the exit side of the draw die would stretch rather than force metal to be pulled through the die opening.

# Problems

- A 42.0-mm-thick plate made of low carbon steel is to be reduced to 34.0 mm in one pass in a rolling operation. As the thickness is reduced, the plate widens by 4%. The yield strength of the steel plate is 174 MPa and the tensile strength is 290 MPa. The entrance speed of the plate is 15.0 m/min. The roll radius is 325 mm and the rotational speed is 49.0 rev/min. Determine (a) the minimum required coefficient of friction that would make this rolling operation possible, (b) exit velocity of the plate, and (c) forward slip.

- Solution: (a) Maximum draft dmax  = 2 R

- Given that d = to - tf = 42 - 34 = 8.0 mm,

- 2 = 8/325 = 0.0246

-  = (0.0246)0.5 = 0.157

- (b) Plate widens by 4%.

- towovo = tfwfvf

- wf = 1.04 wo

- 42(wo)(15) = 34(1.04wo)vf

- vf = 42(wo)(15)/ 34(1.04wo) = 630/35.4 = 17.8 m/min

- (c) vr = π r2N= π(0.325)2(49.0) = 16.26 m/min

- s = (vf - vr)/vr = (17.8 – 16.26)/16.26 = 0.0947

- A 2.0-in-thick slab is 10.0 in wide and 12.0 ft long. Thickness is to be reduced in three steps in a hot rolling operation. Each step will reduce the slab to 75% of its previous thickness. It is expected that for this metal and reduction, the slab will widen by 3% in each step. If the entry speed of the slab in the first step is 40 ft/min, and roll speed is the same for the three steps, determine: (a) length and (b) exit velocity of the slab after the final reduction.

- Solution: (a) After three passes, tf = (0.75)(0.75)(0.75)(2.0) = 0.844 in

- wf = (1.03)(1.03)(1.03)(10.0) = 10.927 in

- towoLo = tfwfLf

- (2.0)(10.0)(12 x 12) = (0.844)(10.927)Lf

- Lf = (2.0)(10.0)(12 x 12)/(0.844)(10.927) = 312.3 in = 26.025 ft

- (b) Given that roll speed is the same at all three steps and that towovo = tfwfvf ,

- Step 1: vf = (2.0)(10.0)(40)/(0.75 x 2.0)(1.03 x 10.0) = 51.78 ft/min

- Step 2: vf = (0.75 x 2.0)(1.03 x 10.0)(40)/(0.752 x 2.0)(1.032 x 10.0) = 51.78 ft/min

- Step 3: vf = (0.752 x 2.0)(1.032 x 10.0)(40)/(0.753 x 2.0)(1.033 x 10.0) = 51.78 ft/min

- A series of cold rolling operations are used to reduce the thickness of a plate from 50 mm down to 25 mm in a reversing two-high mill. Roll diameter = 700 mm and coefficient of friction between rolls and work = 0.15. The specification is that the draft is to be equal on each pass. Determine (a) minimum number of passes required, and (b) draft for each pass?

- Solution: (a) Maximum draft dmax = 2 R = (0.15)2 (350) = 7.875 mm

- Minimum number of passes = (to - tf)/dmax = (50 - 25)/7.875 = 3.17  4 passes

- (b) Draft per pass d = (50 - 25)/4 = 6.25 mm

- In the previous problem, suppose that the percent reduction were specified to be equal for each pass, rather than the draft. (a) What is the minimum number of passes required? (b) What is the draft for each pass?

- Solution: (a) Maximum possible draft occurs on first pass: dmax = 2 R = (0.15)2 (350) = 7.875 mm

- This converts into a maximum possible reduction x = 7.875/50 = 0.1575

- Let x = fraction reduction per pass, and n = number of passes. The number of passes must be an integer. To reduce from to = 50 mm to to = 25 mm in n passes, the following relationship must be satisfied:

- 50(1 - x)n = 25

- (1 - x)n = 25/50 = 0.5

- (1 - x) = 0.51/n

- Try n = 4: (1 - x) = (0.5)1/4 = 0.8409

- x = 1 - 0.8409 = 0.1591, which exceeds the maximum possible reduction of 0.1575.

- Try n = 5: (1 - x) = (0.5)1/5 = 0.87055

- x = 1 - 0.87055 = 0.12945, which is within the maximum possible reduction of 0.1575.

- (b) Pass 1: d = 50(0.12945) = 6.47 mm, tf = 50 - 6.47 = 43.53 mm

- Pass 2: d = 43.53(0.12945) = 5.63 mm, tf = 43.53 - 5.63 = 37.89 mm

- Pass 3: d = 37.89(0.12945) = 4.91 mm, tf = 37.89 - 4.91 = 32.98 mm

- Pass 4: d = 32.98(0.12945) = 4.27 mm, tf = 32.98 - 4.27 = 28.71 mm

- Pass 5: d = 28.71(0.12945) = 3.71 mm, tf = 28.71 - 3.71 = 25.00 mm

- A plate that is 250 mm wide and 25 mm thick is to be reduced in a single pass in a two-high rolling mill to a thickness of 20 mm. The roll has a radius = 500 mm, and its speed = 30 m/min. The work material has a strength coefficient = 240 MPa and a strain hardening exponent = 0.2. Determine (a) roll force, (b) roll torque, and (c) power required to accomplish this operation.

- Solution: (a) Draft d = 25 - 20 = 5 mm,

- Contact length L = (500 x 5).5 = 50 mm

- True strain  = ln(25/20) = ln 1.25 = 0.223

- Yf= 240(0.223)0.20/1.20 = 148.1 MPa

- Rolling force F = 148.1(250)(50) = 1,851,829 N

- (b) Torque T = 0.5(1,851,829)( 50 x 10-3) = 46,296 N-m

- (c) N = (30 m/min)/(2 x 0.500) = 9.55 rev/min = 0.159 rev/s

- Power P = 2(0.159)(1,851,829)(50 x 10-3) = 92,591 N-m/s = 92,591 W

- Solve Problem 13.5 using a roll radius = 250 mm.

- Solution: (a) Draft d = 25 - 20 = 5 mm,

- Contact length L = (250 x 5).5 = 35.35 mm

- True strain  = ln(25/20) = ln 1.25 = 0.223

- Yf= 240(0.223)0.20/1.20 = 148.1 MPa

- Rolling force F = 148.1(250)(35.35) = 1,311,095 N

- (b) Torque T = 0.5(1,311,095)(35.35 x 10-3) = 23,174 N-m

- (c) N = (30 m/min)/(2 x 0.250) = 19.1 rev/min = 0.318 rev/s

- Power P = 2(0.318)(1,311,095)(35.35 x 10-3) = 92,604 N-m/s = 92,604 W

- Note that the force and torque are reduced as roll radius is reduced, but that the power remains the same (within calculation error) as in the previous problem.

- A 4.50-in-thick slab that is 9 in wide and 24 in long is to be reduced in a single pass in a two-high rolling mill to a thickness of 3.87 in. The roll rotates at a speed of 5.50 rev/min and has a radius of 17.0 in. The work material has a strength coefficient = 30,000 lb/in2 and a strain hardening exponent = 0.15. Determine (a) roll force, (b) roll torque, and (c) power required to accomplish this operation.

- Solution: (a) Draft d = 4.50 – 3.87 = 0.63 in,

- Contact length L = (17.0 x 0.63)0.5 = 3.27 in

- True strain  = ln(4.5/3.87) = ln 1.16 = 0.1508

- Yf= 30,000(0.1508)0.15/1.15 = 19,642 lb/in2

- Rolling force F = YfwL = 16,414(9.0)(3.27) = 483,000 lb

- (b) Torque T = 0.5FL = 0.5(483000)(3.27) = 789,700 in-lb.

- (c) N = 5.50 rev/min

Power P = 2(5.50)(483000)(3.27) = 54,580,500  in-lb/min

- HP = (54,580,500 in-lb/min)/(396,000) = 138 hp

- A single-pass rolling operation reduces a 20 mm thick plate to 18 mm. The starting plate is 200 mm wide. Roll radius = 250 mm and rotational speed = 12 rev/min. The work material has a strength coefficient = 600 MPa and a strength coefficient = 0.22. Determine (a) roll force, (b) roll torque, and (c) power required for this operation.

- Solution: (a) Draft d = 20 - 18 = 2.0 mm,

- Contact length L = (250 x 2).5 = 11.18 mm = 0.0112 m

- True strain  = ln(20/18) = ln 1.111 = 0.1054

- Yf = 600(0.1054)0.22/1.22 = 300 MPa

- Rolling force F = 300(0.0112)(0.2) = 0.672 MN = 672,000 N

- (b) Torque T = 0.5(672,000)(0.0112) = 3,720 N-m

- (c) Given that N = 12 rev/min

- Power P = 2(12/60)(672,000)(0.0112) = 37,697 W

- A hot rolling mill has rolls of diameter = 24 in. It can exert a maximum force = 400,000 lb. The mill has a maximum horsepower = 100 hp. It is desired to reduce a 1.5 in thick plate by the maximum possible draft in one pass. The starting plate is 10 in wide. In the heated condition, the work material has a strength coefficient = 20,000 lb/in2 and a strain hardening exponent = zero. Determine (a) maximum possible draft, (b) associated true strain, and (c) maximum speed of the rolls for the operation.

- Solution: (a) Assumption: maximum possible draft is determined by the force capability of the rolling mill and not by coefficient of friction between the rolls and the work.

- Draft d = 1.5 - tf

- Contact length L = (12d)0.5

- Yf = 20,000()0/1.0 = 20,000 lb/in2

- Force F = 20,000(10) (12d)0.5 = 400,000 (the limiting force of the rolling mill)

- (12d)0.5 = 400,000/200,000 = 2.0

- 12 d = 2.02 = 4

- d = 4/12 = 0.333 in

- (b) True strain  = ln(1.5/tf)

- tf = to -d = 1.5 - 0.333 = 1.167 in

-  = ln(1.5/1.167) = ln 1.285 = 0.251

- (c) Given maximum possible power HP = 100 hp = 100 x 396000 (in-lb/min)/hp = 39,600,000 in-lb/min

- Contact length L = (12 x 0.333)0.5 = 2.0 in

- P = 2N(400,000)(2.0) = 5,026,548N in-lb/min

- 5,026,548N = 39,600,000

- N = 7.88 rev/min

- vr = 2RN = 2(12/12)(7.88) = 49.5 ft/min

- A cylindrical part is warm upset forged in an open die. The initial diameter is 45 mm and the initial height is 40 mm. The height after forging is 25 mm. The coefficient of friction at the die-work interface is 0.20. The yield strength of the work material is 285 MPa, and its flow curve is defined by a strength coefficient of 600 MPa and a strain-hardening exponent of 0.12. Determine the force in the operation (a) just as the yield point is reached (yield at strain = 0.002), (b) at a height of 35 mm, (c) at a height of 30 mm, and (d) at a height of 25 mm. Use of a spreadsheet calculator is recommended.

- Solution: (a) V = D2L/4 = (45)2(40)/4 = 63,617 mm3

- Given  = 0.002, Yf = 600(0.002)0.12 = 284.6 MPa, and h = 40 - 40(0.002) = 39.92

- A = V/h = 63,617/39.92 = 1594 mm2

- Kf = 1 + 0.4(0.2)(45)/39.92 = 1.09

- F = 1.09(284.6)(1594) = 494,400 N

- (b) Given h = 35,  = ln(40/35) = ln 1.143 = 0.1335

- Yf = 600(0.1335)0.12 = 471.2 MPa

- V = 63,617 mm3 from part (a) above.

- At h = 35, A = V/h = 63617/35 = 1818 mm2

- Corresponding D = 48.1 mm (from A = D2/4)

- Kf = 1 + 0.4(0.2)(48.1)/35 = 1.110

- F = 1.110(471.2)(1818) = 950,700 N

- (c) Given h = 30,  = ln(40/30) = ln 1.333 = 0.2877

- Yf = 600(0.2877)0.12 = 516.7 MPa

- V = 63,617 mm3 from part (a) above.

- At h = 30, A = V/h = 63,617/30 = 2120.6 mm2

- Corresponding D = 51.96 mm (from A = D2/4)

- Kf = 1 + 0.4(0.2)(51.96)/30 = 1.138

- F = 1.138(516.7)(2120.6) = 1,247,536 N

- (d) Given h = 25,  = ln(40/25) = ln 1.6 = 0.4700

- Yf = 600(0.470)0.12 = 548.0 MPa

- V = 63,617 mm3 from part (a) above.

- At h = 25, A = V/h = 63,617/25 = 2545 mm2

- Corresponding D = 56.9 mm (from A = D2/4)

- Kf = 1 + 0.4(0.2)(56.9)/25 = 1.182

- F = 1.182(548.0)(2545) = 1,649,000 N

- A cylindrical workpart with diameter = 2.5 in and height = 2.5 in is upset forged in an open die to a height = 1.5 in. Coefficient of friction at the die-work interface = 0.10. The work material has a flow curve defined by: K = 40,000 lb/in2 and n = 0.15. Yield strength = 15,750 lb/in2. Determine the instantaneous force in the operation (a) just as the yield point is reached (yield at strain = 0.002), (b) at height h = 2.3 in, (c) h = 2.1 in, (d) h = 1.9 in, (e) h = 1.7 in, and (f) h = 1.5 in. Use of a spreadsheet calculator is recommended.

- Solution: (a) V = D2L/4 = (2.5)2(2.5)/4 = 12.273 in3

- Given  = 0.002, Yf = 40,000(0.002)0.15 = 15,748 lb/in2 and h = 2.5 - 2.5(0.002) = 2.495

- A = V/h = 12.273/2.495 = 4.92 in2

- Kf = 1 + 0.4(0.1)(2.5)/2.495 = 1.04

- F = 1.04(15,748)(4.92) = 80,579 lb

- (b) Given h = 2.3,  = ln(2.5/2.3) = ln 1.087 = 0.0834

- Yf = 40,000(0.0834)0.15 = 27,556 lb/in2

- V = 12.273 in3 from part (a) above.

- At h = 2.3, A = V/h = 12.273/2.3 = 5.34 in2

- Corresponding D = 2.61 (from A = D2/4)

- Kf = 1 + 0.4(0.1)(2.61)/2.3 = 1.045

- F = 1.045(27,556)(5.34) = 153,822 lb

- (c) Given h = 2.1,  = ln(2.5/2.1) = ln 1.191 = 0.1744

- Yf = 40,000(0.1744)0.15 = 30,780 lb/in2

- V = 12.273 in3 from part (a) above.

- At h = 2.1, A = V/h = 12.273/2.1 = 5.84 in2

- Corresponding D = 2.73 (from A = D2/4)

- Kf = 1 + 0.4(0.1)(2.73)/2.1 = 1.052

- F = 1.052(30,780)(5.84) = 189,236 lb

- (d) Given h = 1.9,  = ln(2.5/1.9) = ln 1.316 = 0.274

- Yf = 40,000(0.274)0.15 = 32,948 lb/in2

- V = 12.273 in3 from part (a) above.

- At h = 1.9, A = V/h = 12.273/1.9 = 6.46 in2

- Corresponding D = 2.87 (from A = D2/4)

- Kf = 1 + 0.4(0.1)(2.87)/1.9 = 1.060

- F = 1.060(32,948)(6.46) = 225,695 lb

- (e) Given h = 1.7,  = ln(2.5/1.7) = ln 1.471 = 0.386

- Yf = 40,000(0.386)0.15 = 34,673 lb/in2

- V = 12.273 in3 from part (a) above.

- At h = 1.7, A = V/h = 12.273/1.7 = 7.22 in2

- Corresponding D = 3.03 (from A = D2/4)

- Kf = 1 + 0.4(0.1)(3.03)/1.7 = 1.071

- F = 1.071(34,673)(7.22) = 268,176 lb

- (f) Given h = 1.5,  = ln(2.5/1.5) = ln 1.667 = 0.511

- Yf = 40,000(0.511)0.15 = 36,166 lb/in2

- V = 12.273 in3 from part (a) above.

- At h = 1.5, A = V/h = 12.273/1.5 = 8.182 in2

- Corresponding D = 3.23 (from A = D2/4)

- Kf = 1 + 0.4(0.1)(3.23)/1.5 = 1.086

- F = 1.086(36,166)(8.182) = 321,379 lb

- A cold heading operation is performed to produce the head on a steel nail. The strength coefficient for this steel is 600 MPa, and the strain hardening exponent is 0.22. Coefficient of friction at the die-work interface is 0.14. The wire stock out of which the nail is made is 5.00 mm in diameter. The head is to have a diameter of 9.5 mm and a thickness of 1.6 mm. The final length of the nail is 120 mm. (a) What length of stock must project out of the die in order to provide sufficient volume of material for this upsetting operation? (b) Compute the maximum force that the punch must apply to form the head in this open-die operation.

- Solution: (a) Volume of nail head V = Df2hf/4 = (9.5)2(1.6)/4 = 113.4 mm3.

- Ao = Do2/4 = (4.75)2/4 = 19.6 mm2

- ho = V/Ao = 113.4/19.6 = 5.78 mm

- (b)  = ln(5.78/1.6) = ln 3.61= 1.2837

- Yf = 600(1.2837)0.22 = 634 MPa

- Af = (9.5)2/4 = 70.9 mm2

- Kf = 1 + 0.4(0.14)(9.5/1.6) = 1.33

- F = 1.33(634)(70.9) = 59,886 N

- Obtain a large common nail (flat head). Measure the head diameter and thickness, as well as the diameter of the nail shank. (a) What stock length must project out of the die in order to provide sufficient material to produce the nail? (b) Using appropriate values for strength coefficient and strain hardening exponent for the metal out of which the nail is made (Table 3.4), compute the maximum force in the heading operation to form the head.

- Solution: Student exercise. Calculations similar to those in the preceding problem for the data developed by the student.

- A hot upset forging operation is performed in an open die. The starting workpart has a diameter = 25 mm and height = 50 mm. The part is upset to an average diameter = 50 mm. The work metal at this elevated temperature yields at 85 MPa (n = 0). Coefficient of friction at the die-work interface = 0.40. Determine (a) final height of the part, and (b) maximum force in the operation.

- Solution: (a) V = Do2ho/4 = (25)2(50)/4 = 24,544 mm3.

- Af = Df2/4 = (50)2/4 = 1963.5 mm2.

- hf = V/Af = 24,544/1963.5 = 12.5 mm.

- (b)  = ln(50/12.5) = ln 4 = 1.3863

- Yf = 85(1.3863)0 = 85 MPa

- Force is maximum at largest area value, Af = 1963.5 mm2

- D = (4 x 1963.5/)0.5 = 50 mm

- Kf = 1 + 0.4(0.4)(50/12.5) = 1.64

- F = 1.64(85)(1963.5) = 273,712 N

- A hydraulic forging press is capable of exerting a maximum force = 1,000,000 N. A cylindrical workpart is to be cold upset forged. The starting part has diameter = 30 mm and height = 30 mm. The flow curve of the metal is defined by K = 400 MPa and n = 0.2. Determine the maximum reduction in height to which the part can be compressed with this forging press, if the coefficient of friction = 0.1. Use of a spreadsheet calculator is recommended.

- Solution: Volume of work V = Do2ho/4 = (30)2(30)/4 = 21,206 mm3.

- Final area Af = 21,206/hf

-  = ln(30/hf)

- Yf = 4000.2 = 400(ln 30/hf)0.2)

- Kf = 1 + 0.4(Df/hf) = 1 + 0.4(0.1)(Df/hf)

- Forging force F = KfYfAf = (1 + 0.04Df/hf)( 400(ln 30/hf)0.2)( 21,206/hf)

- Requires trial and error solution to find the value of hf that will match the force of 1,000,000 N.

- (1) Try hf = 20 mm

- Af = 21,206/20 = 1060.3 mm2

-  = ln(30/20) = ln 1.5 = 0.405

- Yf = 400(0.405)0.2 = 333.9 MPa

- Df = (4 x 1060.3/)0.5 = 36.7 mm

- Kf = 1 + 0.04(36.7/20) = 1.073

- F = 1.073(333.9)(1060.3) = 380,050 N

- Too low. Try a smaller value of hf to increase F.

- (2) Try hf = 10 mm.

- Af = 21,206/10 = 2120.6 mm2

-  = ln(30/10) = ln 3.0 = 1.099

- Yf = 400(1.099)0.2 = 407.6 MPa

- Df = (4 x 2120.6/)0.5 = 51.96 mm

- Kf = 1 + 0.04(51.96/10) = 1.208

- F = 1.208(407.6)(2120.6) = 1,043,998 N

- Slightly high. Need to try a value of hf between 10 and 20, closer to 10.

- (3) Try hf = 11 mm

- Af = 21,206/11 = 1927.8 mm2

-  = ln(30/11) = ln 2.7273 = 1.003

- Yf = 400(1.003)0.2 = 400.3 MPa

- Df = (4 x 1927.8/)0.5 = 49.54 mm

- Kf = 1 + 0.04(51.12/11) = 1.18

- F = 1.18(400.3)(1927.8) = 910,653 N

- (4) By linear interpolation, try hf = 10 + (44/133) = 10.33 mm

- Af = 21,206/10.33 = 2052.8 mm2

-  = ln(30/10.33) = ln 2.9042 = 1.066

- Yf = 400(1.066)0.2 = 405.16 MPa

- Df = (4 x 2052.8/)0.5 = 51.12 mm

- Kf = 1 + 0.04(51.12/10.33) = 1.198

- F = 1.198(405.16)(2052.8) = 996,364 N

- (5) By further linear interpolation, try hf = 10 + (44/48)(0.33) = 10.30

- Af = 21,206/10.30 = 2058.8 mm2

-  = ln(30/10.30) = ln 2.913 = 1.069

- Yf = 400(1.069)0.2 = 405.38 MPa

- Df = (4 x 2058.8/)0.5 = 51.2 mm

- Kf = 1 + 0.04(51.2/10.3) = 1.199

- F = 1.199(405.38)(2058.8) = 1,000,553 N

- Close enough!  Maximum height reduction = 30.0 - 10.3 = 19.7 mm

- Using a spreadsheet calculator, the author’s program (written in Excel) obtained a value of h = 19.69603 mm to achieve a force of 1,000,000 lb within one pound.

- A part is designed to be hot forged in an impression die. The projected area of the part, including flash, is 16 in2. After trimming, the part has a projected area of 10 in2. Part geometry is complex. As heated the work material yields at 10,000 lb/in2, and has no tendency to strain harden. At room temperature, the material yields at 25,000 lb/in2 Determine the maximum force required to perform the forging operation.

- Solution: Since the work material has no tendency to work harden, n = 0.

- From Table 13.1, choose Kf = 8.0.

- F = 8.0(10,000)(16) = 1,280,000 lb.

- A connecting rod is designed to be hot forged in an impression die. The projected area of the part is 6,500 mm2. The design of the die will cause flash to form during forging, so that the area, including flash, will be 9,000 mm2. The part geometry is considered to be complex. As heated the work material yields at 75 MPa, and has no tendency to strain harden. Determine the maximum force required to perform the operation.

Solution: Since the work material has no tendency to work harden, n = 0.

From Table 13.1, choose Kf =8.0.

F = 8.0(75)(9,000) = 5,400,000 N.

- A cylindrical billet that is 100 mm long and 50 mm in diameter is reduced by indirect (backward) extrusion to a 20 mm diameter. The die angle is 90. In the Johnson equation, a = 0.8 and b = 1.4. In the flow curve for the work metal, the strength coefficient = 800 MPa and strain hardening exponent = 0.13. Determine (a) extrusion ratio, (b) true strain (homogeneous deformation), (c) extrusion strain, (d) ram pressure, and (e) ram force.

- Solution: (a) rx = Ao/Af = Do2/Df2 = (50)2/(20)2 =  6.25

- (b)  = ln rx = ln 6.25 = 1.833

- (c) x = a + b ln rx = 0.8 + 1.4(1.833) = 3.366

- (d) Yf= 800(1.833)0.13/1.13 = 766.0 MPa

- p = 766.0(3.366) = 2578 MPa

- (e) Ao = Do2/4 = (50)2/4 = 1963.5 mm2

- F = 2578(1963.5) = 5,062,000 N

- A 3.0-in-long cylindrical billet whose diameter = 1.5 in is reduced by indirect extrusion to a diameter = 0.375 in. Die angle = 90. In the Johnson equation, a = 0.8 and b = 1.5. In the flow curve for the work metal, K = 75,000 lb/in2 and n = 0.25. Determine (a) extrusion ratio, (b) true strain (homogeneous deformation), (c) extrusion strain, (d) ram pressure, (e) ram force, and (f) power if the ram speed = 20 in/min.

- Solution: (a) rx = Ao/Af = Do2/Df2 = (1.5)2/(0.375)2 = 42 = 16.0

- (b)  = ln rx = ln 16 = 2.773

- (c) x = a + b ln rx = 0.8 + 1.5(2.773) = 4.959

- (d) Yf= 75,000(2.773)0.25/1.25 = 77,423 lb/in2

- p = 77,423(4.959) = 383,934 lb/in2

- (e) Ao = Do2/4 = (1.5)2/4 = 1.767 in2

- F = (383,934)(1.767) = 678,411 lb.

- (f) P = 678,411(20) = 13,568,228 in-lb/min

- HP = 13,568,228/396,000 = 34.26 hp

- A billet that is 75 mm long with diameter = 35 mm is direct extruded to a diameter of 20 mm. The extrusion die has a die angle = 75. For the work metal, K = 600 MPa and n = 0.25. In the Johnson extrusion strain equation, a = 0.8 and b = 1.4. Determine (a) extrusion ratio, (b) true strain (homogeneous deformation), (c) extrusion strain, and (d) ram pressure and force at L = 70, 60, 50, 40, 30, 20, and 10 mm. Use of a spreadsheet calculator is recommended for part (d).

- Solution: (a) rx = Ao/Af = Do2/Df2 = (35)2/(20)2 = 3.0625

- (b)  = ln rx = ln 3.0625 = 1.119

- (c) x = a + b ln rx = 0.8 + 1.4(1.119) = 2.367

- (d) Yf= 600(1.119)0.25/1.25 = 493.7 MPa

- Ao = (35)2/4 = 962.1 mm2

- It is appropriate to determine the volume of metal contained in the cone of the die at the start of the extrusion operation, to assess whether metal has been forced through the die opening by the time the billet has been reduced from L = 75 mm to L = 70 mm. For a cone-shaped die with angle = 75, the height h of the frustum is formed by metal being compressed into the die opening: The two radii are: R1 = 0.5Do = 17.5 mm and R2 = 0.5Df = 10 mm, and h = (R1 - R2)/tan 75 = 7.5/tan 75 = 2.01 mm

- Frustum volume V = 0.333h(R12 + R1R2 + R22) = 0.333(2.01)(17.52 + 10 x 17.5 + 102) = 1223.4 mm3. Compare this with the volume of the portion of the cylindrical billet between L = 75 mm and L = 70 mm.

- V = Do2 h/4 = 0.25(35)2(75 - 70) = 4810.6 mm3

- Since this volume is greater than the volume of the frustum, this means that the metal has extruded through the die opening by the time the ram has moved forward by 5 mm.

- L = 70 mm: pressure p = 493.7(2.367 + 2 x 70/35) = 3143.4 MPa

- Force F = 3143.4(962.1) = 3,024, 321 N

- L = 60 mm: pressure p = 493.7(2.367 + 2 x 60/35) = 2861.3 MPa

- Force F = 2861.3(962.1) = 2,752,890 N

- L = 50 mm: pressure p = 493.7(2.367 + 2 x 50/35) = 2579.2 MPa

- Force F = 2579.2(962.1) = 2,481,458 N

- L = 40 mm: pressure p = 493.7(2.367 + 2 x 40/35) = 2297.1 MPa

- Force F = 2297.1(962.1) = 2,210,027 N

- L = 30 mm: pressure p = 493.7(2.367 + 2 x 30/35) = 2014.9 MPa

- Force F = 2014.9(962.1) = 1,938,595 N

- L = 20 mm: pressure p = 493.7(2.367 + 2 x 20/35) = 1732.8 MPa

- Force F = 1732.8(962.1) = 1,667,164 N

- L = 10 mm: pressure p = 493.7(2.367 + 2 x 10/35) = 1450.7 MPa

- Force F = 1450.7(962.1) = 1,395,732 N

- A 2.0-in-long billet with diameter = 1.25 in is direct extruded to a diameter of 0.50 in. The extrusion die angle = 90. For the work metal, K = 45,000 lb/in2, and n = 0.20. In the Johnson extrusion strain equation, a = 0.8 and b = 1.5. Determine (a) extrusion ratio, (b) true strain (homogeneous deformation), (c) extrusion strain, and (d) ram pressure at L = 2.0, 1.5, 1.0, 0.5 and zero in. Use of a spreadsheet calculator is recommended for part (d).

- Solution: (a) rx = Ao/Af = Do2/Df2 = (1.25)2/(0.5)2 =  6.25

- (b)  = ln rx = ln 6.25 = 1.8326

- (c) x = a + b ln rx = 0.8 + 1.5(1.8326) = 3.549

- (d) Yf= 45,000(1.8326)0.20/1.20 = 42,330 lb/in2

- Ao = (1.25)2/4 = 1.227 in2

- Unlike the previous problem, the die angle  = 90, so metal is forced through the die opening as soon as the billet starts to move forward in the chamber.

- L = 2.0 in: pressure p = 42,330(3.549 + 2 x 2.0/1.25) = 285,677 lb/in2

- Force F = 285,677(1.227) = 350,579 lb

- L = 1.5 in: pressure p = 42,330(3.549 + 2 x 1.5/1.25) = 251,813 lb/in2

- Force F = 251,813(1.227) = 309,022 lb

- L = 1.0 in: pressure p = 42,330(3.549 + 2 x 1.0/1.25) = 217,950 lb/in2

- Force F = 217,950(1.227) = 267,465 lb

- L = 0.5 in: pressure p = 42,330(3.549 + 2 x 0.5/1.25) = 184,086 lb/in2

- Force F = 184,086(1.227) = 225,908 lb

- L = 0.0 in: pressure p = 42,330(3.549 + 2 x 0.0/1.25) = 150,229 lb/in2

- Force F = 150,229(1.227) = 184,351 lb

- These last values for L = 0 are not possible because of the increase in pressure and force due to the butt remaining in the extruder container at the end of the operation.

- An indirect extrusion process starts with an aluminum billet with diameter = 2.0 in and length = 3.0 in. Final cross section after extrusion is a square with 1.0 in on a side. The die angle = 90. The operation is performed cold and the strength coefficient of the metal K = 26,000 lb/in2 and strain-hardening exponent n = 0.20. In the Johnson extrusion strain equation, a = 0.8 and b = 1.2. (a) Compute the extrusion ratio, true strain, and extrusion strain. (b) What is the shape factor of the product? (c) If the butt left in the container at the end of the stroke is 0.5 in thick, what is the length of the extruded section? (d) Determine the ram pressure in the process.

- Solution: (a) rx = Ao/Af

- Ao = Do2/4 = (2)2/4 = 3.142 in2

- Af = 1.0 x 1.0 = 1.0 in2

- rx = 3.142/1.0 = 3.142

-  = ln 3.142 = 1.145

- x = 0.8 + 1.3(1.145) = 2.174

- (b) To determine the die shape factor we need to determine the perimeter of a circle whose area is equal to that of the extruded cross section, A = 1.0 in2. The radius of the circle is R = (1.0/)0.5 = 0.5642 in, Cc = 2(0.5642) = 3.545 in

- The perimeter of the extruded cross section Cx = 4(1.0) = 4.0 in

- Kx = 0.98 + 0.02(4.0/3.545)2.25 = 1.006

- (c) Given that the butt thickness = 0.5 in

- Original volume V = (3.0)( x 22/4) = 9.426 in3

- The final volume consists of two sections: (1) butt, and (2) extrudate. The butt volume V1 = (0.5)(22/4) = 1.571 in3. The extrudate has a cross-sectional area Af = 1.0 in2. Its volume V2 = LAf = 9.426 - 1.571 = 7.855 in3. Thus, length L = 7.855/1.0 = 7.855 in

- (d) Yf= 26,000(1.145)0.2/1.2 = 22,261 lb/in3

- p = 1.006(22,261)(2.174) = 48,698 lb/in2

- A cup-shaped part is backward extruded from an aluminum slug that is 50 mm in diameter. The final dimensions of the cup are: OD = 50 mm, ID = 40 mm, height = 100 mm, and thickness of base = 5 mm. Determine (a) extrusion ratio, (b) shape factor, and (c) height of starting slug required to achieve the final dimensions. (d) If the metal has flow curve parameters K = 400 MPa and n = 0.25, and the constants in the Johnson extrusion strain equation are: a = 0.8 and b = 1.5, determine the extrusion force.

- Solution: (a) rx = Ao/Af

- Ao = 0.25(50)2  = 1963.75 mm2

- Af = 0.25(502 - 402) = 706.86 mm2

- rx = 1963.75/706.86 = 2.778

- (b) To determine the die shape factor we need to determine the perimeter of a circle whose area is equal to that of the extruded cross section, A = 706.86 mm2.  The radius of the circle is R = (706.86/)0.5 = 15 mm, Cc = 2(15) = 94.25 mm.

- The perimeter of the extruded cross section Cx = (50 + 40) = 90 = 282.74 mm.

- Kx = 0.98 + 0.02(282.74/94.25)2.25 = 1.217

- (c) Volume of final cup consists of two geometric elements: (1) base and (2) ring.

- (1) Base t = 5 mm and D = 50 mm.  V1 = 0.25(50)2(5) = 9817.5 mm3

- (2) Ring OD = 50 mm, ID = 40 mm, and h = 95 mm.

- V2 = 0.25(502 - 402)(95) = 0.25(2500 - 1600)(95) = 67,151.5 mm3

- Total V = V1 + V2 = 9817.5 + 67,151.5 = 76,969 mm3

- Volume of starting slug must be equal to this value V = 76,969 mm3

- V = 0.25(50)2(h) = 1963.5h = 76,969 mm3

- h = 39.2 mm

- (d)  = ln 2.778 = 1.0218

- x = 0.8 + 1.5(1.0218) = 2.33

- Yf= 400(1.0218)0.25/1.25 = 321.73 MPa

- p = Kx Yfx = 1.217(321.73)(2.33) = 912.3 MPa

- Ao = 0.25(40)2 = 1256.6 mm2

- F = 912.3(1256.6) = 1,146,430 N

- Determine the shape factor for each of the extrusion die orifice shapes in Figure P13.24.

Solution: (a) Ax = 20 x 60 = 1200 mm, Cx = 2(20 + 60) = 160 mm

Ao = R2 = 1200

R2 = 1200/ = 381.97,  R = 19.544 mm,  Cc = 2R = 2(19.544) = 122.8 mm

Kx = 0.98 + 0.02(160/122.8)2.25 = 1.016

(b) Ax = Ro2 - Ri2 = (252 - 22.52) = 373.06 mm2

Cx = Do + Di = (50 + 45) = 298.45 mm

R2 = 373.06/ = 118.75,  R = 10.897 mm,  Cc = 2R = 2(10.897) = 68.47 mm

Kx = 0.98 + 0.02(298.45/68.47)2.25 = 1.53

(c) Ax = 2(5)(30) + 5(60 - 10) = 300 + 250 = 550 mm2

Cx = 30 + 60 + 30 + 5 + 25 + 50 + 25 + 5 = 230 mm

Ao = R2 = 550, R2 = 550/ = 175.07, R = 13.23 mm

Cc = 2R = 2(13.23) = 83.14 mm

Kx = 0.98 + 0.02(230/83.14)2.25 = 1.177

(d) Ax = 5(55)(5) + 5(85 - 5x5) = 1675 mm2

Cx = 2 x 55 + 16 x 25 + 8 x 15 + 10 x 5 = 680 mm

Ao = R2 = 1675, R2 = 1675/ = 533.17,  R = 23.09 mm

Cc = 2R = 2(23.09) = 145.08 mm

Kx = 0.98 + 0.02(680/145.08)2.25 = 1.626

- A direct extrusion operation produces the cross section shown in Figure P13.24(a) from a brass billet whose diameter = 125 mm and length = 350 mm. The flow curve parameters of the brass are K = 700 MPa and n = 0.35. In the Johnson strain equation, a = 0.7 and b = 1.4. Determine (a) the extrusion ratio, (b) the shape factor, (c) the force required to drive the ram forward during extrusion at the point in the process when the billet length remaining in the container = 300 mm, and (d) the length of the extruded section at the end of the operation if the volume of the butt left in the container is 600,000 mm3.

- Solution: (a) rx = Ao/Af

- Ao = (125)2/4 = 12,272 mm2

- Af = Ax = 20(60) = 1200 mm2

- rx = 12272/1200 = 10.23

- (b) To determine the die shape factor we need to determine the perimeter of a circle whose area is equal to that of the extruded cross section, Af = 1200 mm2.

- The radius of the circle is R = (1200/)0.5 = 19.544 mm, Cc = 2(19.544) = 122.8 mm.

- The perimeter of the extruded cross section Cx = 2(20 + 60) = 160 mm

- Kx = 0.98 + 0.02(160/122.8)2.25 = 1.016

- (c)  = ln 10.23 = 2.325

- x = 0.7 + 1.4(2.325) = 3.955

- Yf= 700(2.325)0.35/1.35 = 696.6 MPa

- p = KxYfx = 1.016(696.6)(3.955 + 2(300)/125) = 6196.3 MPa

- F = pAo = 6196.3(12,272) = 76,295,200 N

- (d) Total original volume V = (125)2(350)/4 = 4,295,200 mm3

- The final volume consists of two sections: (1) butt, and (2) extrudate.

- The butt volume as given V1 = 600,000 mm3.

- The extrudate has a cross-sectional area Af = 1200 mm2.

- Its volume V2 = LAf = 4,295,200 – 600,000 = 3,695,200 mm3.

- Thus, length L = 3,695,200/1200 = 3079.3 mm = 3.079 m

- In a direct extrusion operation the cross section shown in Figure P13.24(b) is produced from a copper billet whose diameter = 100 mm and length = 500 mm. In the flow curve for copper, the strength coefficient = 300 MPa and strain hardening exponent = 0.50. In the Johnson strain equation, a = 0.8 and b = 1.5. Determine (a) the extrusion ratio, (b) the shape factor, (c) the force required to drive the ram forward during extrusion at the point in the process when the billet length remaining in the container = 450 mm, and (d) the length of the extruded section at the end of the operation if the volume of the butt left in the container is 350,000 mm3.

- Solution: (a) rx = Ao/Af

- Ao = (100)2/4 = 7854 mm2

- Af = Ax = (50)2/4 - (45)2/4 = 1963.5 – 1590.4 = 373.1 mm2

- rx = 7854/373.1 = 21.05

- (b) To determine the die shape factor we need to determine the perimeter of a circle whose area is equal to that of the extruded cross section, Ax = 373.1 mm2.

- The radius of the circle is R = (373.1/)0.5 = 10.9 mm, Cc = 2(10.9) = 68.5 mm.

- The perimeter of the extruded cross section Cx = (50) + (45) = 298.5 mm

- Kx = 0.98 + 0.02(298.5/68.5)2.25 = 1.53

- (c)  = ln 21.05= 3.047

- x = 0.8 + 1.5(3.047) = 5.37

- Yf= 300(3.047)0.50/1.50 = 349.1 MPa

- p = KxYfx = 1.53(349.1)(5.37 + 2(450)/100) = 7675.3 MPa

- F = pAo = 7675.3(7854) = 60,282,179 N

- (d) Total original volume V = (100)2(500)/4 = 3,926,991 mm3

- The final volume consists of two sections: (1) butt, and (2) extrudate.

- The butt volume as given V1 = 350,000 mm3.

- The extrudate has a cross-sectional area Af = 373.1 mm2.

- Its volume V2 = LAf = 3,926,991 – 350,000 = 3,576,991 mm3.

- Thus, length L = 3,576,991/373.1 = 9,587.2 mm = 9.587 m

- A direct extrusion operation produces the cross section shown in Figure P13.24(c) from an aluminum billet whose diameter = 150 mm and length = 500 mm. The flow curve parameters for the aluminum are K = 240 MPa and n = 0.16. In the Johnson strain equation, a = 0.8 and b = 1.2. Determine (a) the extrusion ratio, (b) the shape factor, (c) the force required to drive the ram forward during extrusion at the point in the process when the billet length remaining in the container = 400 mm, and (d) the length of the extruded section at the end of the operation if the volume of the butt left in the container is 600,000 mm3.

- Solution: (a) rx = Ao/Af

- Ao = (150)2/4 = 17,671.5 mm2

- Af = Ax = 60(5) + 2(25)(5) = 300 + 250 = 550 mm2

- rx = 17,671.5/550 = 32.1

- (b) To determine the die shape factor we need to determine the perimeter of a circle whose area is equal to that of the extruded cross section, Ax = 550 mm2.

Cx = 30 + 60 + 30 + 5 + 25 + 50 + 25 + 5 = 230 mm

Ao = R2 = 550, R2 = 550/ = 175.07, R = 13.23 mm

Cc = 2R = 2(13.23) = 83.14 mm

Kx = 0.98 + 0.02(230/83.14)2.25 = 1.177

- (c)  = ln 32.1= 3.47

- x = 0.8 + 1.2(3.47) = 4.96

- Yf= 240(3.47)0.16/1.16 = 252.5 MPa

- p = KxYfx = 1.177(252.5)(4.96 + 2(400)/150) = 3059.1 MPa

- F = pAo = 3059.1(17,671.5) = 54,058,912 N

- (d) Total original volume V = (150)2(500)/4 = 8,835,750 mm3

- The final volume consists of two sections: (1) butt, and (2) extrudate.

- The butt volume as given V1 = 600,000 mm3.

- The extrudate has a cross-sectional area Af = 550 mm2.

- Its volume V2 = LAf = 8,835,750 – 600,000 = 8,235,750 mm3.

- Thus, length L = 8,835,750/550 = 14,974 mm = 14.974 m

- A direct extrusion operation produces the cross section shown in Figure P13.24(d) from an aluminum billet whose diameter = 150 mm and length = 900 mm. The flow curve parameters for the aluminum are K = 240 MPa and n = 0.16. In the Johnson strain equation, a = 0.8 and b = 1.5. Determine (a) the extrusion ratio, (b) the shape factor, (c) the force required to drive the ram forward during extrusion at the point in the process when the billet length remaining in the container = 850 mm, and (d) the length of the extruded section at the end of the operation if the volume of the butt left in the container is 600,000 mm3.

- Solution: (a) rx = Ao/Af

- Ao = (150)2/4 = 17,671.5 mm2

- Af = Ax = 5(55)(5) + 5(85 – 5(5)) = 1675 mm2

- rx = 17,671.5/1675 = 10.55

- (b) To determine the die shape factor we need to determine the perimeter of a circle whose area is equal to that of the extruded cross section, Ax = 1675 mm2.

Cx = 2 x 55 + 16 x 25 + 8 x 15 + 10 x 5 = 680 mm

Ao = R2 = 1675, R2 = 1675/ = 533.17,  R = 23.09 mm

Cc = 2R = 2(23.09) = 145.08 mm

Kx = 0.98 + 0.02(680/145.08)2.25 = 1.626

- (c)  = ln 10.55= 2.36

- x = 0.8 + 1.5(2.36) = 4.33

- Yf= 240(2.36)0.16/1.16 = 237.4 MPa

- p = KxYfx = 1.626(237.4)(4.33 + 2(850)/150) = 6046.2 MPa

- F = pAo = 6046.2(17,671.5) = 106,846,146 N

- (d) Total original volume V = (150)2(900)/4 = 15,904,313 mm3

- The final volume consists of two sections: (1) butt, and (2) extrudate.

- The butt volume as given V1 = 600,000 mm3.

- The extrudate has a cross-sectional area Af = 1675 mm2.

- Its volume V2 = LAf = 15,904,313 – 600,000 = 15,304,313 mm3.

- Thus, length L = 15,304,313/1675 = 9,137 mm = 9.137 m

- A spool of wire has a starting diameter of 2.5 mm. It is drawn through a die with an opening that is 2.1 mm. The entrance angel of the die is 18 degrees. Coefficient of friction at the work-die interface is 0.08. The work metal has a strength coefficient of 450 MPa and a strain hardening coefficient of 0.26. The drawing is performed at room temperature. Determine (a) area reduction, (b) draw stress, and (c) draw force required for the operation.

- Solution: (a) r = (Ao - Af)/Ao

- Ao = 0.25(2.50)2 = 4.91 mm2

- Af = 0.25(2.1)2 = 3.46 mm2

- r = (4.91 – 3.46)/4.91 = 0.294

- (b) Draw stress d:

-  = ln(4.91/3.46) = ln 1.417 = 0.349

- Yf= 450(0.349)0.26/1.26 = 271.6 MPa

-  = 0.88 + 0.12(D/Lc)

- D = 0.5(2.5 + 2.1) = 2.30

- Lc = 0.5(2.5 - 2.1)/sin 18 = 0.647

-  = 0.88 + 0.12(2.30/0.647) = 1.31

- d = Yf(1 + /tan )(ln Ao/Af) = 271.6(1 + 0.08/tan 18)(1.31)(0.349) = 154.2 MPa

- (c) Draw force F:

- F = Af d = 3.46(154.2) = 534.0 N

- Rod stock that has an initial diameter of 0.50 in is drawn through a draw die with an entrance angle of 13. The final diameter of the rod is = 0.375 in. The metal has a strength coefficient of 40,000 lb/in2 and a strain hardening exponent of 0.20. Coefficient of friction at the work-die interface = 0.1. Determine (a) area reduction, (b) draw force for the operation, and (c) horsepower to perform the operation if the exit velocity of the stock = 2 ft/sec.

- Solution: (a) r = (Ao - Af)/Ao

- Ao = 0.25(0.50)2 = 0.1964 in2

- Af = 0.25(0.35)2 = 0.1104 in2

- r = (0.1964 - 0.1104)/0.1964 = 0.4375

- (b) Draw force F:

-  = ln(0.1964/0.1104) = ln 1.778 = 0.5754

- Yf= 40,000(0.5754)0.20/1.20 = 29,845 lb/in2

-  = 0.88 + 0.12(D/Lc)

- D = 0.5(.50 + 0.375) = 0.438

- Lc = 0.5(0.50 - 0.375)/sin 13 = 0.2778

-  = 0.88 + 0.12(0.438/0.2778) = 1.069

- F = Af Yf(1 + /tan )(ln Ao/Af)

- F = 0.1104(29,845)(1 + 0.1/tan 13)(1.069)(0.5754) = 2907 lb

- (c) P = 2907(2 ft/sec x 60) = 348,800 ft/lb/min

- HP = 348800/33,000 = 10.57 hp

- Bar stock of initial diameter = 90 mm is drawn with a draft = 15 mm. The draw die has an entrance angle = 18, and the coefficient of friction at the work-die interface = 0.08. The metal behaves as a perfectly plastic material with yield stress = 105 MPa. Determine (a) area reduction, (b) draw stress, (c) draw force required for the operation, and (d) power to perform the operation if exit velocity = 1.0 m/min.

- Solution: (a) r = (Ao - Af)/Ao

- Ao = 0.25(90)2 = 6361.7 mm2

- Df = Do - d = 90 - 15 = 75 mm,

- Af = 0.25(75)2 = 4417.9 mm2

- r = (6361.7 - 4417.9)/6361.7 = 0.3056

- (b) Draw stress d:

-  = ln(6361.7 /4417.9) = ln 1.440 = 0.3646

- Yf= k = 105 MPa

-  = 0.88 + 0.12(D/Lc)

- D = 0.5(90 + 75) = 82.5 mm

- Lc = 0.5(90 - 75)/sin 18 = 24.3 mm

-  = 0.88 + 0.12(82.5/24.3) = 1.288

- d = Yf(1 + /tan )(ln Ao/Af) = 105(1 + 0.08/tan 18)(1.288)(0.3646) = 61.45 MPa

- (c) F = Af d = 4417.9 (61.45) =  271,475 N

- (d) P = 271,475(1 m/min) = 271,475 N-m/min = 4524.6 N-m/s = 4524.6 W

- Wire stock of initial diameter = 0.125 in is drawn through two dies each providing a 0.20 area reduction. The starting metal has a strength coefficient = 40,000 lb/in2 and a strain hardening exponent = 0.15. Each die has an entrance angle of 12, and the coefficient of friction at the work-die interface is estimated to be 0.10. The motors driving the capstans at the die exits can each deliver 1.50 hp at 90% efficiency. Determine the maximum possible speed of the wire as it exits the second die.

Solution: First draw: Do = 0.125 in, Ao = 0.25(0.125)2 = 0.012273 in2 009819 in2

 = ln(0.012273/0.009819) = ln 1.250 = 0.2231

r = (Ao - Af)/Ao, Af = Ao(1 - r) = 0.012273(1 - 0.2) = 0.009817

Yf = 40,000(0.2231)0.15/1.15 = 27,775 lb/in2

 = 0.88 + 0.12(D/Lc)

Df = 0.125(1 - r)0.5 = 0.125(0.8).5 = 0.1118 in

D = 0.5(0.125 + 0.1118) = 0.1184

Lc = 0.5(0.125 - 0.1118)/sin 12 = 0.03173

 = 0.88 + 0.12(0.1184/0.03173) = 1.33

F = Af Yf(1 + /tan )(ln Ao/Af)

F = 0. 009817(27,775)(1 + 0.1/tan 12)(1.33)(0.2231) = 119 lb

1.5 hp at 90% efficiency = 1.5 x 0.90(33,000 ft-lb/min)/60 = 742.5 ft-lb/sec

P = Fv = 119v = 742.5

v = 742.5/119 = 6.24 ft/sec

Second draw: Do = 0.1118 in, Ao = 0.25(0.1118)2 = 0.009819 in2

r = (Ao - Af)/Ao, Af = Ao(1 - r) = 0.009819(1 - 0.2) = 0.007855 in2

 = ln(0.009819/0.007855) = ln 1.250 = 0.2231

Total strain experienced by the work metal is the sum of the strains from the first and second draws:

 = 1 + 2 = 0.2231 + 0.2231 = 0.4462

Yf= 40,000(0.4462)0.15/1.15 = 30,818 lb/in2

 = 0.88 + 0.12(D/Lc)

Df = 0.1118(1 - r)0.5 = 0.1118(.8).5 = 0.100 in

D = 0.5(0.1118 + 0.100) = 0.1059

Lc = 0.5(0.1118 - 0.100)/sin 12 = 0.0269

 = 0.88 + 0.12(0.1059/0.0269) = 1.35

F = Af Yf(1 + /tan )(ln Ao/Af)

F = 0.007855(30,818)(1 + 0.1/tan 12)(1.35)(0.4462) = 214 lb.

1.5 hp at 90% efficiency = 742.5 ft-lb/sec as before in the first draw.

P = Fv = 214v = 742.5

v = 742.5/214 = 3.47 ft/sec

Note: The calculations indicate that the second draw die is the limiting step in the drawing sequence. The first operation would have to be operated at well below its maximum possible speed; or the second draw die could be powered by a higher horsepower motor; or the reductions to achieve the two stages could be reallocated to achieve a higher reduction in the first drawing operation.