20 HEAT TREATMENT OF METALS

### Review Questions

- Why are metals heat treated?

- Answer. Metals are heat-treated to effect metallurgical changes that beneficially alter properties.

- Identify the important reasons why metals are annealed.

- Answer. Reasons for annealing include (1) to reduce brittleness and improve toughness, (2) to alter microstructure so that desirable mechanical properties can be obtained, (3) to soften metals for improved machinability or formability, (4) to recrystallize cold-worked metals, and (5) to relieve residual stresses from prior processes.

- What is the most important heat treatment for hardening steels?

- Answer. The most important heat treatment for steels is martensite formation by heating steel into the austenite region and quenching.

- What is the mechanism by which carbon strengthens steel during heat treatment?

- Answer. When steel containing carbon is heat-treated, martensite is formed which is a hard and brittle non-equilibrium phase of steel. The extreme hardness of martensite results from the lattice strain created by carbon atoms trapped in the body-centered tetragonal structure, thus providing a barrier to slip.

- What information is conveyed by the TTT curve?

- Answer. The time-temperature-transformation (TTT) curve indicates what phases in the iron-carbon phase diagram will be produced under various conditions of cooling.

- What function is served by tempering of martensite?

- Answer. Tempering involves heating and soaking of martensite for about one hour at a temperature below the austenitizing region, followed by slow cooling to reduce brittleness, relieve stresses, and increase toughness and ductility.

- Define hardenability.

- Answer. Hardenability is the relative capacity of a steel to be hardened by transformation to martensite.

- Name some of the elements that have the greatest effect on the hardenability of steel.

- Answer. Important hardenability elements are chromium, manganese, molybdenum, and nickel.

- Indicate how the hardenability alloying elements in steel affect the TTT curve.

- Answer. The hardenability alloying elements operate by pushing the nose of the TTT curve to the right, thereby permitting slower cooling rates for conversion of austenite to martensite.

- Define precipitation hardening.

- Answer. Precipitation hardening is a heat treatment in which very fine particles (precipitates) are formed so that dislocation movement is blocked and the metal is thus strengthened and hardened.

- How does carburizing work?

- Answer. Carburizing adds carbon to the surface of low-C steel, thereby transforming the surface into high-C steel for greater hardening potential.