10 POWDER METALLURGY

##### Review Questions

- Name some of the reasons for the commercial importance of powder metallurgy technology.

- Answer. PM is important because (1) parts can be made to net or near net shape, (2) parts can be made with a controlled level of porosity, (3) certain metals difficult to process by other methods can be processed by PM, and (4) PM allows the formulation of unusual alloys not easily obtained by traditional alloying methods.

- What are some of the disadvantages of PM methods?

- Answer. Disadvantages include (1) high tooling costs, (2) metal powders are expensive, (3) difficulties in storing and handling metallic powders, (4) certain limitations on part geometry imposed by the uniaxial press methods, and (5) variations in density in a PM component can be troublesome.

- What are the principal methods used to produce metallic powders?

- Answer. The powder production methods are (1) atomization - the conversion of molten metal into droplets which solidify into powders; (2) chemical reduction - reducing metallic oxides by use of reducing agents which combine with the oxygen to free the metals in the form of powders; and (3) electrolysis - use of an electrolytic cell to deposit particles of the metal onto the cathode in the cell.

- What are the three basic steps in the conventional powder metallurgy shaping process?

- Answer. The steps are (1) blending and/or mixing, (2) pressing, and (3) sintering.

- What is the technical difference between blending and mixing in powder metallurgy?

- Answer. Blending refers to combining particles of the same chemistry but different sizes, whereas mixing means combining metal powders of different chemistries.

- What are some of the ingredients usually added to the metallic powders during blending and/or mixing?

- Answer. The additives include (1) lubricants, (2) binders, and (3) deflocculants.

- What is meant by the term green compact?

- Answer. The green compact is the pressed but not yet sintered PM part.

- Describe what happens to the individual particles during compaction.

- Answer. Starting with the initial powder arrangement, the particles are first repacked into a more efficient arrangement, followed by deformation of the particles as pressure is increased.

- What are the three steps in the sintering cycle in PM?

- Answer. The three steps in the cycle are (1) preheat, in which lubricants and binders are burned off, (2) sintering, and (3) cool down.

- What are some of the reasons why a controlled atmosphere furnace is desirable in sintering?

- Answer. Some of the purposes of a controlled atmosphere furnace are (1) to protect against oxidation, (2) to provide a reducing atmosphere to remove existing oxides, (3) to provide a carburizing atmosphere, and (4) to remove lubricants and binders from pressing.

- What is the difference between impregnation and infiltration in PM?

Answer. Impregnation is the term used when oil or other fluid (e.g., polymer melt) is permeated into the pores of a sintered PM part, whereas infiltration is an operation in which the pores of the PM part are filled with a molten metal whose melting point is below that of the PM part..

- How is isostatic pressing distinguished from conventional pressing and sintering in PM?

- Answer. Isostatic pressing applies hydrostatic pressure to all sides of the mold, whereas conventional pressing is uniaxial.

- Describe liquid phase sintering.

- Answer. Liquid phase sintering occurs when two metals of different melting temperatures are sintered at a temperature between their melting points.  Accordingly, one metal melts, thoroughly wetting the solid particles and creating a strong bonding between the metals upon solidification.

- What are the two basic classes of metal powders as far as chemistry is concerned?

- Answer. The two classes are (1) elemental powders - powders of pure metal such as iron or copper, and (2) pre-alloyed powders - powders of alloys such as stainless steel or brass.

- Why is PM technology so well suited to the production of gears and bearings?

Answer. The reasons are (1) the geometries of these parts lend themselves to conventional PM pressing, which consists of pressing in one direction, and (2) the porosity allows impregnation of the PM parts with lubricants.

# Problems

- In a certain pressing operation, the metallic powder fed into the open die has a packing factor of 0.5. The pressing operation reduces the powders to 2/3 of their starting volume. In the subsequent sintering operation, shrinkage amounts to 10% on a volume basis. Given that these are the only factors that affect the structure of the finished part, determine its final porosity.

- Solution: Packing factor = bulk density / true density

- Density = (specific volume)-1

- Packing factor = true specific volume / bulk specific volume

- Pressing reduces bulk specific volume to 2/3 = 0.667

- Sintering further reduces the bulk specific volume to 0.90 of value after pressing.

- Let true specific volume = 1.0

- Thus for a packing factor of 0.5, bulk specific volume = 2.0.

- Packing factor after pressing and sintering = 1.0/(2.0 x .667 x .90) = 1.0/1.2 = 0.833

- By Eq. (18.7), porosity = 1 - 0.833 = 0.167

- A bearing of simple geometry is to be pressed out of bronze powders, using a compacting pressure of 207 MPa. The outside diameter = 44 mm, the inside diameter = 22 mm, and the length of the bearing = 25 mm. What is the required press tonnage to perform this operation?

- Solution: Projected area of part Ap = 0.25(Do2 - Di2) = 0.25(442 - 222) = 1140.4 mm2

- F = Appc = 1140.4(207) = 236,062 N

- The part shown in Figure P10.3 is to be pressed of iron powders using a compaction pressure of 75,000 lb/in2. Dimensions are inches. Determine (a) the most appropriate pressing direction, (b) the required press tonnage to perform this operation, and (c) the final weight of the part if the porosity is 10%. Assume shrinkage during sintering can be neglected.

Solution: (a) Most appropriate pressing direction is parallel to the part axis.

(b) Press tonnage F = Appc

Projected area of part Ap = 0.25(Do2 - Di2) =  0.25(2.82 - 0.8752) = 5.556 in2

F = Appc = 5.556(75,000) = 416,715 lb = 208 tons.

(c) V = 0.25(2.82 - 0.8752)(0.5) + 0.25(2.82 - 1.52)(1.25 - 0.5) = 0.25(3.5372 + 4.1925)

= 6.071 in3

From Table 4.1, density of iron  = 0.284 lb/in3.

At 10% porosity, part weight W = 6.071(0.284)(0.90) = 1.55 lb.

- For each of the four part drawings in Figure P10.4, indicate which PM class the parts belong to, whether the part must be pressed from one or two directions, and how many levels of press control will be required? Dimensions are mm.

Solution: (a) Class II, 2 directions because of axial thickness, one level of press control.

(b) Class I, one direction part is relatively thin, one level of press control.

(c) Class IV, 2 directions of pressing, 3 levels of press control required.

(d) Class IV, 2 directions of pressing, 4 or 5 levels of press control due to multiple steps in part design.