8 SHAPING PROCESSES FOR PLASTICS

##### Review Questions

- What are some of the reasons why plastic shaping processes are important?

- Answer. The reasons include (1) many of the processes are net shape processes; (2) in general, less energy is employed than in metalworking processes; (3) lower temperatures are required to process plastics than metals or ceramics; (4) there is great flexibility in geometry; and (5) painting and other finishing processes are generally not required.

- Identify the main categories of plastics shaping processes, as classified by the resulting product geometry.

- Answer. The categories are (1) continuous extruded products with constant cross section other than sheets, films, and filaments; (2) continuous sheets and films; (3) continuous filaments (fibers); (4) molded parts that are mostly solid; (5) hollow molded parts with relatively thin walls; (6) discrete parts made of formed sheets and films; (7) castings; and (8) foamed products.

- Viscosity is an important property of a polymer melt in plastics shaping processes. Upon what parameters does viscosity depend?

- Answer. Viscosity of a polymer melt depends on (1) temperature and (2) shear rate. Also, (3) the molecular weight of the polymer affects viscosity.

- How does the viscosity of a polymer melt differ from most fluids that are Newtonian.

- Answer. A polymer melt exhibits pseudoplasticity, which means that its value decreases with increasing shear rate.

- What does viscoelasticity mean, when applied to a polymer melt?

- Answer. Viscoelasticity is a combination of viscous and elastic properties which cause the melt to exhibit memory - the tendency to return to its previous shape, as exhibited by die swell in extrusion.

- Define die swell in extrusion.

- Answer. Die swell is the tendency of the extrudate to expand in cross-sectional dimensions immediately on exiting the die orifice. It results from the viscoelastic properties of the polymer melt.

- Briefly describe the plastic extrusion process.

- Answer. In plastic extrusion, a polymer melt is compressed to flow through a die orifice and thus the continuous length of the plastic assumes a cross-sectional shape that is approximately the same as that of the orifice.

- The barrel and screw of an extruder are generally divided into three sections; identify the sections.

- Answer. The sections are (1) the feed section, in which the feed stock is fed from the hopper and heated; (2) the compression section, in which the polymer changes to a viscous fluid; and (3) the metering section, in which pressure is developed to pump the plastic through the die orifice.

- What are the functions of the screen pack and breaker plate at the die end of the extruder barrel?

- Answer. The functions are to (1) filter dirt and lumps, (2) build pressure, (3) straighten the flow and remove memory of the polymer melt.

- What are the various forms of extruded shapes and corresponding dies?

- Answer. The shapes are (1) solid profiles, such as rounds and L-shapes; (2) hollow profiles, such as tubes; (3) wire and cable coating; (4) sheet and film; and (5) filaments (continuous fibers).

- What is the distinction between plastic sheet and film?

- Answer. The distinction is based on thickness. Sheet stock has a thickness greater than 0.5 mm (0.020 in), while film stock is less than 0.5 mm (0.020 in) thick.

- What is the blown-film process for producing film stock?

Answer. The blown-film process is a widely used process for making thin polyethylene film for packaging. It combines extrusion and blowing to produce a tube of thin film. The process begins with the extrusion of a tube that is immediately drawn upward while still molten and simultaneously expanded in size by air inflated into it through the die mandrel.

- Describe the calendering process.

Answer. Calendering is a process for producing sheet and film stock out of rubber or rubbery thermoplastics such as plasticized PVC. In the process, the initial feedstock is passed through a series of rolls to work the material and reduce its thickness to the desired gage.

- Polymer fibers and filaments are used in several applications; what is the most important commercial application?

- Answer. Textiles.

- What is the technical difference between a fiber and a filament?

- Answer. A fiber is a long, thin strand of material of finite length; a filament of continuous length.

- Briefly describe the injection molding process.

- Answer. Injection molding is a process in which a polymer is heated to a highly plastic state and forced to flow under high pressure into a mold cavity, where it solidifies. The molding is then removed from the cavity.

- An injection-molding machine is divided into two principal components. Name them.

- Answer. The components of an injection-molding machine are (1) the injection unit and (2) the clamping unit.

- What is the function of gates in injection molds?

- Answer. The function of gates in an injection mold is to constrict the flow of molten plastic into the cavity, which increases the shear rate and reduces the viscosity of the polymer melt.

- What are the advantages of a three-plate mold over a two-plate mold in injection molding?

- Answer. As the mold opens, the three-plate mold automatically separates the molded part(s) from the runner system.

- Discuss some of the defects that can occur in plastic injection molding.

- Answer. The defects include (1) short shots, in which the polymer melt solidifies before filling the cavity; (2) flashing, in which the polymer melt is squeezed into the parting surfaces between the mold halves and around ejection pins; (3) sink marks, in which the surface is drawn into the molding by contraction of internal material; and (4) weld lines where the melt has flowed around a core or other convex detail in the mold cavity and met from opposite directions, thus resulting in mechanical properties that are inferior to those in the rest of the part.

- What are the significant differences in the equipment and operating procedures between injection molding of thermoplastics and injection molding of thermosets?

- Answer. The differences in injection molding of thermosets are (1) shorter barrel length, (2) lower temperatures in the barrel, these first two reasons to prevent premature curing; and (3) use of a heated mold to cause cross-linking of the TS polymer.

- What is reaction injection molding?

- Answer. Reaction injection molding involves the mixing of two highly reactive liquid ingredients and immediately injecting the mixture into a mold cavity where chemical reactions leading to solidification occur. The two ingredients form the components used in catalyst-activated or mixing-activated thermoset systems.

- What kinds of products are produced by blow molding?

- Answer. Blow molding is used to produce hollow, seamless containers, such as bottles.

- What is the form of the starting material in thermoforming?

- Answer. Thermoforming starts with a thermoplastic sheet or film.

- What is the difference between a positive mold and a negative mold in thermoforming?

- Answer. A positive mold has a convex shape; a negative mold has a concave cavity.

- Why are the molds generally more costly in mechanical thermoforming than in pressure or vacuum thermoforming?

- Answer. In mechanical thermoforming, matching mold halves are required; while in other thermoforming processes, only one mold form is required.

- What are some of the general considerations that product designers must keep in mind when designing components out of plastics?

Answer. Some of the general considerations are the following: (1) Plastics are not as strong or stiff as metals and should not be used in applications where high stresses will be encountered. (2) Impact resistance of plastics is general good, better than many ceramics. (3) Service temperatures of plastics are limited relative to engineering metals and ceramics. (4) Thermal expansion is greater for plastics than metals; so dimensional changes due to temperature variations are much more significant than for metals. (5) Many types of plastics degrade from sunlight and certain other forms of radiation. Also, some plastics degrade in oxygen and ozone atmospheres. Finally, plastics are soluble in many common solvents.

# Problems

- The diameter of an extruder barrel is 65 mm and its length = 1.75 m. The screw rotates at 55 rev/min. The screw channel depth = 5.0 mm, and the flight angle = 18. The head pressure at the die end of the barrel is 5.0 x 106 Pa. The viscosity of the polymer melt is given as 100 Pa-s. Find the volume flow rate of the plastic in the barrel.

- Solution: Qd = 0.52(65x10-3)2(55/60)(5x10-3)sin 18 cos 18 = 95,560x10-9(0.3090)(0.9510)

- = 28.081 x 10-6 m3/s

- p = 5 MPa = 5x106 n/m2

- Qb = (5x106)(65x10-3)(5x10-3)3(sin 18)2/12(100)(1.75) = 5.804(10-6) m3/s

- Qx = 28.081 - 5.804 = 22.277 x 10-6 m3/s.

- An extruder barrel has a diameter of 110 mm and a length of 3.0 m. The screw channel depth = 7.0 mm, and its pitch = 95 mm. The viscosity of the polymer melt is 105 Pa-s, and the head pressure in the barrel is 4.0 MPa. What rotational speed of the screw is required to achieve a volumetric flow rate of 90 cm3/s?

- Solution: A = tan-1(p/(πD)) = tan-1(95/110) = 15.37

- Qd = 0.5π2 D2 N dc sinAcosA = 0.52(0.110)2(N)(7.0x10-3)sin 15.37 cos 15.37

- = 106.8 N x 10-6 m3/s

- Qb = (4x106)(0.110)(7x10-3)3(sin 15.37)2/12(105)(3.0) = 8.81 x 10-6 m3/s

- Qx = Qd - Qb = 106.8 N x 10-6 – 8.81 x 10-6 = 90 x 10-6 m3/s

- 106.8 N = 90.0 + 8.81 = 98.81

- N = 98.81/106.8 = 0.9252 rev/s = 55.51 rev/min.

- An extruder has diameter = 80 mm and length = 2.0 m. Its screw has a channel depth = 5 mm, flight angle = 18 degrees, and it rotates at 1 rev/sec. The plastic melt has a shear viscosity = 150 Pa-s. Determine the extruder characteristic by computing Qmax and pmax and then finding the equation of the straight line between them.

- Solution: Qmax = Qd = 0.52(0.08)2(1)(5x10-3)sin 18 cos 18 = 0.158 x 10-3(0.3090)(0.9510)

- = 46.4 x 10-6 m3/s

- pmax = 6(0.08)(1)(2)(150)(cot 18)/(5x10-3)2 = 452.4(3.077)/25x10-6 = 55 x 106 Pa = 55 MPa

- Qx = 46.4 x 10-6 - (46.4x10-6/55)p

- Qx = 46.4 x 10-6 - 0.8436 x 10-6 p, where p has units of MPa

- Determine the helix angle A such that the screw pitch p is equal to the screw diameter D. This is called the "square" angle in plastics extrusion - the angle that provides a flight advance equal to one diameter for each rotation of the screw.

- Solution: Assume flight land = zero.

- From Eq. (8.4), tan A = pitch/D

- If pitch = D, then A = tan-1(1/) = 17.66

- An extruder barrel has a diameter of 2.5 in. The screw rotates at 60 rev/min; its channel depth = 0.20 in, and its flight angle = 17.5. The head pressure at the die end of the barrel is 800 lb/in2 and the length of the barrel is 50 in. The viscosity of the polymer melt is 122 x 10-4 lb-sec/in2. Determine the volume flow rate of the plastic in the barrel.

- Solution: Qd = 0.52(2.5)2(1)(.2)sin 17.5 cos 17.5 = 0.5(12.337)(0.3007)(0.9537) = 1.769 in3/sec

- Qb = (800)(2.5)(.2)3(sin 17.5)2/12(122x10-4)(50) = 0.621 in3/sec

- Qx = 1.769 - 0.621 = 1.148 in3/sec.

- An extruder barrel has a diameter of 4.0 in and an L/D ratio of 28. The screw channel depth = 0.25 in, and its pitch = 4.8 in. It rotates at 60 rev/min. The viscosity of the polymer melt is 100 x 10-4 lb-sec/in2. What head pressure is required to obtain a volume flow rate = 150 in3/min?

- Solution: A = tan-1(pitch/D) = tan-1(4.8/4) = 20.9

- Qd = 0.52(4)2(1)(0.25)sin 20.9 cos 20.9 = 19.74(0.3567)(0.9342) = 6.578 in3/sec = 394.66 in3/min

- Qx = Qd - Qb = 394.66 - Qd = 150

- Qb = 394.66 - 150 = 244.66 in3/min = 4.078 in3/sec

- L = 4(28) = 112 in.

- Qb = p(4)(0.25)3(sin 20.9)2/(12(100x10-4)(112)) = 4.078

- 0.0018592 p = 4.078

- p = 2193.4 lb/in2

- An extruder has barrel diameter and length of 100 mm and 2.8 m, respectively. The screw rotational speed = 50 rev/min, channel depth = 7.5 mm, and flight angle = 17. The plastic melt has a shear viscosity = 175 Pa-s. Determine: (a) the extruder characteristic, (b) the shape factor Ks for a circular die opening with diameter = 3.0 mm and length = 12.0 mm, and (c) the operating point (Q and p).

- Solution: Qmax = Qd  = 0.52(.1)2(50/60)(7.5x10-3) sin 17 cos 17 = 308.4 x 10-6(0.2924)(0.9563)

- = 86.2 x 10-6 m3/s

- pmax = 6(.1)(50/60)(2.8)(175)(cot 17)/(7.5x10-3)2 = 44.75 x 106 Pa =44.75 MPa

- Qx = 86.2 x 10-6 - 1.926 x 10-12 p, where p has units of Pa

- (b) Given: Dd = 3 mm, Ld = 12 mm.

- Ks = (3 x 10-3)4/(128(175)(12 x 10-3)) = 0.9467 x 10-12

- (c) 0.9467 x 10-12 p = 86.2 x 10-6 - 1.926 x 10-12 p

- 2.8727 x 10-12 p = 86.2 x 10-6

- p = 30.0 x 106 Pa = 30 MPa

- Qx = 0.9467 x 10-12 (30 x 106) = 28.4 x 10-6 m3/s

- Check with extruder characteristic: Qx = 86.2 x 10-6 - 1.926 x 10-12 (30 x 106) = 28.4 x 10-6 m3/s.

- Consider an extruder in which the barrel diameter = 4.5 in and length = 11 ft. The extruder screw rotates at 60 rev/min; it has channel depth = 0.35 in and flight angle = 20. The plastic melt has a shear viscosity = 125 x 10-4 lb-sec/in2. Determine: (a) Qmax and pmax; (b) the shape factor Ks for a circular die opening in which Dd = 0.312 in and Ld = 0.75 in; and (c) the values of Q and p at the operating point.

- Solution: (a) Qmax =  0.52(4.5)2(1)(0.35)sin 20 cos 20 = 34.975(0.342)(0.9397) = 11.24 in3/sec

- pmax = 6(4.5)(1)(132)(0.0125)(cot 20)/(0.35)2 = 3139 lb/in2

- (b) Given: Dd = 0.312 in., Ld = 0.75 in.

- Ks = (0.312)4/128(0.0125)(0.75) = 0.024808

- (c) From (a), Qx = Qmax - (Qmax/pmax)p = 11.24 - 0.003581p

- From (b), Qx = 0.024808p

- Combining, .024808p = 11.24 - .003581p

- 0.02839p = 11.24		p = 395.9 lb/in2

- Qx = 11.24 - 0.003581(395.9) = 9.82 in3/sec

- The specified dimension = 225.00 mm for a certain injection molded part made of ABS. Compute the corresponding dimension to which the mold cavity should be machined, using the value of shrinkage given in Table 8.1.

- Solution: S = 0.006 for ABS from Table 8.1.

- Dc = 225.00 + 225.00(0.006) + 225.00(0.006)2 = 225.00 + 1.35 + 0.0081 = 226.36 mm.

- The part dimension for a certain injection molded part made of polycarbonate is specified as 3.75 in. Compute the corresponding dimension to which the mold cavity should be machined, using the value of shrinkage given in Table 8.1.

- Solution: S = 0.007 for polycarbonate from Table 8.1.

- Dc = 3.75 + 3.75(0.007) + 3.75 (0.007)2 = 3.75 + 0.0263 + 0.0002 = 3.7765 in.

- The foreman in the injection molding department says that a polyethylene part produced in one of the operations has greater shrinkage than the calculations indicate it should have. The important dimension of the part is specified as 112.5 0.25 mm. However, the actual molded part measures 112.02 mm. (a) As a first step, the corresponding mold cavity dimension should be checked. Compute the correct value of the mold dimension, given that the shrinkage value for polyethylene is 0.025 (from Table 8.1). (b) What adjustments in process parameters could be made to reduce the amount of shrinkage?

Solution: (a) Given: S = 0.025, Dc = 112.5 + 112.5(.025) + 112.5(.025)2 = 115.383 mm

(b) Adjustments to reduce shrinkage include: (1) increase injection pressure, (2) increase compaction time, and (3) increase molding temperatures.

- The extrusion die for a polyethylene parison used in blow molding has a mean diameter of 18.0 mm. The size of the ring opening in the die is 2.0 mm. The mean diameter of the parison is observed to swell to a size of 21.5 mm after exiting the die orifice. If the diameter of the blow molded container is to be 150 mm, determine (a) the corresponding wall thickness of the container and (b) the wall thickness of the parison.

- Solution: (a) rs = Dp/Dd = 21.5/18.0 = 1.194

- tm = tp Dp/Dm = rs td Dp/Dm = (1.194)(2.0)(21.5)/150.0 = 0.342 mm

- (b) tp = rs td = (1.194)(2.0) = 2.388 mm

- A parison is extruded from a die with outside diameter = 11.5 mm and inside diameter = 7.5 mm. The observed die swell is 1.25. The parison is used to blow mold a beverage container whose outside diameter = 112 mm (a standard size 2-liter soda bottle). (a) What is the corresponding wall thickness of the container? (b) Obtain an empty 2-liter plastic soda bottle and (carefully) cut it across the diameter. Using a micrometer, measure the wall thickness to compare with your answer in (a).

- Solution: (a) Dd = (11.5 + 7.5)/2 = 9.5 mm, and td = (11.5 - 7.5)/2 = 2.0 mm

- tm = (1.25)2(2.0)(9.5)/112 = 0.265 mm (= 0.010 in)

- (b) Measured value should be close to calculated value. Some wall thicknesses are less.

- An extrusion operation is used to produce a parison whose mean diameter = 27 mm. The inside and outside diameters of the die that produced the parison are 18 mm and 22 mm, respectively. If the minimum wall thickness of the blow-molded container is to be 0.40 mm, what is the maximum possible diameter of the blow mold?

- Solution: Dd = (22 + 18)/2 = 20 mm, and td = (22 - 18)/2 = 2 mm

- rs = 27/20 = 1.35

- Rearranging Eq. (8.22) in text, Dm = rsd2tdDd/tm = (1.35)2(2)(20)/(0.40) = 182.25 mm

- A rotational molding operation is to be used to mold a hollow playing ball out of polypropylene. The ball will be 1.25 ft in diameter and its wall thickness should be 3/32 in. What weight of PP powder should be loaded into the mold in order to meet these specifications? The specific gravity of the PP grade is 0.90, and the density of water is 62.4 lb/ft3.

Solution: Density  = specific gravity of polymer x ρwater = 0.90(62.4 lb/ft3) = 56.2 lb/ft3

Convert to lb/in3: ρ = 56.2 lb/ft3 /(1728 in3/ft3) = 0.0325 lb/in3

- Volume = (Do3 - Di3)/6 = 0.16667[(1.25x12)3 - (1.25x12 - 3/16)3] = 10.91 in3

- Weight W = (10.91)(0.0325) = 0.355 lb.

- The problem in a certain thermoforming operation is that there is too much thinning in the walls of the large cup-shaped part. The operation is conventional pressure thermoforming using a positive mold, and the plastic is an ABS sheet with an initial thickness of 3.2 mm. (a) Why is thinning occurring in the walls of the cup? (b) What changes could be made in the operation to correct the problem?

Solution: (a) As the starting flat sheet is draped over the convex cup-shaped mold, the portion contacting the base of the cup experiences little stretching. However, the remaining portions of the sheet must be stretched significantly to conform to the sides of the cup. Hence, thinning in these sides results.

(b) The problem could be solved by fabricating a negative mold to replace the current positive mold, since a negative mold will distribute the material more uniformly and result in approximately equal thinning throughout the sheet.