19 NONTRADITIONAL MACHINING PROCESSES

# Review Questions

- Why are the nontraditional material removal processes important?

- Answer. Reasons for importance of nontraditional material removal processes are (1) the need to shape new metal alloys and non-metals that are difficult to machine by conventional processes; (2) the requirement of unusual and complex workpart geometries; and (3) the need to avoid surface damage which is often associated with conventional machining.

- There are four categories of nontraditional machining processes, based on principal energy form.  Name the four categories.

- Answer. The four categories are (1) mechanical, but not including conventional machining; (2) electrical; (3) thermal; and (4) chemical.

- How does the ultrasonic machining process work?

- Answer. In ultrasonic machining, abrasives contained in a slurry are driven at high velocity against the work by a tool vibrating at low amplitude and high frequency. The tool oscillates in a direction perpendicular to the work surface, and is fed slowly into the work, so that the shape of the tool is formed in the part. The abrasives, impinging against the work surface, perform the chip removal.

- Describe the water jet cutting process.

- Answer. Water jet cutting uses a high-pressure, high-velocity stream of water directed at the work surface to cut the work.

- What is the difference between water jet cutting, abrasive water jet cutting, and abrasive jet cutting?

- Answer. WJC cuts with a narrow, high velocity water stream; AWJC adds abrasive grits to the water stream; and AJM cuts with abrasive particles that have been added to a high velocity air stream.

- Name the three main types of electrochemical machining.

- Answer. The three types are electrochemical machining, deburring, and grinding.

- Identify the two significant disadvantages of electrochemical machining.

- Answer. Disadvantages of ECM include (1) cost of electrical power to operate the process, and (2) cost of disposal of electrolyte sludge.

- How does increasing discharge current affect metal removal rate and surface finish in electric discharge machining?

- Answer. As discharge current increases, metal removal rate increases and surface finish is degraded.

- What is meant by the term overcut in electric discharge machining?

- Answer. Overcut refers to the gap between the electrode (tool) in EDM on each side of the tool and the machined hole, cavity, or kerf (in wire EDM).

- Name the four principal steps in chemical machining.

- Answer. The four steps are (1) cleaning, (2) masking, (3) etching, and (4) demasking.

- What are the three methods of performing the masking step in chemical machining?

- Answer. The three masking methods are (1) cut and peel, (2) screen resist, and (3) photographic resist.

- What is a photoresist in chemical machining?

Answer. A photoresist is a masking material that is sensitive to light.  When exposed, it chemically transforms and can be removed from the surface of the work, leaving the desired surface unprotected by the maskant.

# Problems

- For the following application, identify one or more nontraditional machining processes that might be used, and present arguments to support your selection. Assume that either the part geometry or the work material (or both) preclude the use of conventional machining. The application is a matrix of 0.1 mm (0.004 in) diameter holes in a plate of 3.2 mm (0.125 in) thick hardened tool steel. The matrix is rectangular, 75 by 125 mm (3.0 by 5.0 in) with the separation between holes in each direction = 1.6 mm ( 0.0625 in).

- Solution: Application: matrix of holes in 3.2 mm (0.125 in) thick hardened steel, hole diameter = 0.1 mm (0.004 in), separation between holes = 1.6 mm (0.0625 in). Possible processes: EBM and LBM can make holes of this size with depth-to-diameter ratios as large as 0.125/0.004 = 31.25.

- For the following application, identify one or more nontraditional machining processes that might be used, and present arguments to support your selection. Assume that either the part geometry or the work material (or both) preclude the use of conventional machining. The application is an engraved aluminum printing plate to be used in an offset printing press to make 275 by 350 mm (11 by 14 in) posters of Lincoln's Gettysburg address.

- Solution: Application: engraved aluminum printing press plate for 275 by 350 mm (11 by 14 in) posters. Possible process: photochemical engraving; making a negative of the speech and transferring this to either a silk screen or directly to the photoresist would seem to be the most straightforward methods.

- For the following application, identify one or more nontraditional machining processes that might be used, and present arguments to support your selection. Assume that either the part geometry or the work material (or both) preclude the use of conventional machining. The application is a through-hole in the shape of the letter L in a 12.5 mm (0.5 in) thick plate of glass. The size of the "L" is 25 by 15 mm (1.0 by 0.6 in) and the width of the hole is 3 mm (1/8 in).

- Solution: Application: through-hole in the shape of the letter “L” drilled through 12.5 mm (0.5-in) thick plate glass. Possible process: USM works on glass and other brittle non-metallic materials. This is probably the best process.

- For the following application, identify one or more nontraditional machining processes that might be used, and present arguments to support your selection. Assume that either the part geometry or the work material (or both) preclude the use of conventional machining. The application is a blind-hole in the shape of the letter G in a 50 mm (2.0 in) cube of steel. The overall size of the "G" is 25 by 19 mm (1.0 by 0.75 in), the depth of the hole is 3.8 mm (0.15 in), and its width is 3 mm (1/8 in).

- Solution: Application: the letter “G” drilled to a depth of 3.8 mm (0.15 in) in a cube of steel. Possible processes: ECM and EDM would be useful for pocketing operations such as this.

- A furniture company that makes upholstered chairs and sofas must cut large quantities of fabrics. Many of these fabrics are strong and wear-resistant, which properties make them difficult to cut. What nontraditional process(es) would you recommend to the company for this application? Justify your answer by indicating the characteristics of the process that make it attractive.

Solution: Water jet cutting would be an ideal process for this application. WJC cuts through fabrics quickly and cleanly, and the process could be readily automated.

- The frontal working area of the electrode in an ECM operation is 2000 mm2. The applied current = 1800 amps and the voltage = 12 volts. The material being cut is nickel (valence = 2). (a) If the process is 90% efficient, determine the rate of metal removal in mm3/min. (b) If the resistivity of the electrolyte = 140 ohm-mm, determine the working gap.

- Solution: (a) From Table 19.1, C = 3.42 x 10-2 mm3/A-s

- From Eq. (19.6) RMR = frA = (CI/A)A = CI = (3.42 x 10-2 mm3/A-s)(1800 A)

- = 6156 x 10-2 mm3/s = 61.56 mm3/s = 3693.6 mm3/min

- At 90% efficiency RMR = 0.9(3693.6 mm3/min) = 3324.2 mm3/min

- (b) Given resistivity r = 140 ohm-mm, I = EA/gr in Eq. (19.2). Rearranging, g = EA/Ir

- g = (12 V)(2000 mm2)/(1800 A)(140 ohm-mm) = 0.095 mm

- In an electrochemical machining operation, the frontal working area of the electrode is 2.5 in2. The applied current = 1500 amps, and the voltage = 12 volts. The work material is pure aluminum. (a) If the ECM process is 90 percent efficient, determine the rate of metal removal in in3/hr. (b) If the resistivity of the electrolyte = 6.2 ohm-in, determine the working gap.

- Solution: (a) From Table 19.1, C = 0.000126 in3/A-min

- RMR = frA = (CI/A)(A) = CI

- RMR = CI = 0.000126(1500) = 0.189 in3/min at 100% efficiency.

- At 90% efficiency RMR = 0.189(0.90) = 0.1701 in3/min = 10.206 in3/hr.

- (b) I = EA/gr;	Rearranging, g = EA/Ir = 12(2.5)/(1500 x 6.2) = 0.0032 in

- A square hole is to be cut using ECM through a plate of pure copper (valence = 1) that is 20 mm thick. The hole is 25 mm on each side, but the electrode used to cut the hole is slightly less that 25 mm on its sides to allow for overcut, and its shape includes a hole in its center to permit the flow of electrolyte and to reduce the area of the cut. This tool design results in a frontal area of 200 mm2. The applied current = 1000 amps. Using an efficiency of 95%, determine how long it will take to cut the hole.

- Solution: From Table 19.1, C = 7.35 x 10-2 mm3/A-s

- From Eq. (19.6) fr = CI/A = (7.35 x 10-2 mm3/A-s)(1000 A)/(200 mm2) = 0.3675 mm/s

- At 95% efficiency, fr = 0.95(0.3675 mm/s) = 0.349 mm/s

- Time to machine = (20 mm)/(0.349 mm/s) = 57.3 s

- A 3.5 in diameter through hole is to be cut in a block of pure iron (Valence = 2) by electrochemical machining. The block is 2.0 in thick. To speed the cutting process, the electrode tool will have a center hole of 3.0 in which will produce a center core that can be removed after the tool breaks through. The outside diameter of the electrode is undersized to allow for overcut. The overcut is expected to be 0.005 in on a side. If the efficiency of the ECM operation is 90%, what current will be required to complete the cutting operation in 20 minutes?

Solution: Electrode frontal gap area A = 0.25(3.52 - 3.02) = 2.553 in2

From Table 19.1, C = 0.000135 in3/A-min

fr = CI/A = 0.000135 I/2.553 = 0.0000529 I in/min at 100% efficiency.

At 90% efficiency fr = 0.9(0.0000529 I) = 0.0000476 I in/min

To cut through a 2.0 inch thickness in 20 minutes requires a feed rate fr = 2.0/20 = 0.1 in/min

fr = 0.1 = 0.0000476 I

I = 0.1/0.0000476 = 2101 A.

- An electric discharge machining operation is performed on two work materials: tungsten and tin. Determine the amount of metal removed in the operation after one hour at a discharge current of 20 amps for each of these metals. Use metric units and express the answers in mm3/hr. Use Table 3.10 to determine melting temperatures for tungsten and tin.

- Solution: From Table 3.10, the melting temperatures for tungsten and tin are 3410C and 232C, respectively. For tungsten, using Eq. (19.7), RMR = KI/Tm1.23 = 664(20)/(34101.23) = 13,280/22,146

- = 0.5997 mm3/s = 2159 mm3/hr

- For tin, RMR = KI/Tm1.23 = 664(20)/(2321.23) = 13,280/812 = 16.355 mm3/s = 58,878 mm3/hr

- An electric discharge machining operation is being performed on two work materials: iron and zinc. Determine the amount of metal removed in the operation after one hour at a discharge amperage = 15 amps for each of these metals. Use U.S. Customary units and express the answer in in3/hr. Use Table 3.10 to determine melting temperatures for iron and zinc.

- Solution: From Table 4.1, the melting temperatures of iron and zinc are 2802F and 787F, respectively. For iron, using Eq. (19.7), RMR = KI/Tm1.23 = 5.08(15)/(28021.23) = 76.2/17,393

- = 0.00438 in3/s = 15.77 in3/hr

- For zinc, RMR = KI/Tm1.23 = 5.08(15)/(7871.23) = 76.2/3648 = 0.02089 in3/s = 75.20 in3/hr

- Suppose the hole in Problem 19.9 were to be cut using EDM rather than ECM. Using a discharge current = 20 amps (which would be typical for EDM), how long would it take to cut the hole? Use Table 3.10 to determine the melting temperature of pure iron.

- Solution: From Table 3.10, the melting temperature of iron is 2802F. Using Eq. (19.7), RMR = 5.08 I/Tm1.23 = 5.08(20)/28021.23 = 101.6/17,393 = 0.00584 in3/min

- Cross-sectional area of tool area A = 0.25(3.52 - 3.02) = 2.553 in2

- fr = RMR/A = 0.00584/2.553 = 0.002293 in/min

- Time to machine the 2.0 inch thickness Tm = 2.0/0.002293 = 874.3 min = 14.57 hr.

- A metal removal rate of 0.01 in3/min is achieved in a certain EDM operation on a pure copper workpart. What metal removal rate would be achieved on nickel in this EDM operation, if the same discharge current were used? Use Table 3.10 to determine the melting temperatures of copper and nickel.

- Solution: From Table 3.10, the melting temperatures of copper and nickel are 1981F and 2651F, respectively. For iron, RMR = 5.08 I/19811.23 = 5.08 I/11,354 = 0.000447 I in3/min

- Given that RMR = 0.01 in3/min

- 0.000447 I = 0.01

- I = 0.01/0.000447 = 22.35 A.

- For = nickel, RMR = 5.08(22.35)/26511.23 = 113.54/16,248 = 0.007 in3/min

- In a wire EDM operation performed on 7-mm-thick C1080 steel using a tungsten wire electrode whose diameter = 0.125 mm, past experience suggests that the overcut will be 0.02 mm, so that the kerf width will be 0.165 mm. Using a discharge current = 10 amps, what is the allowable feed rate that can be used in the operation? Use a melting temperature of 1500C for 1080 steel.

- Solution: Given Tm = 1500C for 1080 steel

- Using Eq. (19.7), RMR = 664(10)/(15001.23) = 6640/8065 = 0.8233 mm3/s

- Frontal area of kerf A = 0.165(7.0) = 1.155 mm2

- fr = 49.4/1.155 = 42.79 mm/min

- A wire EDM operation is to be performed on a slab of ¾-in-thick aluminum using a brass wire electrode whose diameter = 0.005 in. It is anticipated that the overcut will be 0.001 in, so that the kerf width will be 0.007 in. Using a discharge current = 7 amps, what is the expected allowable feed rate that can be used in the operation? The melting temperature of aluminum is 1220F.

- Solution: Using Eq. (19.7), RMR = 5.08(7)/12201.23 = 35.56/6255 = 0.005685 in3/min

- Frontal area of kerf A = 0.75(0.007) = 0.00525 in2

- fr = 0.005685/0.00525 = 1.083 in/min

- Chemical milling is used in an aircraft plant to create pockets in wing sections made of an aluminum alloy. The starting thickness of one workpart of interest is 20 mm. A series of rectangular-shaped pockets 12 mm deep are to be etched with dimensions 200 mm by 400 mm. The corners of each rectangle are radiused to 15 mm. The part is an aluminum alloy and the etchant is NaOH. Use Table 19.2 to determine the penetration rate and etch factor for this combination. Determine (a) metal removal rate in mm3/min, (b) time required to etch to the specified depth, and (c) required dimensions of the opening in the cut and peel maskant to achieve the desired pocket size on the part.

- Solution: From Table 19.2, the penetration rate = 0.025 mm/min and the etch factor = 1.75.

- (a) Neglecting the fact that the initial area would be less than the given dimensions of 200 mm by 400 mm, and that the material removal rate (RMR) would therefore increase during the cut as the area increased, area A = 200 x 400 – (30 x 30 - (15)2) = 80,000 – 193 = 79,807 mm2

- RMR = (0.025 mm/min)(79,807 mm2) = 1995.2 mm3/min

- (b) Time to machine (etch) Tm = 12/0.025 = 480 min = 8.0 hr.

- (c) Given Fe = 1.75, undercut u = d/Fe = 12/1.75 = 6.86 mm

- Maskant opening length = L – 2u = 400 – 2(6.86) = 386.28 mm

- Maskant opening width = W – 2u = 200 – 2(6.86) = 186.28 mm

- Radius on corners = R – u = 15 – 6.86 = 8.14 mm

- In a chemical milling operation on a flat mild steel plate, it is desired to cut an ellipse-shaped pocket to a depth of 0.4 in. The semiaxes of the ellipse are a = 9.0 in and b = 6.0 in. A solution of hydrochloric and nitric acids will be used as the etchant. Use Table 19.2 to determine the penetration rate and etch factor for this combination. Determine (a) metal removal rate in in3/hr, (b) time required to etch to depth, and (c) required dimensions of the opening in the cut and peel maskant required to achieve the desired pocket size on the part.

- Solution: From Table 19.2, the penetration rate = 0.001 in/min and the etch factor = 2.0.

- (a) Neglecting the fact that the initial area would be less than the given dimensions of 9 in by 6 in, and that the material removal rate (RMR) would therefore increase during the cut as the area increased, area of an ellipse A = ab = (9.0)(6.0) = 54 = 169.65 in2

- RMR = (0.001 in/min)(169.65 in2) = 0.16965 in3/min = 10.18 in3/hr

- (b) Time to machine (etch) Tm = 0.4/0.001 = 400 min = 6.67 hr.

- (c) Given Fe = 2.0, undercut u = d/Fe = 0.4/2.0 = 0.2 mm

- This must be doubled to determine the effect on a and b.

- Maskant opening a’ = a – u = 9.0 – 2(0.2) = 8.6 in

- Maskant opening b’ = b – u = 6.0 – 2(0.2) = 5.6 in

- In a certain chemical blanking operation, a sulfuric acid etchant is used to remove material from a sheet of magnesium alloy. The sheet is 0.25 mm thick. The screen resist method of masking was used to permit high production rates to be achieved. As it turns out, the process is producing a large proportion of scrap. Specified tolerances of 0.025 mm are not being achieved. The foreman in the CHM department complains that there must be something wrong with the sulfuric acid. "Perhaps the concentration is incorrect," he suggests. Analyze the problem and recommend a solution.

- Solution: The problem in this chemical blanking operation is that the screen resist method of masking cannot achieve the tolerances specified. The photoresist method should have been used, and the process should be changed over to adopt this method.

- In a chemical blanking operation, stock thickness of the aluminum sheet is 0.015 in. The pattern to be cut out of the sheet is a hole pattern, consisting of a matrix of 0.100 in diameter holes. If photochemical machining is used to cut these holes, and contact printing is used to make the resist (maskant) pattern, determine the diameter of the holes that should be used in the pattern.

Solution: From Table 19.2, Fe = 1.75.

In chemical blanking, etching will occur on both sides of the part. Therefore, the effective hole depth on each side = one-half of the stock thickness = 0.015/2 = 0.0075 in.

Undercut u = 0.0075/1.75 = 0.0043 in

Diameter of opening = 0.100 - 2(0.0043) = 0.0914 in