7 GLASSWORKING

#### Review Questions

- Glass is classified as a ceramic material; yet glass is different from the traditional and new ceramics. What is the difference?

- Answer. Glass is vitreous - it is in the glassy state, whereas traditional and new ceramics are, by and large, polycrystalline materials.

- What is the predominant chemical compound in almost all glass products?

- Answer. Silica - SiO2.

- What are the three basic steps in the glassworking sequence?

- Answer. (1) raw materials preparation and melting, (2) shaping, and (3) heat treatment.  Finishing operations (e.g., grinding, polishing, etching) are performed on some glass products, if needed.

- Describe the spinning process in glassworking.

- Answer. Spinning in glassworking is similar to centrifugal casting in metalworking.  A gob of molten glass is dropped into a conical mold which spins, causing centrifugal force to spread the glass upward onto the mold surface.

- What is the main difference between the press-and-blow and the blow-and-blow shaping processes in glassworking?

- Answer. In the press-and-blow process, the initial forming step is pressing of the part, while the first step in the blow-and-blow process is blowing.

- There are several ways of shaping plate or sheet glass. Name and briefly describe one of them.

- Answer. The methods described in this text are (1) rolling, in which the hot glass is squeezed between opposing cylindrical rolls; and (2) the float process, in which the melted glass flows onto a molten tin surface to achieve uniform thickness and smoothness.

- Describe the Danner process.

- Answer. In the Danner process, molten glass flows around a rotating hollow mandrel through which air is blown while the glass is being drawn. The temperature of the air and its volumetric flow rate as well as the drawing velocity determine the diameter and wall thickness of the tubular cross-section. During hardening, the glass tube is supported by a series of rollers extending beyond the mandrel.

- Name and briefly describe the two processes for forming glass fibers are discussed in the text.

- Answer. The two processes in the text are (1) drawing, in which fine glass fibers are pulled through small orifices in a heated plate; and (2) centrifugal spraying, in which molten glass is forced to flow through small orifices in a rapidly rotating bowl to form glass fibers.

- What is the purpose of annealing in glassworking?

- Answer. Annealing is performed on glass to remove internal stresses that result from shaping and solidification.

- Describe how a piece of glass is heat treated to produce tempered glass.

- Answer. The glass is heated to a temperature above the annealing temperature and the surfaces are then quenched by air jets to cool and harden them while the interior of the piece remains plastic; as the interior cools and contracts, it puts the previously hardened surfaces in compression, which strengthens the glass product.

- Describe the type of material that is commonly used to make windshields for automobiles.

- Answer. Laminated glass, in which two sheets of glass are laminated on either side of a polymer sheet.  This has good impact resistance and does not splinter when broken.