5 FUNDAMENTALS OF METAL CASTING

# Review Questions

- Identify some of the important advantages of shape-casting processes.

- Answer. Advantages include (1) complex part geometries are possible; (2) some casting operations are net shape processes, meaning that no further manufacturing operations are needed to accomplish the final part geometry; (3) very large parts are possible; (4) casting is applicable to any metal that can be melted; and (5) some casting processes are suited to mass production.

- What are some of the limitations and disadvantages of casting?

- Answer. Disadvantages include (1) limitations on mechanical strength properties; (2) porosity; (3) poor dimensional accuracy; (4) safety hazards due to handling of hot metals; and (5) environmental problems.

- What is a factory that performs casting operations usually called?

- Answer. A foundry.

- What is the difference between an open mold and a closed mold?

- Answer. An open mold is open to the atmosphere at the top; it is an open container in the desired shape which must be flat at the top. A closed mold has a cavity that is entirely enclosed by the mold, with a passageway (called the gating system) leading from the outside into the cavity.  Molten metal is poured into this gating system to fill the mold.

- Name the two basic mold types that distinguish casting processes.

- Answer. The two mold types are (1) expendable molds and (2) permanent molds.

- Which casting process is the most important commercially?

- Answer. Sand casting is the most important casting process.

- What is the difference between a pattern and a core in sand molding?

- Answer. The pattern determines the external shape of the cast part, while a core determines its internal geometry if the casting includes a cavity.

- What is meant by the term superheat?

- Answer. Superheat is the temperature difference above the melting point at which the molten metal is poured.  The term also refers to the amount of heat that is removed from the molten metal between pouring and solidification.

- Why should turbulent flow of molten metal into the mold be avoided?

- Answer. Turbulence causes the following problems: (1) it accelerates formation of oxides in the solidified metal, and (2) it causes mold erosion or gradual wearing away of the mold due to impact of molten metal.

- What is the continuity law as it applies to the flow of molten metal in casting?

- Answer. The continuity law, or continuity equation, indicates that the volumetric flow rate is constant throughout the liquid flow.

- What does heat of fusion mean in casting?

- Answer. Heat of fusion is the amount of heat energy required to transform the metal from solid state to liquid state.

- How does solidification of alloys differ from solidification of pure metals?

- Answer. Pure metals solidify at a single temperature equal to the melting point. Most alloys (exceptions are eutectic alloys) start to solidify at the liquidus and complete solidification occurs at the solidus, where the liquidus is a higher temperature than the solidus.

- What is a eutectic alloy?

- Answer. A eutectic alloy is a particular composition in an alloy system for which the solidus and liquidus temperatures are equal.  The temperature is called the eutectic temperature.  Hence, solidification occurs at a single temperature, rather than over a temperature range.

- What is the relationship known as Chvorinov's rule in casting?

- Answer. Chvorinov's rule is summarized: TTS = Cm(V/A)2, where TTS = total solidification time, Cm = mold constant, V = volume of casting, and A = surface area of casting.

- Identify the three sources of contraction in a metal casting after pouring.

- Answer. The three contractions occur due to (1) contraction of the molten metal after pouring, (2) solidification shrinkage during transformation of state from liquid to solid, and (3) thermal contraction in the solid state.

# Problems

- The downsprue leading into the runner of a certain mold has a length = 175 mm. The cross-sectional area at the base of the sprue is 400 mm2. The mold cavity has a volume = 0.001 m3. Determine (a) the velocity of the molten metal flowing through the base of the downsprue, (b) the volume rate of flow, and (c) the time required to fill the mold cavity.

- Solution: (a) Velocity v = (2 x 9815 x 175)0.5 = (3,435,096)0.5 = 1853 mm/s

- (b) Volume flow rate Q = vA = 1853 x 400 = 741,200 mm3/s

- (c) Time to fill cavity TMF = V/Q = 1,000,000/741,200 = 1.35 s

- A mold has a downsprue of length = 6.0 in. The cross-sectional area at the bottom of the sprue is 0.5 in2. The sprue leads into a horizontal runner which feeds the mold cavity, whose volume = 75 in3. Determine (a) the velocity of the molten metal flowing through the base of the downsprue, (b) the volume rate of flow, and (c) the time required to fill the mold cavity.

- Solution: (a) Velocity v = (2 x 32.2 x 12 x 6.0)0.5 = (4636.8)0.5 = 68.1 in/sec

- (b) Volume flow rate Q = vA = 68.1 x 0.5 = 34.05 in3/sec

- (c) Time to fill cavity TMF = V/Q = 75.0/34.05 = 2.2 sec.

- The flow rate of liquid metal into the downsprue of a mold = 1 liter/sec. The cross-sectional area at the top of the sprue = 800 mm2, and its length = 175 mm. What area should be used at the base of the sprue to avoid aspiration of the molten metal?

- Solution: Flow rate Q = 1.0 L/s = 1,000,000 mm3/s

- Velocity v = (2 x 9815 x 175)0.5 = 1854 mm/s

- Area at base A = 1,000,000/1854 = 540 mm2

- The volume rate of flow of molten metal into the downsprue from the pouring cup is 50 in3/sec. At the top where the pouring cup leads into the downsprue, the cross-sectional area = 1.0 in2. Determine what the area should be at the bottom of the sprue if its length = 8.0 in. It is desired to maintain a constant flow rate, top and bottom, in order to avoid aspiration of the liquid metal.

- Solution: Velocity at base v = (2gh)0.5 = (2 x 32.2 x 12 x 8)0.5 = 78.6 in/sec

- Assuming volumetric continuity, area at base A = (50 in/sec)/(78.6 in/sec) = 0.636 in2

- Molten metal can be poured into the pouring cup of a sand mold at a steady rate of 1000 cm3/s. The molten metal overflows the pouring cup and flows into the downsprue. The cross section of the sprue is round, with a diameter at the top = 3.4 cm. If the sprue is 25 cm long, determine the proper diameter at its base so as to maintain the same volume flow rate.

- Solution: Velocity at base v = (2gh)0.5 = (2 x 981 x 25)0.5 = 221.5 cm/s

- Assuming volumetric continuity, area at base A = (1000 cm/s)/(221.5 cm/s) = 4.51 cm2

- Area of sprue A = D2/4; rearranging, D2 = 4A/ = 4(4.51)/ = 5.74 cm2

- D = 2.39 cm

- Determine the shrink rule to be used by pattern makers for white cast iron. Using the shrinkage value in Table 5.1, express your answer in terms of decimal fraction inches of elongation per foot of length compared to a standard one-foot scale.

Solution: For white cast iron, shrinkage 2.1% from Table 5.1.

Thus, linear contraction = 1.0 – 0.021 = 0.979.

Shrink rule elongation = (0.979)-1 = 1.02145

For a 12-inch rule, L = 1.02145(12) = 12.257 in

Elongation per foot of length = 0.257 in

- Determine the shrink rule to be used by mold makers for die casting of zinc. Using the shrinkage value in Table 5.1, express your answer in terms of decimal mm of elongation per 300 mm of length compared to a standard 300-mm scale.

Solution: For zinc, shrinkage 2.6% from Table 5.1.

Thus, linear contraction = 1.0 – 0.026 = 0.974.

Shrink rule elongation = (0.974)-1 = 1.0267

For a 300-mm rule, L = 1.0267(300) = 308.008 mm

Elongation per 300 mm of length = 8.008 mm

- A flat plate is to be cast in an open mold whose bottom has a square shape that is 200 mm by 200 mm. The mold is 40 mm deep. A total of 1,000,000 mm3 of molten aluminum is poured into the mold. Solidification volumetric shrinkage is known to be 6.0%. Table 5.1 lists the linear shrinkage due to thermal contraction after solidification to be 1.3%. If the availability of molten metal in the mold allows the square shape of the cast plate to maintain its 200 mm by 200 mm dimensions until solidification is completed, determine the final dimensions of the plate.

Solution: The initial volume of liquid metal = 1,000,000 mm3. When poured into the mold it takes the shape of the open mold, which is 200 mm by 200 mm square, or 40,000 mm2. The starting height of the molten metal is 1,000,000 / 40,000 = 25 mm.

Volumetric solidification shrinkage is 6%, so when the aluminum has solidified its volume = 1,000,000(0.94) = 940,000 mm3. Because its base still measures 200 mm by 200 mm due to the flow of liquid metal before solidification, its height has been reduced to 940,000 / 40,000 = 23.5 mm.

Thermal contraction causes a further shrinkage of 1.3%. Thus the final dimensions of the plate are 200(0.987) by 200(0.987) by 23.5(0.987) = 197.40 mm by 197.40 mm by 23.195 mm.

- In the casting of steel under certain mold conditions, the mold constant in Chvorinov's rule is known to be 4.0 min/cm2, based on previous experience. The casting is a flat plate whose length = 30 cm, width = 10 cm, and thickness = 20 mm. Determine how long it will take for the casting to solidify.

- Solution: Volume V = 30 x 10 x 2 = 600 cm3

- Area A = 2(30 x 10 + 30 x 2 + 10 x 2) = 760 cm2

- Chvorinov’s rule: TTS = Cm (V/A)2  = 4(600/760)2 = 2.49 min

- Solve for total solidification time in the previous problem only using an exponent value of 1.9 in Chvorinov's rule instead of 2.0. What adjustment must be made in the units of the mold constant?

- Solution: Chvorinov’s rule: TTS = Cm (V/A)1.9  = 4(600/760)1.9 = 2.55 min

- The units for Cm become min/in1.9 - strange units but consistent with Chvorinov’s empirical rule.

- A disk-shaped part is to be cast out of aluminum. The diameter of the disk = 500 mm and its thickness = 20 mm. If the mold constant = 2.0 sec/mm2 in Chvorinov's rule, how long will it take the casting to solidify?

- Solution: Volume V = D2t/4 = (500)2(20)/4 = 3,926,991 mm3

- Area A = 2D2/4 + Dt = (500)2/2 + (500)(20) = 424,115 mm2

- Chvorinov’s rule: TTS = Cm (V/A)2 = 2.0(3,926,991/424,115)2  = 171.5 s = 2.86 min

- In casting experiments performed using a certain alloy and type of sand mold, it took 155 sec for a cube-shaped casting to solidify. The cube was 50 mm on a side. (a) Determine the value of the mold constant in Chvorinov's rule. (b) If the same alloy and mold type were used, find the total solidification time for a cylindrical casting in which the diameter = 30 mm and length = 50 mm.

- Solution: (a) Volume V = (50)3 = 125,000 mm3

- Area A = 6 x (50)2 = 15,000 mm2

- (V/A) = 125,000/15,000 = 8.333 mm

- Cm = TTS /(V/A)2 = 155/(8.333)2 = 2.232 s/mm2

- (b) Cylindrical casting with D = 30 mm and L = 50 mm.

- Volume V = D2L/4 = (30)2(50)/4 = 35,343 mm3

- Area A = 2D2/4 + DL = (30)2/2 + (30)(50) = 6126 mm2

- V/A = 35,343/6126 = 5.77

- TTS = 2.232 (5.77)2 = 74.3 s = 1.24 min.

- A steel casting has a cylindrical geometry with 4.0 in diameter and weighs 20 lb. This casting takes 6.0 min to completely solidify. Another cylindrical-shaped casting with the same diameter-to-length ratio weighs 12 lb. This casting is made of the same steel, and the same conditions of mold and pouring were used. Determine: (a) the mold constant in Chvorinov's rule, (b) the dimensions, and (c) the total solidification time of the lighter casting. The density of steel = 490 lb/ft3.

- Solution: (a) For steel,  = 490 lb/ft3 = 0.2836 lb/in3

- Weight W = V, V = W/ = 20/0.2836 = 70.53 in3

- Volume V = D2L/4 =  (4)2L/4 = 4L = 70.53 in3

- Length L = 70.53/4 = 5.61 in

- Area A = 2D2/4 + DL = 2(4)2/4 + (4)(5.61) = 95.63 in2

- (V/A) = 70.53/95.63 = 0.7375

- Cm = 6.0/(0.7353)2 = 11.03 min/in2

- (b) Find dimensions of smaller cylindrical casting with same D/L ratio and w = 12 lb.

- Weight is proportional to volume: V = (12/20)(70.53) = 42.32 in3

- D/L ratio = 4.0/5.61 = 0.713; thus L = 1.4025D

- Volume V = D2L/4 = (D)2(1.4025D)/4 = 1.1015D3

- D3 = (42.32 in3)/1.1015 = 38.42 in3

- D = (38.42)0.333 = 3.374 in

- L = 1.4025(3.374) = 4.732 in

- (c) V = D2L/4 = (3.374)2(4.732)/4 = 42.32 in3

- A = 2D2/4 + DL = 0.5(3.374)2 + (3.374)(4.732) = 68.04 in2

- V/A = 42.32/68.04 = 0.622 in.

- TTS = 11.03(.622)2 = 4.27 min.

- The total solidification times of three casting shapes are to be compared: (1) a sphere, (2) a cylinder, in which the length-to-diameter ratio = 1.0, and (3) a cube. For all three geometries, the volume = 1000 cm3. The same casting alloy is used in the three cases. (a) Determine the relative solidification times for each geometry. (b) Based on the results of part (a), which geometric element would make the best riser? (c) If the mold constant = 3.5 min/cm2 in Chvorinov's rule, compute the total solidification time for each casting.

- Solution: For ease of computation, make the substitution 10 cm = 1 decimeter (1 dm). Thus 1000 cm3 = 1.0 dm3.

- (1) Sphere volume V = D3/6 = 1.0 dm3.  D3 = 6/ = 1.910 dm3.  D = (1.910)0.333 = 1.241 dm

- Sphere area A = D2 = (1.241)2 = 4.836 dm2

- V/A = 1.0/4.836 = 0.2067 dm

- Chvorinov’s rule TTS = (0.2067)2Cm = 0.0428Cm

- (2) Cylinder volume V = D2H/4 = D3/4 = 1.0 dm3.   D3 = 4/ = 1.273 dm3

- Therefore, D = H = (1.273)0.333 = 1.084 dm

- Cylinder area A = 2D2/4 + DL = 2(1.084)2/4 + (1.084)(1.084) = 5.536 dm2

- V/A =  1.0/5.536 = 0.1806 dm

- Chvorinov’s rule TTS = (0.1806)2Cm = 0.0326Cm

- (3) Cube: V = L3 =1.0 dm3.  L = 1.0 dm

- Cube area = 6L2 = 6(1)2 = 6.0 dm2

- V/A = 1.0/6.0 = 0.1667 dm

- Chvorinov’s rule TTS = (0.1667)2Cm = 0.02778Cm

- (b) Sphere would be the best riser, since V/A ratio is greatest.

- (c) Given that Cm = 3.5 min/cm2 = 350 min/dm3

- Sphere: TTS = 0.0428(350) = 14.98 min

- Cylinder: TTS = 0.0326(350) = 11.41 min

- Cube: TTS = 0.02778(350) = 9.72 min

- A cylindrical riser is to be used for a sand-casting mold. For a given cylinder volume, determine the diameter-to-length ratio that will maximize the time to solidify.

- Solution: To maximize TTS, the V/A ratio must be maximized.

- Cylinder volume V = D2L/4.    L = 4V/D2

- Cylinder area A = 2D2/4 + DL

- Substitute the expression for L from the volume equation in the area equation:

- A = D2/2 + DL = D2/2 + D(4V/D2) = D2/2 + 4 V/D

- Differentiate the area equation with respect to D:

- dA/dD = D – 4 V/D2 = 0		Rearranging, D = 4V/D2

- D3 = 4 V/

- D = (4 V/)0.333

- From the previous expression for L, substituting in the equation for D that we have developed,

- L = 4V/D2 = 4V/(4V/)0.667 = (4V/)0.333

- Thus, optimal values are D = L = (4V/)0.333, and therefore the optimal D/L ratio = 1.0

- A cylindrical riser is to be designed for a sand casting mold. The length of the cylinder is to be 1.25 times its diameter. The casting is a square plate, each side = 10 in and thickness = 0.75 in. If the metal is cast iron, and the mold constant = 16.0 min/in2 in Chvorinov's rule, determine the dimensions of the riser so that it will take 30% longer for the riser to solidify.

- Solution: Casting volume V = tL2 = 0.75(10.0)2 = 75 in3

- Casting area A = 2L2 + 4Lt = 2(10.0)2 + 4(10.0)(0.75) = 230.0 in2

- V/A = 75/230 = 0.3261	Casting TTS = 16(0.3261)2 = 1.70 min

- Riser TTS = 1.30(1.70) = 2.21 min

- Riser volume V = D2H/4 = 0.25D2(1.25D) = 0.3125D3

- Riser area A = 2D2/4 + DH = 0.5D2 + 1.25D2 = 1.75D2

- V/A = 0.3125D3/1.75D2 = 0.1786D

- Riser TTS = 16.0(0.1786D)2 = 16.0(0.03189)D2 = 0.5102D2 = 2.21 min

- D2 = 2.21/0.5102 = 4.3316

- D = (4.3316)0.5 = 2.081 in

- H = 1.25(2.081) = 2.602 in.