21 SURFACE PROCESSING OPERATIONS

### Review Questions

- What are some of the important reasons why manufactured parts must be cleaned?

- Answer. The reasons include (1) to prepare the surface for subsequent industrial processing, (2) to improve hygiene conditions, (3) to remove contaminants which might chemically react with the surface; and (4) to enhance product appearance and performance.

- Mechanical surface treatments are often performed for reasons other than or in addition to cleaning.  What are the reasons?

- Answer. Reasons for mechanical surface treatments include deburring, improving smoothness, adding luster, and enhancing surface properties.

- What are the basic types of contaminants that must be cleaned from metallic surfaces in manufacturing?

- Answer. Basic contaminant types mentioned in the text are (1) oil and grease, (2) solid particles, such as metal chips, abrasive grits, shop dirt, and dust, (3) buffing and polishing compounds, and (4) oxide films, rust, and scale.

- Name some of the important chemical cleaning methods.

- Answer. The chemical cleaning methods can be categorized as follows (1) alkaline cleaning, (2) emulsion cleaning, (3) solvent cleaning, (4) acid cleaning and pickling, and (5) ultrasonic cleaning.

- In addition to surface cleaning, what is the main function performed by shot peening?

- Answer. Shot peening is primarily used to improve the fatigue strength of metals by introducing cold working the metallic surface.

- What is meant by the term mass finishing?

- Answer. In mass finishing, parts are mechanically cleaned and deburred in bulk, usually in a barrel by the mixing action of an abrasive media.

- What is the difference between diffusion and ion implantation?

- Answer. Diffusion is a process in which atoms or molecules move across a boundary between two contacting materials. Ion implantation produces a similar result, but the process involves penetration of high-velocity ions into the surface of a substrate material.

- What is calorizing?

Answer. Calorizing is the diffusion of aluminum into carbon steel, alloy steels, and the alloys of nickel and cobalt. The process is also known as aluminizing.

- Why are metals coated?

- Answer. Reasons for coating metals include (1) to provide corrosion protection, (2) to enhance appearance, (3) to provide a specific color, (4) to increase electrical conductivity, (5) to increase electrical resistance, and (6) prepare surface for subsequent processing.

- Identify the most common types of coating processes.

- Answer. The common coating processes covered in the text are (1) plating, (2) chemical conversion coatings, such as anodizing, (3) vapor deposition processes such as PVD and CVD, and (4) organic coating, such as painting.

- What is the most commonly plated substrate metal?

- Answer. The most commonly plated substrate metal is steel.

- One of the mandrel types in electroforming is a solid mandrel. How is the part removed from a solid mandrel?

- Answer. A solid mandrel has certain geometric features, such as a taper, that permit the part to be removed.  Parts are also sometimes removed by taking advantage of a difference in coefficient of thermal expansion.

- How does electroless plating differ from electrochemical plating?

- Answer. Electroless plating uses only chemical reactions to form the plating; electroplating uses electrolysis.

- What is a conversion coating?

- Answer. A conversion coating is a thin coating produced by chemical reaction of the metallic surface.  The most common conversion coatings are phosphates, chromates, and oxides.

- How does anodizing differ from other conversion coatings?

- Answer. Anodizing uses electrochemical processing methods to convert the metallic surface. The best example is aluminum anodizing.

- What is physical vapor deposition?

- Answer. Physical vapor deposition (PVD) refers to a family of processes in which a material is converted to its vapor phase in a vacuum chamber and condensed onto a substrate surface as a very thin film.

- What is the difference between physical vapor deposition (PVD) and chemical vapor deposition (CVD)?

- Answer. In PVD, the coating vapors are synthesized by heating the coating material and allowing it to condense as a thin film on the surface of the workpart.  In CVD a coating is formed on a heated substrate by the chemical reaction or dissociation of vapors and/or gases; the reaction product nucleates and grows on the substrate surface.

- Name the commonly used coating materials deposited by PVD onto cutting tools?

- Answer. The common coating materials deposited by PVD onto cutting tools are titanium nitride (TiN), titanium carbide (TiC), and aluminum oxide (Al2O3). TiN is probably the most common.

- What are some of the advantages of chemical vapor deposition?

- Answer. Advantages of CVD include (1) capability to deposit refractory materials at temperatures below their melting or sintering temperatures, (2) grain size control, (3) process is performed at atmospheric pressure, and (4) good bonding to substrate surface.

- Identify the four major types of ingredients in organic coatings.

- Answer. The major ingredients are (1) binder, which are polymers, (2) dyes or pigments, which provide color, (3) solvents, and (4) additives such as surfactants and plasticizers.

- What is meant by the term transfer efficiency in organic coating technology?

- Answer. Transfer efficiency indicates how much of the organic coating liquid reaches the target surface.

- Describe the principal methods by which organic coatings are applied to a surface.

- Answer. The main methods include brushing and rolling, spraying, immersion (dip coating), and flow coating.

- The terms drying and curing have different meanings; indicate the distinction.

- Answer. Drying means evaporation of solvents in the organic coating liquid. Curing involves a chemical change in the organic resin (polymerization and/or cross-linking) which hardens the coating.

# Problems

- What volume (cm3) and weight (g) of zinc will be deposited onto a cathodic workpart if 10 amps of current are applied for one hour?

- Solution: From Table 21.1, C = 4.75 x 10-2 mm3/A-s, cathode efficiency E = 95%.

- Volume V = ECIt = 0.95(4.75 x 10-2 mm3/A-s)(10 A)(1 hr)(3600 s/hr) = 1624.5 mm3

- = 1.6245 cm3

- Density of zinc from Table 3.10  = 7.15 g/cm3.	Weight W = 1.6245(7.15) = 11.615 g

- A sheet metal steel part with surface area = 100 cm2 is to be zinc plated. What average plating thickness will result if 15 amps are applied for 12 minutes in a chloride electrolyte solution?

- Solution: From Table 21.1, C = 4.75 x 10-2 mm3/A-s, cathode efficiency E = 95%.

- Volume V = ECIt = 0.95(4.75 x 10-2 mm3/A-s)(15 A)(12 min)(60 s/min) = 487.35 mm3

- Area A = 100 cm2 = 10,000 mm2

- Plating thickness d = 487.35 mm3/10,000 mm2 = 0.049 mm

- A sheet metal steel part with surface area = 15.0 in2 is to be chrome plated. What average plating thickness will result if 15 amps are applied for 10 minutes in a chromic acid-sulfate bath?

- Solution: From Table 21.1, C = 0.92 x 10-4 in3/A-min, cathode efficiency E = 15%.

- Volume V = ECIt = 0.15(0.92 x 10-4)(15)(10) = 0.00207 in3.

- Plating thickness d = 0.00207/15 = 0.000138 in.

- Twenty-five jewelry pieces, each with a surface area = 0.5 in2 are to be gold plated in a batch plating operation. (a) What average plating thickness will result if 8 amps are applied for 10 min in a cyanide bath? (b) What is the value of the gold that will be plated onto each piece if one ounce of gold is valued at $1000? The density of gold = 0.698 lb/in3.

- Solution: (a) From Table 21.1, C = 3.87 x 10-4 in3/A-min, cathode efficiency E = 80%.

- Volume V = ECIt = 0.80(3.87 x 10-4)(8)(10) = 0.02477 in3.

- With Q = 25 pieces and average area per piece = 0.5 in2, total area A = 25(0.5) = 12.5 in2

- Plating thickness d = 0.02477/12.5 = 0.00198 in.

- (b) Given density for gold  = 0.698 lb/in3

- Weight of plated gold = (0.698 lb/in3)(0.02477 in3) = 0.01729 lb = 0.277 oz.

- At $1000/oz, the total value of plated gold = $1000(0.277) = $277

- The value per piece is $277/25 = $11.08

- A part made of sheet steel is to be nickel plated. The part is a rectangular flat plate that is 0.075 cm thick and whose face dimensions are 14 cm by 19 cm. The plating operation is carried out in an acid sulfate electrolyte, using a current = 20 amps for a duration = 30 min. Determine the average thickness of the plated metal resulting from this operation.

- Solution: From Table 21.1, C = 3.42 x 10-2 mm3/A-s, cathode efficiency E = 95%.

- Volume V = ECIt = 0.95(3.42 x 10-2 mm3/A-s)(20 A)(30 min)(60 s/min) = 1169.6 mm3

- Area A = 2(19 x 14) + 0.075 x 2(19 + 14) = 536.95 cm2 = 53,695 mm2

- Plating thickness d = 1169.6/53,695 = 0.022 mm

- A steel sheet metal part has total surface area = 36 in2. How long will it take to deposit a copper plating (assume valence = +1) of thickness = 0.001 in onto the surface if 15 amps of current are applied?

- Solution: From Table 21.1, C = 2.69 x 10-4 in3/A-min, cathode efficiency E = 98%.

- Required volume of plate metal = 36(0.001) = 0.036 in3

- Plated volume V = ECIt = 0.98(2.69 x 10-4 in3/A-min)(15 A) t = 0.003954 t in3

- 0.003954 t = 0.036		t = 0.036/0.003954 = 9.1 min.