14 SHEET METALWORKING

### Review Questions

- Identify the three basic types of sheet metalworking operations.

- Answer. The three basic types of sheet metalworking operations are (1) cutting, (2) bending, and (3) drawing.

- In conventional sheet metalworking operations, (a) what is the name of the tooling and (b) what is the name of the machine tool used in the operations?

- Answer. (a) The tooling is called a punch-and-die. (b) The machine tool is called a stamping press.

- In blanking of a circular sheet-metal part, is the clearance applied to the punch diameter or the die diameter?

- Answer. The die diameter equals the blank diameter, and the punch diameter is smaller by twice the clearance.

- What is the difference between a cutoff operation and a parting operation?

- Answer. A cutoff operation separates parts from a strip by shearing one edge of each part in sequence. A parting operation cuts a slug between adjacent parts in the strip. See Figure 14.7.

- What is the difference between a notching operation and a seminotching operation?

- Answer. A notching operation cuts out a portion of the sheet metal from the side of the sheet or strip, while a seminotching operation removes a portion of the sheet metal from the interior of the sheet or strip.

- Describe each of the two types of sheet-metal-bending operations: V-bending and edge bending.

- Answer. In V-bending, a simple punch and die that each have the included angle are used to bend the part. In edge bending, the punch forces a cantilevered sheet-metal section over a die edge to obtain the desired bend angle. See Figure 14.10.

- For what is the bend allowance intended to compensate?

- Answer. The bend allowance is intended to compensate for stretching of the sheet metal that occurs in a bending operation when the bend radius is small relative to the stock thickness. In principle the bend allowance equals the length of the bent metal along its neutral axis.

- What is springback in sheet-metal bending?

- Answer. Springback is the elastic recovery of the sheet metal after bending; it is usually measured as the difference between the final included angle of the bent part and the angle of the tooling used to make the bend, divided by the angle of the tooling.

- Define drawing in the context of sheet metalworking.

- Answer. Drawing is a sheet metalworking operation used to produce cup-shaped or box-shaped, or other complex-curved, hollow parts. Drawing is accomplished by placing a piece of sheet metal over a die cavity and then using a punch to push the metal into the cavity.

- What are some of the simple measures used to assess the feasibility of a proposed cup-drawing operation?

- Answer. Measures of drawing feasibility include (1) drawing ratio DR = D/Dp; (2) reduction r = (D - Dp)/D; and (3) thickness-to-diameter ratio, t/D; where t = stock thickness, D = blank diameter, and Dp = punch diameter.

- Distinguish between redrawing and reverse drawing.

- Answer. In redrawing, the shape change is significant enough (e.g., drawing ratio greater than 2.0) that it must be carried out in two drawing steps, probably with an annealing operation between the steps. In reverse drawing, two draws are accomplished on the part, one in one direction, the second in the opposite direction.

- What are some of the possible defects in drawn sheet-metal parts?

- Answer. Drawing defects include (1) wrinkling, (2) tearing, (3) earing, and (4) surface scratches, as described in Section 14.3.4.

- What is an embossing operation?

- Answer. Embossing is a sheet metalworking operation used to create indentations in the sheet, such as raised lettering or strengthening ribs.

- What is stretch forming?

- Answer. Stretch forming of sheet metal consists of simultaneously stretching and bending the sheet-metal workpart to achieve shape change.

- What are the two basic categories of structural frames used in stamping presses?

- Answer. Two basic categories of press frame are (1) gap frame, also called C-frame because its profile is the shape of the letter “C”, and (2) straight-sided frame, which has full sides for greater strength and stiffness of the frame.

- What are the relative advantages and disadvantages of mechanical presses versus hydraulic presses in sheet metalworking?

- Answer. The main advantage of mechanical presses is faster cycle rates. Advantages of hydraulic presses are longer ram strokes and uniform force throughout stroke.

- What is the Guerin process?

- Answer. The Guerin process is a sheet-metal forming process that uses a rubber die that flexes to force the sheet metal to take the shape of a form block (punch).

- Distinguish between roll bending and roll forming.

Answer. Roll bending involves the forming of large sheet and plate metal sections into curved forms. Roll forming involves feeding a lone strip or coil through rotating rolls so that the shape of the rolls is imparted to the strip.

Problems

- A power shears is used to cut soft cold-rolled steel that is 4.75 mm thick. At what clearance should the shears be set to yield an optimum cut?

- Solution: From Table 14.1, Ac = 0.060.	Thus, c = Act = 0.060(4.75) = 0.285 mm

- A blanking operation is to be performed on 2.0 mm thick cold-rolled steel (half hard). The part is circular with diameter = 75.0 mm. Determine the appropriate punch and die sizes for this operation.

- Solution: From Table 14.1, Ac = 0.075.	Thus, c = 0.075(2.0) = 0.15 mm.

- Punch diameter = Db - 2c = 75.0 - 2(0.15) = 74.70 mm.

- Die diameter = Db = 75.0 mm.

- A compound die will be used to blank and punch a large washer out of 6061ST aluminum alloy sheet stock 3.50 mm thick. The outside diameter of the washer is 50.0 mm and the inside diameter is 15.0 mm. Determine (a) the punch and die sizes for the blanking operation, and (b) the punch and die sizes for the punching operation.

- Solution: From Table 14.1, Ac = 0.060.	Thus, c = 0.060(3.50) = 0.210 mm

- (a) Blanking punch diameter = Db - 2c = 50 - 2(0.21) = 49.58 mm

- Blanking die diameter = Db = 50.00 mm

- (b) Punching punch diameter = Dh = 15.00 mm

- Punching die diameter = Dh + 2c = 30 + 2(0.210) = 15.42 mm

- A blanking die is to be designed to blank a rectangular part that is 105 mm by 37.5 mm. The sheet metal is 4 mm thick stainless steel (half hard). Determine the dimensions of the blanking punch and the die opening.

- Solution: From Table 14.1, Ac = 0.075.	Thus, c = 0.075(4.0) = 0.30 mm

- Blanking die: dimensions are 105 mm by 37.5 mm.

- Blanking punch: 105 mm length dimension = 105 - 2(0.3) = 104.4 mm

- 37.5 mm width dimension = 37.5 - 2(0.3) = 36.9 mm

- Determine the blanking force required in Problem 14.2, if the shear strength of the steel = 325 MPa and the tensile strength is 450 MPa.

- Solution: F = StL

- t = 2.0 mm from Problem 14.2.

- L = D = 75 = 235.65 mm

- F = 325(2.0)(235.65) = 153,200 N

- Determine the minimum tonnage press to perform the blanking and punching operation in Problem 14.3. The aluminum sheet metal has a tensile strength = 310 MPa, a strength coefficient of 350 MPa, and a strain-hardening exponent of 0.12. (a) Assume that blanking and punching occur simultaneously. (b) Assume the punches are staggered so that punching occurs first, then blanking.

- Solution: (a) F = 0.7(TS)tL

- t =3.5 mm from Problem 14.3.

- L = 50 + 15 = 65 = 204.2 mm

- F = 0.7(310)(3.5)(235.6) = 155,100 N = 155,1000/(4.4482*2000) tons = 17.4 tons => 18 ton press

- (b) Longest length will determine the minimum tonnage press required.

- Punching length of cut, L= 15π, blanking length of cut, L=50π = 157.1 mm (use blanking)

- F = 0.7(310)(3.5)(157.1) = 119,300 N = 119,3000/(4.4482*2000) tons = 13.4 tons => 14 ton press

- Determine the tonnage requirement for the blanking operation in Problem 14.4, given that the stainless steel has a yield strength = 500 MPa, a shear strength = 600 MPa, and a tensile strength = 700 MPa.

- Solution: F = StL

- t = 4 mm from Problem 14.4.

- L = 2(105 + 37.5) = 285 mm

- F = 600(4.0)(285) = 684,000 N

- A bending operation is to be performed on the part shown in Figure 14.13 except that the dimensions are changed as follows: stock thickness = 5.0 mm instead of 3.2 mm, inside bend radius = 8.0 mm instead of 4.75 mm, and included angle = 65 instead of 120. Other dimensions are the same. Determine the blank size required.

- Solution:  = 180 - ’ = 180 – 65 = 115.

- Ab = 2(/360)(R + Kbat)

- R/t = (8.0)/(5.00) = 1.6, which is less than 2.0; therefore, Kba = 0.333

- Ab = 2(115/360)(8.0 + 0.333 x 5.0) = 19.40 mm

- Dimensions of starting blank: w = 35 mm, L = 38 + 19.4 + 25 = 82.4 mm

- Solve Problem 14.8 except that the inside bend radius R = 11.0 mm.

- Solution:  = 180 - ’ = 180 – 65 = 115.

- Ab = 2(/360)(R + Kbat)

- R/t = (11.0)/(5.00) = 2.2; therefore, Kba = 0.5

- Ab = 2(115/360)(11.0 + 0.5 x 5.00) = 27.1 mm

- Dimensions of starting blank: w = 35 mm, L = 38 + 27.1 + 25 = 90.1 mm

- A bending operation is to be performed on 4.0 mm thick cold-rolled steel sheet that is 25 mm wide and 100 mm long. The sheet is bent along the 25 mm direction, so that the bend is 25 mm long. The resulting sheet metal part has an acute angle of 30 and a bend radius of 6 mm. Determine (a) the bend allowance and (b) the length of the neutral axis of the part after the bend. (Hint: the length of the neutral axis before the bend = 100.0 mm).

- Solution: (a) Given that ’ = 30, R = 6.0 mm, and t = 4.0 mm

-  = 180 - ’ = 150.

- Ab = 2(/360)(R + Kbat)

- R/t = 6/4 = 1.5, which is less than 2.0; therefore, Kba = 0.333

- Ab = 2(150/360)(6.0 + 0.333 x 4.0) = 19.195 mm

(b) Due to stretching, the neutral axis of the final part will be greater than 100.0 mm. The amount of stretching will be the difference between the bend allowance and the length of the bent section, which is computed as 2(150/360)(6.0 + 0.5 x 4.0) = 20.944.

- The difference = 20.944 – 19.195 = 1.75 mm

- Thus, the final length of the neutral axis will be L = 100 + 1.75 = 101.75 mm

However, if stretching occurs along the neutral axis of the bend, then thinning of the stretched metal will also occur, and this will affect the preceding calculated value of the length of the bent section. The amount of thinning will be inversely proportional to the amount of stretching because volume must remain constant, before and after bending. The sheet thickness after bending (assuming uniform stretching and thinning) = (19.195/20.944)(4.0) = 3.67 mm. Now let us recalculate the length of the bent section with this new value of t.

The bend radius will remain the same (R = 6.0 mm) because it is located at the inside of the bend. Length of neutral axis along the bend = 2(150/360)(6.0 + 0.5 x 3.67) = 20.512 mm. Now the difference between the length of the bent section and the bend allowance = 20.512 – 19.195 = 1.317 mm. The new final length of the neutral axis is L = 100 + 1.32 = 101.32 mm

The amount of stretching is less than previously determined, and so is the amount of thinning. An iterative procedure must be used to arrive at the final values of stretching and thinning.

- Recalculate the thickness of the stretched sheet as (19.195/20.512)(4.0) = 3.74 mm, and recalculating the length of the bent section based on this value, we have the following:

Length of neutral axis along the bend = 2(150/360)(6.0 + 0.5 x 3.74) = 20.608 mm

- The new difference between the length of the bent section and the bend allowance = 20.608 – 19.195 = 1.413 mm, and the new final length of the neutral axis is L = 100 + 1.41 = 101.41 mm

One more iteration: The thickness of the stretched sheet is (19.195/20.608)(4.0) = 3.73 mm, and recalculating the length of the bent section based on this value, we have 2(150/360)(6.0 + 0.5 x 3.73) = 20.585 mm. The new before and after difference = 20.585 – 19.195 = 1.39 mm, and the new final length of the neutral axis is L = 100 + 1.39 = 101.39 mm

- Determine the bending force required in Problem 14.8 if the bend is to be performed in a V-die with a die opening dimension of 30 mm. The material has a tensile strength of 600 MPa and a shear strength of 430 MPa.

- Solution: For V-bending, Kbf = 1.33.

- F = Kbf(TS)wt2/D = 1.33(600)(44.5)(5.0)2/30 = 29,593 N

- Solve Problem 14.11 except that the operation is performed using a wiping die with die opening dimension = 22 mm.

- Solution: For edge-bending in a wiping die, Kbf = 0.33.

- F = Kbf(TS)wt2/D = 0.33(600)(44.5)(5.0)2/22 = 10,013 N

- A sheet-metal part 3.0 mm thick and 20.0 mm long is bent to an included angle = 60 and a bend radius = 7.5 mm in a V-die. The metal has a yield strength = 220 MPa and a tensile strength = 340 MPa. Compute the required force to bend the part, given that the die opening dimension = 15 mm.

Solution: For V-bending, Kbf = 1.33.

F = Kbf(TS)wt2/D = 1.33(340)(20)(3)2/15 = 5426 N

- Derive an expression for the reduction r in drawing as a function of drawing ratio DR.

- Solution: Reduction r = (Db - Dp)/Db

- Drawing ratio DR = Db/Dp

- r = Db/Db - Dp/Db = 1 - Dp/Db = 1 - 1/DR

- A cup is to be drawn in a deep drawing operation. The height of the cup is 75 mm and its inside diameter = 100 mm. Sheet-metal thickness = 2 mm. If the blank diameter = 225 mm, determine (a) drawing ratio, (b) reduction, and (c) thickness-to-diameter ratio. (d) Does the operation seem feasible?

- Solution: (a) DR = Db/Dp = 225/100 = 2.25

- (b) r = (Db - Dp)/Db = (225 - 100)/225 = 0.555 = 55.5%

- (c) t/Db = 2/225 = 0.0089 = 0.89%

- (d) Feasibility? No! DR is too large (greater than 2.0), r is too large (greater than 50%), and t/D is too small (less than 1%).

- Solve Problem 14.15 except that the starting blank size diameter = 175 mm.

- Solution: (a) DR = Db/Dp = 175/100 = 1.75

- (b) r = (Db - Dp)/Db = (175 - 100)/175 = 0.429 = 42.9%

- (c) t/Db = 2/175 = 0.0114 = 1.14%

- (d) Feasibility? DR < 2.0, r < 50%, and t/D > 1%. However, the operation is not feasible because the 175 mm diameter blank size does not provide sufficient metal to draw a 75 mm cup height. The actual cup height possible with a 175 mm diameter blank can be determined by comparing surface areas (one side only for convenience) between the cup and the starting blank. Blank area = D2/4 = (175)2/4 = 24,053 mm2. To compute the cup surface area, let us divide the cup into two sections: (1) walls, and (2) base, assuming the corner radius on the punch has a negligible effect in our calculations and there is no earing of the cup. Thus, Cup area = Dph + Dp2/4 = 100h + (100)2/4 = 100h + 2500 = 314.16h + 7854. Set surface area of cup = surface are of starting blank:

- 314.16h + 7854= 24,053

- 314.16h = 16,199

- h = 51.56 mm. This is less than the specified 75 mm height.

- A deep drawing operation is performed in which the inside of the cylindrical cup has a diameter of 4.25 in and a height = 2.65 in. Stock thickness = 3/16 in, and starting blank diameter = 7.7 in. Punch and die radii = 5/32 in. The metal has a tensile strength = 65,000 lb/in2, a yield strength = 32,000 lb/in2, and a shear strength = 40,000 lb/in2. Determine (a) drawing ratio, (b) reduction, (c) drawing force, and (d) blankholder force.

- Solution: (a) DR = 7.7/4.25 = 1.81

- (b) r = (Db – Dp)/Db = (7.7 – 4.25)/7.7 = 3.45/7.70 = 0.448 = 44.8%

- (c) F = Dpt(TS)(Db/Dp - 0.7) = (4.25)(0.1875)(65,000)(7.7/4.25 - 0.7) = 180,900 lb.

- (d) Fh = 0.015Y(Db2 - (Dp + 2.2t + 2Rd)2)

- Fh = 0.015(32,000)(7.72 - (4.25 + 2.2 x 0.1875 + 2 x 0.15625)2) = 0.015(32,000)(7.72 - 4.9752)

- Fh = 52,100 lb

- Solve Problem 14.17 except that the stock thickness t = 1/8 in.

- Solution: (a) DR = 7.7/4.25 = 1.81    (same as previous problem)

- (b) t/Db = 0.125/7.7 = 0.01623 = 1.623%

- (c) F = Dpt(TS)(D/Dp - 0.7) = (4.25)(0.125)(65,000)(7.7/4.25 - 0.7) = 120,600 lb.

- (d) Fh = 0.015Y(D2 - (Dp + 2.2t + 2Rd)2)

- Fh = 0.015(32,000)(7.72 - (4.25 + 2.2 x 0.125 + 2 x 0.15625)2) = 0.015(32,000)(7.72 - 4.83752)

- Fh = 54,100 lb

- A cup-drawing operation is performed in which the inside diameter = 80 mm and the height = 50 mm. Stock thickness = 3.0 mm, and starting blank diameter = 150 mm. Punch and die radii = 4 mm. Tensile strength = 400 MPa and yield strength = 180 MPa for this sheet metal. Determine (a) drawing ratio, (b) reduction, (c) drawing force, and (d) blankholder force.

- Solution: (a) DR = 150/80 = 1.875

- (b) r = (Db - Dp)/Db = (150 – 80)/150 = 70/150 = 0.46

- (c) F = Dpt(TS)(Db/Dp - 0.7) = (80)(3)(400)(150/80 - 0.7) = 354,418 N.

- (d) Fh = 0.015Y(Db2 - (Dp + 2.2t + 2Rd)2)

- Fh = 0.015(180)(1502 - (80 + 2.2 x 3 + 2 x 4)2) = 0.015(180)(1502 - 94.62)

- Fh = 114,942 N

- A deep drawing operation is performed on a sheet-metal blank that is 1/8 in thick. The height (inside dimension) of the cup = 3.8 in and the diameter (inside dimension) = 5.0 in. Assuming the punch radius = 0, compute the starting diameter of the blank to complete the operation with no material left in the flange. Is the operation feasible (ignoring the fact that the punch radius is too small)?

- Solution: Use surface area computation, assuming thickness t remains constant.

- Cup area = wall area + base area = Dph + Dp2/4 = 5(3.8) + 0.25(5)2 = 25.25 in2

- Blank area = Db2/4 = 0.25Db2

- Setting blank area = cup area: 0.25Db2 = 25.25

- Db2 = 25.25/0.25 = 101.0

- Db = 10.050 in

- Test for feasibility: DR = Db/Dp = 10.050/5.0 = 2.01. Because DR > 2.0, this operation may not be feasible. Of course, the zero punch radius makes this operation infeasible anyway. With a rounded punch radius, the blank size would be slightly smaller, which would reduce DR.

- Solve Problem 14.20 except use a punch radius = 0.375 in.

- Solution: Use surface area computation, assuming thickness t remains constant. The surface area of the cup will be divided into three sections: (1) straight walls, whose height = 3.80 - 0.375 = 3.425 in, (2) quarter toroid formed by the 0.375 radius at the base of the cup, and (3) base, which has a diameter = 5.0 - 2 x 0.375 = 4.25 in

- A1 = Dph = (5.0)(3.425) = 53.807 in2

- A2 = length of the quarter circle at the base multiplied by the circumference of the circle described by the centroid (Pappus-Guldin Theorem): length of quarter circle = D/4 = 0.25(2 x 0.375) = 0.589 in. The centroid is located at the center of the arc, which is 0.375 sin 45 = 0.265 beyond the center of the 0.375 in radius.  Thus, the diameter of the circle described by the centroid is 4.25 + 2 x 0.265 = 4.780 in

- A2 = 4.78(0.589) = 8.847 in2

- A3 = (4.25)2/4 = 14.188 in2

- Total area of cup = 53.807 + 8.847 + 14.188 = 76.842 in2

- Blank area = Db2/4 = 0.7855Db2

- Setting blank area = cup area: 0.7855Db2 = 76.842

- Db2 = 76.842/0.7855 = 97.825

- Db = 9.890 in

- Test for feasibility: DR = Db/Dp = 9.89/5.0 = 1.978, which is less than the limiting ratio of 2.0. The thickness to diameter ratio t/Db = 0.125/9.89 = 0.0126 = 1.26%, which is above the value of 1% used as a criterion of feasibility in cup drawing.  Whereas the operation in Problem 14.23 was not feasible, the operation in the present problem seems feasible.

- A drawing operation is performed on 3.0 mm stock. The part is a cylindrical cup with height = 50 mm and inside diameter = 70 mm. Assume the corner radius on the punch is zero. (a) Find the required starting blank size Db. (b) Is the drawing operation feasible?

- Solution: Use surface area computation, assuming thickness t remains constant.

- Cup area = wall area + base area = Dph + Dp2/4 = (70)(50) + 0.25(70)2 = 14,846 mm2.

- Blank area = Db2/4 = 0.7855Db2

- Setting blank area = cup area: 0.7855Db2 = 14,846

- Db2 = 14,846/0.7855 = 18,900

- Db = 137.48 mm

- Test for feasibility: DR = Db/Dp = 137.48/70 = 1.964; t/Db = 3/137.48 = 0.0218 = 2.18%.  These criteria values indicate that the operation is feasible; however, with a punch radius Rp = 0, this shape would be difficult to draw because the drawing punch would act on the metal like a blanking punch.

- Solve Problem 14.22 except that the height = 60 mm.

- Solution: Cup area = wall area + base area

- Cup area = Dph + Dp2/4 = (70)(60) + 0.25(70)2 = 17,045 mm2.

- Blank area = Db2/4 = 0.7855Db2

- Setting blank area = cup area: 0.7855Db2 = 17,045

- Db2 = 17,045/0.7855 = 21,700

- Db = 147.31 mm.

- Test for feasibility: DR = Db/Dp = 147.31/70 = 2.10; t/Db = 3/147.31 = 0.0204 = 2.04%.  Since the DR is greater than 2.0, this operation is considered infeasible. Also, as in the previous problem, the punch radius Rp = 0 would render this operation difficult if not infeasible.

- Solve Problem 14.23 except that the corner radius on the punch = 10 mm.

- Solution: Use surface area computation, assuming thickness t remains constant. The surface area of the cup will be divided into three sections: (1) straight walls, whose height = 60 - 10 = 50 mm, (2) quarter toroid formed by the 0.375 radius at the base of the cup, and (3) base, which has a diameter = 70 - 2 x 10 = 50 mm.

- A1 = Dph = (70)(50) = 10,995.6 mm2

- A2 = length of the quarter circle at the base multiplied by the circumference of the circle described by the centroid (Pappus-Guldin Theorem): length of quarter circle = 2Rp/4 = 0.25(2 x 10) = 15.71 mm. The centroid is located at the center of the arc, which is 10 sin 45 = 7.071 beyond the center of the 0.375 in radius. Thus, the diameter of the circle described by the centroid is 50 + 2 x 7.071 = 64.142 mm.

- A2 = 64.142(15.71) = 3166.1 mm2

- A3 = (50)2/4 = 1963.8 mm2

- Total area of cup = 10,995.6 + 3166.1 + 1963.8 = 16,125.5 mm2

- Blank area = Db2/4 = 0.7855Db2

- Setting blank area = cup area: 0.7855Db2 = 16,125.5

- Db2= 16,125.5/0.7855 = 20,529.0

- Db = 143.28 mm

- Test for feasibility: DR = Db/Dp = 143.28/70 = 2.047. Since the DR is greater than 2.0, this operation is considered infeasible.

- The foreman in the drawing section of the shop brings to you several samples of parts that have been drawn in the shop. The samples have various defects. One has ears, another has wrinkles, and still a third has torn sections at its base. What are the causes of each of these defects and what remedies would you propose?

- Solution: (1) Ears are caused by sheet metal that has directional properties. The material is anisotropic. One remedy is to anneal the metal to reduce the directionality of the properties.

- (2) Wrinkles are caused by compressive buckling of the flange as it is drawn inward to form the cup. There are several possible remedies: (a) increase the t/D ratio by using a thicker gage sheet metal. This may not be possible since a design change is required. (b) Increase the blankholder pressure against the work during drawing.

- (3) Tearing occurs due to high tensile stresses in the walls of the cup near the base. A remedy would be to provide a large punch radius. Tearing can also occur due to a die corner radius that is too small.