15 THEORY OF METAL MACHINING

### Review Questions

- What are the three basic categories of material removal processes?

- Answer. As organized in this text, the three basic categories of material removal processes are (1) conventional machining, (2) abrasive processes, and (3) nontraditional processes.

- What distinguishes machining from other manufacturing processes?

- Answer. In machining, material is removed from the workpart so that the remaining material is the desired part geometry.

- Identify some of the reasons why machining is commercially and technologically important.

- Answer. The reasons include the following: (1) it is applicable to most materials; (2) it can produce a variety of geometries to a part; (3) it can achieve closer tolerances than most other processes; and (4) it can create good surface finishes.

- Name the three most common machining processes.

- Answer. The three common machining processes are (1) turning, (2) drilling, and (3) milling.

- What are the two basic categories of cutting tools in machining? Give two examples of machining operations that use each of the tooling types.

- Answer. The two categories are (1) single-point tools, used in operations such as turning and boring; and (2) multiple-edge cutting tools, used in operations such as milling and drilling.

- What are the parameters of a machining operation that are included within the scope of cutting conditions?

- Answer. Cutting conditions include speed, feed, depth of cut, and whether or not a cutting fluid is used.

- Explain the difference between roughing and finishing operations in machining.

- Answer. A roughing operation is used to remove large amounts of material rapidly and to produce a part geometry close to the desired shape.  A finishing operation follows roughing and is used to achieve the final geometry and surface finish.

- What is a machine tool?

- Answer. A machine tool can be defined as a power-driven machine that positions and moves a tool relative to the work to accomplish machining or other metal shaping process.

- What is an orthogonal cutting operation?

- Answer. Orthogonal cutting involves the use of a wedge-shaped tool in which the cutting edge is perpendicular to the direction of speed motion into the work material.

- Why is the orthogonal cutting model useful in the analysis of metal machining?

- Answer. Orthogonal cutting is useful in the analysis of metal machining because it simplifies the rather complex three-dimensional machining situation to two dimensions. In addition, the tooling in the orthogonal model has only two parameters (rake angle and relief angle), which is a simpler geometry than a single-point tool.

- Name and briefly describe the four types of chips that occur in metal cutting.

- Answer. The four types are (1) discontinuous, in which the chip is formed into separated segments; (2) continuous, in which the chip does not segment and is formed from a ductile metal; (3) continuous with built-up edge, which is the same as (2) except that friction at the tool-chip interface causes adhesion of a small portion of work material to the tool rake face, and (4) serrated, which are semi-continuous in the sense that they possess a saw-tooth appearance that is produced by a cyclical chip formation of alternating high shear strain followed by low shear strain.

- Identify the four forces that act upon the chip in the orthogonal metal cutting model but cannot be measured directly in an operation.

- Answer. The four forces that act upon the chip are (1) friction force, (2) normal force to friction, (3) shear force, and (4) normal force to friction.

- Identify the two forces that can be measured in the orthogonal metal cutting model.

- Answer. The two forces that can be measured in the orthogonal metal cutting model are (1) cutting force and (2) thrust force.

- What is the relationship between the coefficient of friction and the friction angle in the orthogonal cutting model?

- Answer. The relationship is that the coefficient of friction is the tangent of the friction angle ( = tan ).

- Describe in words what the Merchant equation tells us.

- Answer. The Merchant equation states that the shear plane angle increases when rake angle is increased and friction angle is decreased.

- How is the power required in a cutting operation related to the cutting force?

- Answer. The power required in a cutting operation is equal to the cutting force multiplied by the cutting speed.

- What is the specific energy in metal machining?

- Answer. Specific energy is the amount of energy required to remove a unit volume of the work material.

- What does the term size effect mean in metal cutting?

- Answer. The size effect refers to the fact that the specific energy increases as the cross-sectional area of the chip (to x w in orthogonal cutting or f x d in turning) decreases.

- What is a tool-chip thermocouple?

Answer. A tool-chip thermocouple is comprised of the tool and chip as the two dissimilar metals forming the thermocouple junction; as the tool-chip interface heats up during cutting, a small voltage is emitted from the junction that can be measured to indicate cutting temperature.

# Problems

- In an orthogonal cutting operation, the tool has a rake angle = 15. The chip thickness before the cut = 0.30 mm and the cut yields a deformed chip thickness = 0.65 mm. Calculate (a) the shear plane angle and (b) the shear strain for the operation.

- Solution: (a) r = to/tc = 0.30/0.65 = 0.4615

-  = tan-1(0.4615 cos 15/(1 - 0.4615 sin 15)) = tan-1(0.5062) = 26.85

- (b) Shear strain  = cot 26.85 + tan (26.85 - 15) = 1.975 + 0.210 = 2.185

- In an orthogonal cutting operation, the 0.250 in wide tool has a rake angle of 5. The lathe is set so the chip thickness before the cut is 0.010 in. After the cut, the deformed chip thickness is measured to be 0.027 in. Calculate (a) the shear plane angle and (b) the shear strain for the operation.

- Solution: (a) r = to/tc = 0.010/0.027 = 0.3701

-  = tan-1(0.3701 cos 5/(1 - 0.3701 sin 5)) = tan-1(0.3813) = 20.9

- (b) Shear strain  = cot 20.9 + tan (20.9 – 5) = 2.623 + 0.284 = 2.907

- In a turning operation, spindle speed is set to provide a cutting speed of 1.8 m/s. The feed and depth of cut are 0.30 mm and 2.6 mm, respectively. The tool rake angle is 8. After the cut, the deformed chip thickness is measured to be 0.49 mm. Determine (a) shear plane angle, (b) shear strain, and (c) material removal rate. Use the orthogonal cutting model as an approximation of the turning process.

- Solution: (a) r = to/tc = 0.30/0.49 = 0.612

-  = tan-1(0.612 cos 8/(1 – 0.612 sin 8)) = tan-1(0.6628) = 33.6

- (b)  = cot 33.6 + tan (33.6 - 8) = 1.509 + 0.478 = 1.987

- (c) RMR = (1.8 m/s x 103 mm/m)(0.3)(2.6) = 1404 mm3/s

- The cutting force and thrust force in an orthogonal cutting operation are 1470 N and 1589 N, respectively. The rake angle = 5, the width of the cut = 5.0 mm, the chip thickness before the cut = 0.6, and the chip thickness ratio = 0.38. Determine (a) the shear strength of the work material and (b) the coefficient of friction in the operation.

- Solution: (a)  = tan-1(0.38 cos 5/(1 - 0.38 sin 5)) = tan-1(0.3916) = 21.38

- Fs = 1470 cos 21.38 – 1589 sin 21.38 = 789.3 N

- As = (0.6)(5.0)/sin 21.38 = 3.0/.3646 = 8.23 mm2

- S = 789.3/8.23 = 95.9 N/mm2 = 95.9 MPa

- (b)  = 45 + /2 - /2; rearranging,  = 2(45) +  - 2

-  = 2(45) + α - 2() = 90 + 5 – 2(21.38) = 52.24

-  = tan 52.24 = 1.291

- The cutting force and thrust force have been measured in an orthogonal cutting operation to be 300 lb and 291 lb, respectively. The rake angle = 10, width of cut = 0.200 in, chip thickness before the cut = 0.015, and chip thickness ratio = 0.4. Determine (a) the shear strength of the work material and (b) the coefficient of friction in the operation.

- Solution:  = tan-1(0.4 cos 10/(1 - 0.4 sin 10)) = tan-1(0.4233) = 22.94

- Fs = 300 cos 22.94 - 291sin 22.94 = 162.9 lb.

- As = (0.015)(0.2)/sin 22.94 = 0.0077 in2

- S = 162.9/0.0077 = 21,167 lb/in2

-  = 2(45) + α - 2() = 90 + 10 - 2(22.94) = 54.1

-  = tan 54.1 = 1.38

- In an orthogonal cutting operation, the rake angle = -5, chip thickness before the cut = 0.2 mm and width of cut = 4.0 mm. The chip ratio = 0.4. Determine (a) the chip thickness after the cut, (b) shear angle, (c) friction angle, (d) coefficient of friction, and (e) shear strain.

- Solution: (a) r = to/tc, tc = to/r = 0.2/.4 = 0.5 mm

- (b)  = tan-1(0.4 cos(–5)/(1 - 0.4 sin(–5))) = tan-1(0.3851) = 21.1

- (c)  = 2(45) + α - 2() = 90 + (-5) - 2(21.8) = 42.9

- (d)  = tan 42.9 = 0.93

- (e)  = cot 31.8 + tan(31.8 - 15) = 2.597 + 0.489 = 3.09

- The shear strength of a certain work material = 50,000 lb/in2. An orthogonal cutting operation is performed using a tool with a rake angle = 20 at the following cutting conditions: cutting speed = 100 ft/min, chip thickness before the cut = 0.015 in, and width of cut = 0.150 in. The resulting chip thickness ratio = 0.50. Determine (a) the shear plane angle, (b) shear force, (c) cutting force and thrust force, and (d) friction force.

- Solution: (a)  = tan-1(0.5 cos 20/(1 - 0.5 sin 20)) = tan-1(0.5668) = 29.5

- (b) As = (0.015)(0.15)/sin 29.5 = 0.00456 in2.

- Fs = AsS = 0.00456(50,000) = 228 lb

- (c)  = 2(45) + α - 2() = 90 + 20 - 2(29.5) = 50.9

- Fc = 228 cos (50.9 - 20)/cos (29.5 + 50.9 -20) = 397 lb

- Ft = 228 sin (50.9 - 20)/cos (29.5 + 50.9 -20) = 238 lb

- (d) F = 397 sin 20 + 238 cos 20 = 359 lb

- A carbon steel bar with 7.64 in diameter has a tensile strength of 65,000 lb/in2 and a shear strength of 45,000 lb/in2. The diameter is reduced using a turning operation at a cutting speed of  400 ft/min. The feed is 0.011 in/rev and the depth of cut is 0.120 in. The rake angle on the tool in the direction of chip flow is 13. The cutting conditions result in a chip ratio of 0.52. Using the orthogonal model as an approximation of turning, determine (a) the shear plane angle, (b) shear force, (c) cutting force and feed force, and (d) coefficient of friction between the tool and chip.

- Solution: (a)  = tan-1(0.52 cos 13/(1 - 0.52 sin 13)) = tan-1(0.5738) = 29.8

- (b) As = tow/sin  = (0.011)(0.12)/sin 29.8 = 0.00265 in2.

- Fs = AsS = 0.00587(40,000) = 119.4 lb

- (c)  = 2(45) + α - 2() = 90 + 10 - 2(29.8) = 43.3

- Fc = Fscos (β – α)/cos ( + β – α)

- Fc = 264.1 cos (43.3 - 13)/cos (29.8 + 43.3 - 13) = 207 lb

- Ft = Fssin (β – α)/cos ( + β – α)

- Ft = 264.1 sin (43.3 - 13)/cos (29.8 + 43.3 - 13) = 121 lb

- (d) μ = tan β = tan 43.3 = 0.942

- Low carbon steel having a tensile strength of 300 MPa and a shear strength of 220 MPa is cut in a turning operation with a cutting speed of 3.0 m/s. The feed is 0.20 mm/rev and the depth of cut is 3.0 mm. The rake angle of the tool is 5 in the direction of chip flow. The resulting chip ratio is 0.45. Using the orthogonal model as an approximation of turning, determine (a) the shear plane angle, (b) shear force, (c) cutting force and feed force.

- Solution: (a)  = tan-1(0.45 cos 5/(1 - 0.45 sin 5)) = tan-1(0.4666) = 25.0

- (b) As = tow/sin  = (0.2)(3.0)/sin 25.0 = 1.42 mm2.

- Fs = AsS = 1.42(220) = 312 N

- (c)  = 2(45) + α - 2() = 90 + 5 - 2(25.0) = 45.0

- Fc = Fscos (β – α)/cos ( + β – α)

- Fc = 312 cos(45 - 5)/cos(25.0 + 45.0 - 5) = 566 N

- Ft = Fssin(β – α)/cos( + β – α)

- Ft = 312 sin(45 - 5)/cos(25.0 + 45.0 - 5) = 474 N

- A turning operation is made with a rake angle of 10, a feed of 0.010 in/rev and a depth of cut = 0.100 in. The shear strength of the work material is known to be 50,000 lb/in2, and the chip thickness ratio is measured after the cut to be 0.40. Determine the cutting force and the feed force. Use the orthogonal cutting model as an approximation of the turning process.

- Solution:  = tan-1(0.4 cos 10/(1 - 0.4 sin 10)) = tan-1(0.4233) = 22.9

- As = (0.010)(0.10)/sin 22.9 = 0.00257 in2

- Fs = AsS = 0.00256(50,000) = 128 lb

-  = 2(45) + α - 2() = 90 + 10 - 2(22.9) = 54.1

- Fc = 128 cos (54.1 - 10)/cos (22.9 + 54.1 - 10) = 236 lb

- Ft = 128 sin (54.1 - 10)/cos (22.9 + 54.1 - 10) = 229 lb

- In a turning operation on stainless steel with hardness = 200 HB, cutting speed = 200 m/min, feed = 0.25 mm/rev, and depth of cut = 7.5 mm. How much power will the lathe draw in performing this operation if its mechanical efficiency = 90%. Use Table 15.2 to obtain the appropriate specific energy value.

- Solution: From Table 15.2, U = 2.8 N-m/mm3 = 2.8 J/mm3

- RMR = vfd = (200 m/min)(103 mm/m)(0.25 mm)(7.5 mm) = 375,000 mm3/min = 6250 mm3/s

- Pc = (6250 mm3/s)(2.8 J/mm3) = 17,500 J/s = 17,500 W = 17.5 kW

- Accounting for mechanical efficiency, Pg = 17.5/0.90 = 19.44 kW

- In Problem 15.11, compute the lathe power requirements if feed is changed to 0.50 mm/rev.

- Solution: This is the same basic problem as the previous, except that a correction must be made for the “size effect.” Using Figure 15.12, for f = 0.50 mm, correction factor = 0.85.

- From Table 15.2, U = 2.8 J/mm3. With the correction factor, U = 2.8(0.85) = 2.38 J/mm3.

- RMR = vfd = (200 m/min)(103 mm/m)(0.50 mm)(7.5 mm) = 750,000 mm3/min = 12,500 mm3/s

- Pc = (12,500 mm3/s)(2.38 J/mm3) = 29,750 J/s = 29,750 W = 29.75 kW

- Accounting for mechanical efficiency, Pg = 29.75/0.90 = 33.06 kW

- In a turning operation on aluminum, cutting speed = 900 ft/min, feed = 0.020 in/rev, and depth of cut = 0.250 in. What horsepower is required of the drive motor, if the lathe has a mechanical efficiency = 87%? Use Table 15.2 to obtain the appropriate unit horsepower value.

- Solution: From Table 15.2, HPu = 0.25 hp/(in3/min) for aluminum. Since feed is greater than 0.010 in/rev in the table, a correction factor must be applied from Figure 15.12. For f = 0.020 in/rev = to, correction factor = 0.9.

- HPc = HPu x RMR, HPg = HPc/E

- RMR = vfd = 900 x 12(.020)(0.250) = 54 in3/min

- HPc = 0.9(0.25)(54) = 12.2 hp

- HPg = 12.2/0.87 = 14.0 hp

- In a turning operation on plain carbon steel whose Brinell hardness = 275 HB, the cutting speed is set at 200 m/min and depth of cut = 6.0 mm. The lathe motor is rated at 25 kW, and its mechanical efficiency = 90%. Using the appropriate specific energy value from Table 15.2, determine the maximum feed that can be set for this operation. Use of a spreadsheet calculator is recommended for the iterative calculations required in this problem.

- Solution: From Table 15.2, U = 2.8 N-m/mm3 = 2.8 J/mm3

- RMR = vfd = (200 m/min)(103 mm/m)(6 mm)f = 1200(103)f mm3/min = 20(103)f mm3/s

- Available power Pc = Pg E = 25(103)(0.90) = 22.5 (103) = 22,500W = 22,500 N-m/s

- Required power Pc = (2.8 N-m/mm3)( 20 x 103) f = 56,000 f (units are N-m/s)

- Setting available power = required power, 22,500 = 56,000 f

- f = 22,500/56,000 = 0.402 mm (this should be interpreted as mm/rev for a turning operation)

- However, for this feed, correction factor in Figure 15.12 = 0.9. Thus U = 2.8(0.90) = 2.52 N-m/mm3 and an iterative calculation procedure is required to match the unit power value with the feed, taking the correction factor into account.

- Required Pc = (2.52)(20 x 103) f = 50,400 f

- Again setting available power = required power, 22,500 = 50,400 f

- f = 22,500/50,400 = 0.446 mm/rev

- One more iteration using the correction factor yields a value around f = 0.45 mm/rev.

- The author’s spreadsheet calculations (using Excel) returned a value closer to f = 0.46 mm/rev. However, whether a spreadsheet is used or not, the difficulty that remains is reading the values of the feed and the correction factor in Figure 15.12.

- A turning operation is to be performed on a 20 hp lathe that has an 87% efficiency rating. The roughing cut is made on alloy steel whose hardness is in the range 325 to 335 HB. The cutting speed is 375 ft/min, feed is 0.030 in/rev, and depth of cut is 0.150 in. Based on these values, can the job be performed on the 20 hp lathe? Use Table 15.2 to obtain the appropriate unit horsepower value.

- Solution: From Table 15.2, HPu = 1.3 hp/(in3/min)

- Since the uncut chip thickness (0.030 in) is different from the tabular value of 0.010, a correction factor must be applied. From Figure 15.12, the correction factor is 0.8. Therefore, the corrected HPu = 0.8*1.3 = 1.04 hp/(in3/min)

- RMR = vfd = 375 ft/min(12 in/ft)(0.03 in)(0.150 in) = 20.25 in3/min

- HPc = (20.25 in3/min)(1.04 hp/(in3/min)) = 21.06 hp required.

- At efficiency E = 87%, available horsepower = 0.87(20) = 17.4 hp

Since required horsepower exceeds available horsepower, the job cannot be accomplished on the 20 hp lathe, at least not at the specified cutting speed of 375 ft/min.

- In a turning operation on low carbon steel (175 BHN), cutting speed = 400 ft/min, feed = 0.010 in/rev, and depth of cut = 0.075 in. The lathe has a mechanical efficiency = 0.85. Based on the unit horsepower values in Table 15.2, determine (a) the horsepower consumed by the turning operation and (b) the horsepower that must be generated by the lathe.

- Solution: (a) From Table 15.2, HPu = 0.6 hp/(in3/min) for low carbon steel.

- HPc = HPu x RMR

- RMR = vfd = 400 x 12(.010)(0.075) = 3.6 in3/min

- HPc = 0.6(3.6) = 2.16 hp

- (b) HPg = 2.16/0.85 = 2.54 hp

- Solve Problem 15.16 except that the feed = 0.0075 in/rev and the work material is stainless steel (Brinell Hardness = 240 HB).

- Solution: (a) From Table 15.2, HPu = 1.0 hp/(in3/min) for stainless steel. Since feed is lower than 0.010 in/rev in the table, a correction factor must be applied from Figure 15.12. For f = 0.0075 in/rev = to, correction factor = 1.1.

- HPc = HPu x RMR

- RMR = 400 x 12(0.0075)(0.12) = 4.32 in3/min

- HPc = 1.1(1.0)(4.32) = 4.75 hp

- (b) HPg = 5.01/0.83 = 5.73 hp

- A turning operation is carried out on aluminum (100 BHN). Cutting speed = 5.6 m/s, feed = 0.25 mm/rev, and depth of cut = 2.0 mm. The lathe has a mechanical efficiency = 0.85. Based on the specific energy values in Table 15.2, determine (a) the cutting power and (b) gross power in the turning operation, in Watts.

- Solution: (a) From Table 15.2, U = 0.7 N-m/mm3 for aluminum.

- RMR = vfd = 5.6(103)(.25)(2.0) = 2.8(103) mm3/s.

- Pc = U RMR = 0.7(2.8)(103) = 1.96(103) N-m/s = 1960 W

- (b) Gross power Pg = 1960/0.85 = 2306 W

- A turning operation is performed on an engine lathe using a tool with zero rake angle in the direction of chip flow. The work material is an alloy steel with hardness = 325 Brinell hardness. The feed is 0.015 in/rev, depth of cut is 0.125 in and cutting speed is 300 ft/min. After the cut, the chip thickness ratio is measured to be 0.45. (a) Using the appropriate value of specific energy from Table 15.2, compute the horsepower at the drive motor, if the lathe has an efficiency = 85%. (b) Based on horsepower, compute your best estimate of the cutting force for this turning operation. Use the orthogonal cutting model as an approximation of the turning process.

- Solution: (a) From Table 15.2, U = Pu = 520,000 in-lb/in3 for alloy steel of the specified hardness. Since feed is greater than 0.010 in/rev in the table, a correction factor must be applied from Figure 15.12. For f = 0.015 in/rev = to, correction factor = 0.95. Thus,

- U = 520,000(0.95) = 494,000 in-lb/in3 = 41,167 ft-lb/in3.

- RMR = 300 x 12(.015)(0.125) = 6.75 in3/min

- Pc = U RMR = 41,167(6.75) = 277,875 ft-lb/min

- HPc = 277,875/33,000 = 8.42 hp

- HPg = 8.42/0.85 = 9.9 hp

- (b) HPc = vFc/33,000. Rearranging, Fc = 33,000 (HPc/v) = 33,000(8.42/300) = 926 lb.

- Check: Use unit horsepower from Table 15.2 rather than specific energy. HPu = 1.3 hp/(in3/min). Applying the correction factor correction factor = 0.95, HPu = 1.235 hp/(in3/min).

- RMR = 300 x 12(.015)(0.125) = 6.75 in3/min, same as before

- HPc = 1.235(6.75) = 8.34 hp

- HPg = 8.34/0.85 = 9.8 hp

- (b) Fc = 33,000 (8.3/300) = 913 lb.

- In a turning operation on an aluminum alloy workpiece, feed = 0.020 in/rev and depth of cut = 0.250 in. The motor horsepower of the lathe is 20 hp and it has a mechanical efficiency = 92%. The unit horsepower value = 0.25 hp/(in3/min) for this aluminum grade. What is the maximum cutting speed that can be used on this job?

- Solution: From Table 15.2, HPu = 0.25 hp/(in3/min) for aluminum. Since feed is greater than 0.010 in/rev in the table, a correction factor must be applied from Figure 15.12. For f = 0.020 in/rev = to, correction factor = 0.9.

- HPc = HPu x RMR, HPg = HPc/E

- RMR = vfd = 12v(.020)(0.250) = 0.06 v in3/min

- HPc = 0.9(0.25)(0.06 v) =  0.0135 v hp

- HPg = 0.0135 v /0.92 = 0.014674 v = 20 hp

- v = 20/0.014674 = 1363 ft/min

- Orthogonal cutting is performed on a metal whose mass specific heat = 1.0 J/g-C, density = 2.9 g/cm3, and thermal diffusivity = 0.8 cm2/s. The cutting speed is 4.5 m/s, uncut chip thickness is 0.25 mm, and width of cut is 2.2 mm. The cutting force is measured at 1170 N. Using Cook's equation, determine the cutting temperature if the ambient temperature = 22C.

- Solution: C = (2.9 g/cm3)(1.0 J/g-C) = 2.90 J/cm3-C = (2.90x10-3) J/mm3-C

- K = 0.8 cm2/s = 80 mm2/s

- U = Fcv/RMR = 1170 N x 4.5 m/s/(4500 mm/s x 0.25 mm x 2.2 mm) = 2.127 N-m/mm3

- T = 0.4U/(ρC) x (vto/K)0.333

- T = 22 + (0.4 x 2.127 N-m/mm3/(2.90x10-3) J/mm3-C) [4500 mm/s x 0.25 mm/80 mm2/s]0.333

- T = 22 + (0.2934 x 103 C)(14.06).333  = 22 + 293.4(2.41) = 22 + 707 = 729C

- Consider a turning operation performed on steel whose hardness = 225 HB at a speed = 3.0 m/s, feed = 0.25 mm, and depth = 4.0 mm. Using values of thermal properties found in the tables and definitions of  Sections 3.6 and 3.7,  and the appropriate specific energy value from Table 15.2, compute an estimate of cutting temperature using the Cook equation. Assume ambient temperature = 20C.

- Solution: From Table 15.2, U = 2.2 N-m/mm3 = 2.2 J/mm3

- From Table 3.10,  = 7.87 g/cm3 = 7.87(10-3) g/mm3

- From Table 3.11, C = 0.11 Cal/g-C. From note “a” at the bottom of the table, 1 cal = 4.186 J.

- Thus, C = 0.11(4.186) = 0.460 J/ g-C

- C = (7.87 g/cm3)(0.46 J/g-C) = 3.62(10-3) J/mm3-C

- From Table 3.11, thermal conductivity k = 0.046 J/s-mm-C

- From Eq. (3.30), thermal diffusivity K = k/C

- K = 0.046 J/s-mm-C /[(7.87 x 10-3 g/mm3)(0.46 J/g-C)] = 12.7 mm2/s

- Using Cook’s equation, to = f = 0.25 mm

- T = (0.4(2.2)/3.62(10-3))[3(103)(0.25)/12.7]0.333 = 0.2428(103)(59.06)0.333

- = 242.8(3.89) = 944.4 C

- Final temperature, taking ambient temperature in account T = 20 + 944 = 964C

- An orthogonal cutting operation is performed on a certain metal whose volumetric specific heat = 110 in-lb/in3-F, and thermal diffusivity = 0.140 in2/sec. The cutting speed = 350 ft/min, chip thickness before the cut = 0.008 in, and width of cut = 0.100 in. The cutting force is measured at 200 lb. Using Cook's equation, determine the cutting temperature if the ambient temperature = 70F.

- Solution: v = 350 ft/min x 12 in/ft/60 sec/min = 70 in/sec.

- U = Fcv/vtow = 200(70)/(70 x 0.008 x 0.100) = 250,000 in-lb/in3.

- T = 70 + (0.4U/C)(vto/K)0.333 =

- T = 70 + (0.4 x 250,000/110)[70 x 0.008/0.14]0.333 = 70 + (909)(4)0.333 = 70 + 1436 = 1506F

- During a turning operation, a tool-chip thermocouple was used to measure cutting temperature. The following temperature data were collected during the cuts at three different cutting speeds (feed and depth were held constant): (1) v = 100 m/min, T = 505C, (2) v = 130 m/min, T = 552C, (3) v = 160 m/min, T = 592C. Determine an equation for temperature as a function of cutting speed that is in the form of the Trigger equation, Eq. (15.23).

Solution: Trigger equation T = Kvm

Choose points (1) and (3) and solve simultaneous equations using T = Kvm as the model.

(1) 505 = K(100)m and (3) 592 = K(160)m

(1) ln 505 = ln K + m ln 100 and (3) ln 592 = ln K + m ln 160

Combining (1) and (3): ln 505 - m ln 100 = ln 592 - m ln 160

6.2246 – 4.6052 m = 6.3835 – 5.0752 m

0.47 m = 0.1589			m = 0.338

(1) K = 505/1000.338 = 505/4.744 = 106.44

(2) K = 592/1600.338 = 592/5.561 = 106.45		Use K = 106.45

Check equation with data point (2): T = 106.45(130)0.338 = 551.87C (pretty close to the given value of 552C).