27 MICROFABRICATION AND NANOFABRICATION TECHNOLOGIES

### Review Questions

- Define microelectromechanical system.

- Answer: A microelectromechanical system (MEMS) is a miniaturized system consisting of both electronic and mechanical components.

- What is the approximate size scale in microsystem technology?

- Answer: Product features in MST are measured in microns.

- Why is it reasonable to believe that microsystem products would be available at lower costs than products of larger, more conventional size?

- Answer: Because less material is used in microsystem products.

- What are some of the basic types of microsystem devices?

- Answer: The text indicates four classifications: (1) microsensors, (2) microactuators, (3) microstructures and microcomponents, and (4) microsystems and micro-instruments.

- Name some products that represent microsystem technology.

- Answer: The text identifies the following MST products: ink-jet printing heads, thin-film magnetic heads, compact discs (CDs), digital versatile discs (DVDs), various automotive sensors, and medical devices.

- Why is silicon a desirable work material in microsystem technology?

- Answer: Reasons given in the text are (1) the microdevices in MST often include electronic circuits, so both the circuit and the microdevice can be fabricated in combination on the same substrate; (2) in addition to its desirable electronic properties, silicon also possesses useful mechanical properties, such as high strength and elasticity, good hardness, and relatively low density; (3) the technologies for processing silicon are well-established, owing to their widespread use in microelectronics; and (4) use of single-crystal silicon permits the production of physical features to very close tolerances.

- What is meant by the term aspect ratio in microsystem technology?

- Answer: The aspect ratio is the height-to-width ratio of the features produced in the MST device.

- What is the difference between bulk micromachining and surface micromachining?

- Answer: Bulk micromachining refers to a relatively deep wet etching process into a single-crystal silicon substrate (Si wafer). Surface micromachining refers to the planar structuring of the substrate surface using much more shallow layering processes.

- What are the three steps in the LIGA process?

- Answer: The three steps in the LIGA process are (1) lithography, specifically X-ray lithography, (2) electroforming or electrodeposition, and (3) plastic molding.

- What is the range of feature sizes of entities associated with nanotechnology?

Answer: The features sizes range from less than 1 nm to 100 nm.

- What is a buckyball?

Answer: A buckyball is the carbon molecule C60, a molecule containing exactly 60 carbon atoms and shaped like a soccer ball. The 60 atoms are arranged symmetrically into 12 pentagonal faces and 20 hexagonal faces to form a ball.

- What is a carbon nanotube?

Answer: A carbon nanotube is another molecular structure of carbon atoms possessing the shape of a tube. It has a typical size of a few nm in diameter and a length of 100 nm or so. Of interest are its mechanical and electrical properties. It can possess strength and stiffness properties exceeding those of steel, and it can be a conductor of electricity or a semiconductor.

- What is a scanning probe instrument, and why is it so important in nanoscience and nanotechnology?

Answer: A scanning probe instrument uses a very sharp probe, whose tip approaches the size of an atom, that moves along the surface of the specimen at a distance of only one nanometer in order to measure properties of the surface. This type of instrument is important because it permits images of the surface to be constructed that are on the scale of the surface atoms.

- What is tunneling, as referred to in the scanning tunneling microscope?

Answer: Tunneling is a quantum mechanics phenomenon in which individual electrons in a solid material jump beyond the surface of the solid into space. The probability of electrons being in this space beyond the surface decreases exponentially in proportion to the distance from the surface. This sensitivity to distance is exploited in the scanning tunneling microscope by positioning the probe tip very close to the surface and applying a small voltage between the two. This causes electrons of surface atoms to be attracted to the small positive charge of the tip, and they tunnel across the gap to the probe.

- What are the two basic categories of approaches used in nanofabrication?

Answer: The two basic categories are (1) top-down approaches, which adapt the microfabrication techniques to nanoscale object sizes and (2) bottom-up approaches, in which atoms and molecules are manipulated and combined into larger structures.

- Why is photolithography based on visible light not used in nanotechnology?

Answer: Because the wavelength of visible light is 400 to 700 nm, well beyond nanoscale.

- What are the lithography techniques used in nanofabrication?

Answer: The lithography techniques discussed in the text are (1) extreme ultraviolet lithography, (2) electron beam lithography, (3) x-ray lithography, and (4) nano-imprint lithography.

- How is nano-imprint lithography different from micro-imprint lithography?

Answer: Nano-imprint lithography is the same basic process as micro-imprint lithography except the deformed features of the resist are of nanoscale proportions.

- What are the limitations of scanning tunneling microscope in nanofabrication that inhibit its commercial application?

Answer: The limitations of STM include (1) they must be carried out in a very high vacuum environment to prevent stray atoms or molecules from interfering with the process and (2) the surface of the substrate must be cooled to temperatures approaching absolute zero (-273C or -460F) in order to reduce thermal diffusion that would gradually distort the atomic structure being formed. These limitations make it a very slow and expensive process.

- What is self-assembly in nanofabrication?

Answer: Self-assembly is a process in which entities at the atomic and/or molecular level combine on their own into larger entities, proceeding in a constructive manner toward the creation of some deliberate thing.

- What are the desirable features of atomic or molecular self-assembly processes in nanotechnology?

Answer: The desirable features of atomic or molecular self-assembly processes include the following: (1) they can be carried out rapidly, (2) they occur automatically and do not require any central control, (3) they exhibit massive replication, and (4) they can be performed at or near atmospheric pressure and room temperature.