3 PROPERTIES OF ENGINEERING MATERIALS

# Review Questions

- What is the dilemma between design and manufacturing in terms of mechanical properties?

- Answer. To achieve design function and quality, the material must be strong; for ease of manufacturing, the material should not be strong, in general.

- What are the three types of static stresses to which materials are subjected?

- Answer. tensile, compressive, and shear.

- State Hooke's law.

- Answer. Hooke's Law defines the stress-strain relationship for an elastic material:  = E, where E = a constant of proportionality called the modulus of elasticity.

- What is the difference between engineering stress and true stress in a tensile test?

- Answer. Engineering stress divides the load (force) on the test specimen by the original area; whereas true stress divides the load by the instantaneous area which decreases as the specimen stretches.

- Define tensile strength of a material.

- Answer. The tensile strength is the maximum load experienced during the tensile test divided by the original area.

- Define yield strength of a material.

- Answer. The yield strength is the stress at which the material begins to plastically deform. It is usually measured as the 0.2% offset value, which is the point where the stress-strain curve for the material intersects a line that is parallel to the straight-line portion of the curve but offset from it by 0.2%.

- Why cannot a direct conversion be made between the ductility measures of elongation and reduction in area using the assumption of constant volume?

- Answer. Because of necking that occurs in the test specimen.

- What is work hardening?

- Answer. Work hardening, also called strain hardening, is the increase in strength that occurs in metals when they are strained.

- Under what circumstances does the strength coefficient have the same value as the yield strength?

- Answer. When the material is perfectly plastic and does not strain harden.

- How does the change in cross-sectional area of a test specimen in a compression test differ from its counterpart in a tensile test specimen?

- Answer. In a compression test, the specimen cross-sectional area increases as the test progresses; while in a tensile test, the cross-sectional area decreases.

- Tensile testing is not appropriate for hard brittle materials such as ceramics. What is the test commonly used to determine the strength properties of such materials?

- Answer. A three-point bending test is commonly used to test the strength of brittle materials. The test provides a measure called the transverse rupture strength for these materials.

- How is the shear modulus of elasticity G related to the tensile modulus of elasticity E, on average?

- Answer. G = 0.4 E, on average.

- How is shear strength S related to tensile strength TS, on average?

- Answer. S = 0.7 TS, on average.

- What is hardness, and how is it generally tested?

- Answer. Hardness is defined as the resistance to indentation of a material. It is tested by pressing a hard object (sphere, diamond point) into the test material and measuring the size (depth, area) of the indentation.

- Why are different hardness tests and scales required?

- Answer. Different hardness tests and scales are required because different materials possess widely differing hardnesses. A test whose measuring range is suited to very hard materials is not sensitive for testing very soft materials.

- Define the recrystallization temperature for a metal.

- Answer. The recrystallization temperature is the temperature at which a metal recrystallizes (forms new grains) rather than work hardens when deformed.

- Define viscosity of a fluid.

- Answer. Viscosity is the resistance to flow of a fluid material; the thicker the fluid, the greater the viscosity.

- What is the defining characteristic of a Newtonian fluid?

- Answer. A Newtonian fluid is one for which viscosity is a constant property at a given temperature. Most liquids (water, oils) are Newtonian fluids.

- What is viscoelasticity, as a material property?

Answer. Viscoelasticity refers to the property most commonly exhibited by polymers that defines the strain of the material as a function of stress and temperature over time. It is a combination of viscosity and elasticity.

- Define density as a material property.

- Answer. Density is the weight per unit volume of a material.

- What is the difference in melting characteristics between a pure metal element and an alloy metal?

- Answer. A pure metal element melts at one temperature (the melting point), while an alloy begins melting at a certain temperature called the solidus and finally completes the transformation to the molten state at a higher temperature called the liquidus.  Between the solidus and liquidus, the metal is a mixture of solid and liquid.

- Define specific heat as a material property.

- Answer. Specific heat is defined as the quantity of heat required to raise the temperature of a unit mass of the material by one degree.

- What is thermal conductivity as a material property?

- Answer. Thermal conductivity is the capacity of a material to transfer heat energy through itself by thermal movement only (no mass transfer).

- Define thermal diffusivity.

- Answer. Thermal diffusivity is the thermal conductivity divided by the volumetric specific heat.

Problems

- A tensile test uses a test specimen that has a gage length of 50 mm and an area = 200 mm2. During the test the specimen yields under a load of 98,000 N. The corresponding gage length = 50.23 mm. This is the 0.2 percent yield point. The maximum load of 168,000 N is reached at a gage length = 64.2 mm. Determine (a) yield strength, (b) modulus of elasticity, and (c) tensile strength. (d) If fracture occurs at a gage length of 67.3 mm, determine the percent elongation. (e) If the specimen necked to an area = 92 mm2, determine the percent reduction in area.

- Solution: (a) Y = 98,000/200 = 490 MPa.

- (b) s = E e

- Subtracting the 0.2% offset, e = (50.23 - 50.0)/50.0 - 0.002 = 0.0026

- E = s/e = 490/0.0026 = 188.5 x 103 MPa.

- (c) TS = 168,000/200 = 840 MPa.

- (d) EL = (67.3 - 50)/50 = 17.3/50 = 0.346 = 34.6%

- (e) AR = (200 - 92)/200 = 0.54 = 54%

- A test specimen in a tensile test has a gage length of 2.0 in and an area = 0.5 in2. During the test the specimen yields under a load of 32,000 lb. The corresponding gage length = 2.0083 in. This is the 0.2 percent yield point. The maximum load of 60,000 lb is reached at a gage length = 2.60 in. Determine (a) yield strength, (b) modulus of elasticity, and (c) tensile strength. (d) If fracture occurs at a gage length of 2.92 in, determine the percent elongation. (e) If the specimen necked to an area = 0.25 in2, determine the percent reduction in area.

- Solution: (a) Y = 32,000/0.5 = 64,000 lb/in2

- (b) s = E e

- Subtracting the 0.2% offset, e = (2.0083 - 2.0)/2.0 - 0.002 = 0.00215

- E = s/e = 64,000/0.00215 = 29.77 x 106 lb/in2

- (c) TS = 60,000/0.5 = 120,000 lb/in2

- (d) EL = (2.92 - 2.0)/2.0 = 0.92/2.0 = 0.46 = 46%

- (e) AR = (0.5 - 0.25)/0.5 = 0.50 = 50%

- In a tensile test on a metal specimen, true strain = 0.08 at a stress = 265 MPa. When true stress = 325 MPa, true strain = 0.27. Determine the strength coefficient and the strain-hardening exponent in the flow curve equation.

Solution: (1) 265 = K(0.08)n  and (2) 325 = K(0.27)n

325/265 = (0.27/0.08)n 		1.2264 = (3.375)n

n ln(3.375) = ln(1.2264)       	1.2164 n = 0.2041		n = 0.1678

Substituting this value with the data back into the flow curve equation, we obtain the value of the strength coefficient K:

(1) K = 265/(0.08).1678 = 404.85 MPa

(2) K = 325/(0.27).1678 = 404.85 MPa

The flow curve equation is:   = 404.85 0.1678

- During a tensile test, a metal has a true strain = 0.10 at a true stress = 37,000 lb/in2. Later, at a true stress = 55,000 lb/in2, true strain = 0.25. Determine the strength coefficient and strain-hardening exponent in the flow curve equation.

Solution: (1) 37,000 = K(0.10)n  and (2) 55,000 = K(0.25)n

55,000/37,000 = (0.25/0.10)n 		1.4865 = (2.5)n

n ln(2.5) = ln(1.4865)       0.9163 n = 0.3964		n = 0.4326

Substituting this value with the data back into the flow curve equation, we obtain the value of the strength coefficient K:

(1) K = 37,000/(0.10)0.4326 = 100,191 lb/in2

(2) K = 55,000/(0.25)0.4326 = 100,191 lb/in2

The flow curve equation is:   = 100,191 0.4326

- A tensile test for a certain metal provides flow curve parameters: strain-hardening exponent is 0.3 and strength coefficient is 600 MPa. Determine (a) the flow stress at a true strain = 1.0 and (b) true strain at a flow stress = 600 MPa.

Solution: (a) Yf = 600(1.0).3 = 600 MPa

(b)  = (600/600)1/.3 = (1.0)3.33 = 1.00

- The flow curve for a certain metal has a strain-hardening exponent of 0.22 and strength coefficient of 54,000 lb/in2. Determine (a) the flow stress at a true strain = 0.45 and (b) the true strain at a flow stress = 40,000 lb/in2.

Solution: (a) Yf = 54,000(0.45).22 = 45,300 lb/in2

(b)  = (40,000/54,000)1/.22 = (0.7407)4.545 = 0.256

- A metal is deformed in a tension test into its plastic region. The starting specimen had a gage length = 2.0 in and an area = 0.50 in2. At one point in the tensile test, the gage length = 2.5 in, and the corresponding engineering stress = 24,000 lb/in2; at another point in the test prior to necking, the gage length = 3.2 in, and the corresponding engineering stress = 28,000 lb/in2. Determine the strength coefficient and the strain-hardening exponent for this metal.

Solution: Starting volume V = LoAo = 2.0(0.5) = 1.0 in3

(1) A = V/L = 1.0/2.5 = 0.4 in2

So, true stress  = 24,000(0.5)/0.4 = 31,250 lb/in2 and  = ln(2.5/2.0) = 0.223

(2) A = 1.0/3.2 = 0.3125 in2

So, true stress  = 28,000(0.5)/0.3125 = 44,800 lb/in2 and  = ln(3.2/2.0) = 0.470

These are two data points with which to determine the parameters of the flow curve equation.

(1) 31,250 = K(0.223)n  and (2) 44,800 = K(0.470)n

44,800/31,250 = (0.470/0.223)n

1.4336 = (2.1076)n

ln(1.4336) = n ln(2.1076)

0.3602 = .7455 n		n = 0.483

(1) K = 31,250/(0.223).483 = 64,513 lb/in2

(2) K = 44,800/(0.470).483 = 64,516 lb/in2		Use average K = 64,515 lb/in2

The flow curve equation is:   = 64,515 0.483

- A tensile specimen is elongated to twice its original length. Determine the engineering strain and true strain for this test. If the metal had been strained in compression, determine the final compressed length of the specimen such that (a) the engineering strain is equal to the same value as in tension (it will be negative value because of compression), and (b) the true strain would be equal to the same value as in tension (again, it will be negative value because of compression). Note that the answer to part (a) is an impossible result. True strain is therefore a better measure of strain during plastic deformation.

Solution: Engineering strain e = (2.0 - 1.0)/1.0 = 1.0

True strain  = ln(2.0/1.0) = ln(2.0) = 0.693

(a) To be compressed to the same engineering strain (e = -1.0) the final height of the compression specimen would have to be zero, which is impossible.

(b) To be compressed to the same true strain value (e = -0.693) the final height of the compression specimen can be determined as follows:

 = -.693 = ln(Lf/Lo)

Lf/Lo = exp.(-0.693) = 0.500		Therefore, Lf = 0.5 Lo

- Show that true strain = ln(1 + e), where e = engineering strain.

Solution: Starting definitions: (1)  = ln(L/Lo) and (2) e = (L - Lo)/Lo

Consider definition (2): e = L/Lo - Lo/Lo = L/Lo - 1

Rearranging, 1 + e = L/Lo

Substituting this into definition (1),  = ln(1 + e)

- A copper wire of diameter 0.80 mm fails at an engineering stress = 248.2 MPa. Its ductility is measured as 75% reduction of area. Determine the true stress and true strain at failure.

Solution: Area reduction AR = (Ao - Af)/Ao = 0.75

Ao - Af = 0.75 Ao

Ao - 0.75Ao = 0.25 Ao = Af

If engineering stress = 248.2 MPa, then true stress  = 248.2/0.25 = 992.8 MPa

True strain  = ln(Lf/Lo) = ln(Ao/Af) = ln(4) = 1.386.

- A steel tensile specimen with starting gage length = 2.0 in and cross-sectional area = 0.5 in2 reaches a maximum load of 37,000 lb. Its elongation at this point is 24%. Determine the true stress and true strain at this maximum load.

Solution: Elongation = (L - Lo)/Lo = 0.24

L - Lo = 0.24 Lo

L = 1.24 Lo

A = Ao/1.24 = 0.8065 Ao

True stress  = 37,000/0.8065(0.5) = 91,754 lb/in2

True strain  = ln(1.24) = 0.215

- A metal alloy has been tested in a tensile test with the following results for the flow curve parameters: strength coefficient = 620.5 MPa and strain-hardening exponent = 0.26. The same metal is now tested in a compression test in which the starting height of the specimen = 62.5 mm and its diameter = 25 mm. Assuming that the cross section increases uniformly, determine the load required to compress the specimen to a height of (a) 50 mm and (b) 37.5 mm.

Solution: Starting volume of test specimen V = hDo2/4 = 62.5(25)2/4 = 30679.6 mm3.

(a) At h = 50 mm,  = ln(62.5/50) = ln(1.25) = 0.223

Yf = 620.5(.223).26 = 420.1 MPa

A = V/L = 30679.6/50 = 613.6 mm2

F = 420.1(613.6) = 257,770 N

(b) At h = 37.5 mm,  = ln(62.5/37.5) = ln(1.667) = 0.511

Yf = 620.5(0.511).26 = 521.1 MPa

A = V/L = 30679.6 /37.5 = 818.1 mm2

F = 521.1(818.1) = 426,312 N

- The flow curve parameters for a certain stainless steel are strength coefficient = 1100 MPa and strain-hardening exponent = 0.35. A cylindrical specimen of starting cross-sectional area = 1000 mm2 and height = 75 mm is compressed to a height of 58 mm. Determine the force required to achieve this compression, assuming that the cross section increases uniformly.

Solution: For h = 58 mm,  = ln(75/58) = ln(1.293) = 0.257

Yf = 1100(.257).35 = 683.7 MPa

Starting volume V = 75(1000) = 75,000 mm3

At h = 58 mm, A = V/L = 75,000/58 = 1293.1 mm2

F = 683.7(1293.1) = 884,095 N.

- A bend test is used for a certain hard material. If the transverse rupture strength of the material is known to be 1000 MPa, what is the anticipated load at which the specimen is likely to fail, given that its width = 15 mm, thickness = 10 mm, and length = 60 mm?

Solution: F = (TRS)(bt2)/1.5L = 1000(15 x 102)/(1.5 x 60) = 16,667 N.

- A special ceramic specimen is tested in a bend test. Its width = 0.50 in and thickness = 0.25 in. The length of the specimen between supports = 2.0 in. Determine the transverse rupture strength if failure occurs at a load = 1700 lb.

Solution: TRS = 1.5FL/bt2 = 1.5(1700)(2.0)/(0.5 x 0.252) = 163,200 lb/in2.

- A torsion test specimen has a radius = 25 mm, wall thickness = 3 mm, and gage length = 50 mm. In testing, a torque of 900 N-m results in an angular deflection = 0.3. Determine (a) the shear stress, (b) shear strain, and (c) shear modulus, assuming the specimen had not yet yielded. (d) If failure of the specimen occurs at a torque = 1200 N-m and a corresponding angular deflection = 10, what is the shear strength of the metal?

Solution: (a)  = T/(2R2t) = (900 x 1000)/(2(25)2(3)) = 76.39 MPa.

(b)  = R/L,  = 0.3(2/360) = 0.005236 radians

 = 25(0.005236)/50 = 0.002618

(c)  = G, G = / = 76.39/0.002618 = 29,179 MPa.

(d) S = (1200(103))/(2(25)2(3)) = 101.86 MPa.

- In a torsion test, a torque of 5000 ft-lb is applied which causes an angular deflection = 1 on a thin-walled tubular specimen whose radius = 1.5 in, wall thickness = 0.10 in, and gage length = 2.0 in. Determine (a) the shear stress, (b) shear strain, and (c) shear modulus, assuming the specimen had not yet yielded. (d) If the specimen fails at a torque = 8000 ft-lb and an angular deflection = 23, calculate the shear strength of the metal.

Solution: (a)  = T/(2R2t) = (5000 x 12)/(2(1.5)2(0.1)) = 42,441 lb/in2.

(b)  = R/L,  = 1(2/360) = 0.01745 rad.,   = 1.5(0.01745)/2.0 = 0.01309

(c)  = G,  G = / = 42,441/0.01309 = 3.24 x 106 lb/in2.

(d) S = (8000 x 12)/(2(1.5)2(0.1)) = 67,906 lb/in2.

- In a Brinell hardness test, a 1500-kg load is pressed into a specimen using a 10-mm-diameter hardened steel ball. The resulting indentation has a diameter = 3.2 mm. (a) Determine the Brinell hardness number for the metal. (b) If the specimen is steel, estimate the tensile strength of the steel.

Solution: (a) HB = 2(1500)/(10(10 - (102 - 3.22).5) = 3000/(10 x 0.5258) = 182 BHN

(b) The estimating formula is: TS = 500(HB).

For a tested hardness of HB = 182, TS = 500(182) = 91,000 lb/in2.

- One of the inspectors in the quality control department has frequently used the Brinell and Rockwell hardness tests, for which equipment is available in the company. He claims that the Rockwell test is based on the same principle as the Brinell test, which is that hardness is always measured as the applied load divided by the area of the impressions made by an indentor. Is he correct? If not, how is the Rockwell test different?

Solution: No, the claim is not correct. The Rockwell hardness test measures the depth of indentation of a cone resulting from an applied load.

- A batch of annealed steel has just been received from the vendor. It is supposed to have a tensile strength in the range 60,000 - 70,000 lb/in2. A Brinell hardness test in the receiving department yields a value of HB = 118. Does the steel meet the specification on tensile strength?

Solution: According to the estimating equation, Eq. (3.22), TS = 500(HB) = 500(118) = 59,000 lb/in2. This lies outside the specified range of 60,000 to 70,000 lb/in2. However, from a legal standpoint, it is unlikely that the batch can be rejected on the basis of its measured Brinell hardness number without using an actual tensile test to measure TS. The formula for converting from Brinell hardness number to tensile strength is only an approximating equation.

- Two flat plates, separated by a space of 4 mm, move relative to each other at a velocity of 5 m/sec. The space between them is occupied by a fluid of unknown viscosity. The motion of the plates is resisted by a shear stress of 10 Pa due to the viscosity of the fluid. Assuming that the velocity gradient of the fluid is constant, determine the coefficient of viscosity of the fluid.

Solution: Shear rate = (5 m/s x 1000 mm/m)/(4 mm) = 1250 s-1

 = (10N/m2)/(1250 s-1) = 0.008 N-s/m2 = 0.008 Pa-s

- Two parallel surfaces, separated by a space of 0.5 in that is occupied by a fluid, move relative to each other at a velocity of 25 in/sec. The motion is resisted by a shear stress of 0.3 lb/in2 due to the viscosity of the fluid. If the velocity gradient in the space between the surfaces is constant, determine the viscosity of the fluid.

Solution: Shear rate = (25 in/sec)/(0.5 in) = 50 sec-1

 = (0.3 lb/in2)/(50 sec-1) = 0.0006 lb-sec/in2.

- The starting diameter of a shaft is 25.00 mm. This shaft is to be inserted into a hole in an expansion fit assembly operation. To be readily inserted, the shaft must be reduced in diameter by cooling. Determine the temperature to which the shaft must be reduced from room temperature (20C) in order to reduce its diameter to 24.98 mm. Refer to Table 3.10.

- Solution: For steel,  = 12(10-6) mm/mm/C according to Table 3.10.

- Revise Eq. (3.29) to D2 - D1 = D1 (T2 - T1).

- 24.98 - 25.00 = 12(10-6)(25.00)(T2 - 20)

- -0.02 = 300(10-6)(T2 - 20)

- -0.02 = 0.0003(T2 - 20) = 0.0003T2 - 0.006

- -.02 + 0.006 = 0.0003T2

- -0.014 = 0.0003T2			T2 = -46.67C

- Aluminum has a density of 2.70 g/cm3 at room temperature (20C). Determine its density at 650C, using data in Table 3.10 as a reference.

- Solution: Assume a 1 cm3 cube, 1 cm on each side.

- From Table 3.10,  = 24(10-6) mm/mm/C

- L2 - L1 = L1 (T2 - T2).

- L2 = 1.0 + 24(10-6)(1.0)(650 - 20) = 1.01512 cm

- (L2 )3 = (1.01512)3 = 1.04605 cm3

- Assume weight remains the same; thus  at 650C = 2.70/1.04605 = 2.581 g/cm3

- With reference to Table 3.10, determine the increase in length of a steel bar whose length = 10.0 in, if the bar is heated from room temperature of 70F to 500F.

- Solution: Increase = (6.7 x 10-6 in/in/F)(10.0 in)(500F - 70F) = 0.0288 in.

- With reference to Table 3.11, determine the quantity of heat required to increase the temperature of an aluminum block that is 10 cm x 10 cm x 10 cm from room temperature (21C) to 300C.

- Solution. Heat = (0.21 cal/g-C)(103 cm3)(2.70 g/cm3)(300C - 21C) = 158,193 cal.

- Conversion: 1.0 cal = 4.184J, so heat = 662,196 J.