22 FUNDAMENTALS OF WELDING

# Review Questions

- What are the advantages and disadvantages of welding compared to other types of assembly operations?

- Answer. Advantages: (1) it provides a permanent joint, (2) joint strength is typically as high as the strength of base metals, (3) it is most economical in terms of material usage, and (4) it is versatile in terms of where it can be accomplished. Disadvantages: (1) it is usually performed manually, so labor cost is high and the skilled labor to perform it is sometimes scarce, (2) welding is inherently dangerous, (3) a welded joint is difficult to disassemble, and (4) quality defects are sometimes difficult to detect.

- What is meant by the term faying surface?

- Answer. The faying surfaces are the contacting surfaces in a welded joint.

- Define the term fusion weld.

- Answer. A fusion weld is a weld in which the metal surfaces have been melted in order to cause coalescence.

- What is the fundamental difference between a fusion weld and a solid state weld?

- Answer.  In a fusion weld, the metal is melted.  In a solid state weld, the metal is not melted.

- What is an autogenous weld?

- Answer. An autogenous weld is a fusion weld made without the addition of filler metal.

- Discuss the reasons why most welding operations are inherently dangerous.

- Answer. Most welding operations are carried out at high temperatures that can cause serious burns on skin and flesh.  In gas welding, the fuels are a fire hazard.  In arc welding and resistance welding, the high electrical energy can cause shocks that are fatal to the worker.  In arc welding, the electric arc emits intense ultraviolet radiation that can cause blinding. Other hazards include sparks, smoke, fumes, and weld spatter.

- What is the difference between machine welding and automatic welding?

- Answer. An automatic welding operation uses a weld cycle controller that regulates the arc movement and workpiece positioning; whereas in machine welding, a human worker must continuously control the arc and the relative movement of the welding head and the workpart.

- Name and sketch the five joint types.

- Answer. Five joint types are (1) butt, (2) corner, (3) lap, (4) tee, (5) edge. For sketches see Figure 22.2 in the text.

- Define and sketch a fillet weld.

- Answer. A fillet weld is a weld joint of approximately triangular cross section used to fill in the edges of corner, lap, and tee joints. See Figure 22.4 in text for sketch.

- Define and sketch a groove weld.

- Answer. A groove weld is a weld joint used to fill in the space between the adjoining edges of butt and other weld types except lap. See Figure 22.5 in text for sketch.

- Why is a surfacing weld different from the other weld types?

- Answer. Because it does not join two distinct parts, but instead adds only filler metal to a surface.

- Why is it desirable to use energy sources for welding that have high heat densities?

- Answer. Because the heat is concentrated in a small region for greatest efficiency and minimum metallurgical damage.

- What is the unit melting energy in welding, and what are the factors on which it depends?

- Answer. The unit melting energy is the amount of heat energy required to melt one cubic millimeter or one cubic inch of metal. The factors on which it depends are (1) specific heat, (2) melting point, and (3) heat of fusion of the metal.

- Define and distinguish the two terms heat transfer factor and melting factor in welding.

- Answer. Heat transfer factor is the ratio of the actual heat received at the work surface divided by the total heat generated by the source. Melting factor is the ratio of heat required for melting divided by the heat received at the work surface.

- What is the heat-affected zone (HAZ) in a fusion weld?

Answer. The HAZ is a region of base metal surrounding the fusion zone in which melting has not occurred, but temperatures from welding were high enough to cause solid state microstructural changes.

# Problems

- A heat source can transfer 3500 J/sec to a metal part surface. The heated area is circular, and the heat intensity decreases as the radius increases, as follows: 70% of the heat is concentrated in a circular area that is 3.75 mm in diameter. Is the resulting power density enough to melt metal?

- Solution: Area A = (3.75)2/4 = 11.045 mm2

- Power P = 0.70(3500) = 2450 J/s = 2450 W.

- Power density PD = 2450 W/11.04472 = 222 W/mm2. This power density is most probably sufficient for melting the metal.

- A welding heat source is capable of transferring 150 Btu/min to the surface of a metal part. The heated area is approximately circular, and the heat intensity decreases with increasing radius as follows: 50% of the power is transferred within a circle of diameter = 0.1 inch and 75% is transferred within a concentric circle of diameter = 0.25 in. What are the power densities in (a) the 0.1-inch diameter inner circle and (b) the 0.25-inch diameter ring that lies around the inner circle? (c) Are these power densities sufficient for melting metal?

- Solution: (a) Area A = (0.1)2/4 = 0.00785 in2

- 150 Btu/min = 2.5 Btu/sec.

- Power P = 0.50(2.5) = 1.25 Btu/sec

- Power density PD = (1.25 Btu/sec)/0.00785 in2 = 159 Btu/sec-in2

- (b) A = (0.252 - 0.12)/4 = 0.0412 in2

- Power P = (0.75 - 0.50)(2.5) = 0.625 Btu/sec

- Power density PD = (0.625 Btu/sec)/0.0412 in2 = 15.16 Btu/sec-in2

- (c) Power densities are sufficient certainly in the inner circle and probably in the outer ring for welding.

- Compute the unit energy for melting for the following metals: (a) aluminum and (b) plain low carbon steel.

- Solution: (a) From Table 22.2, Tm for aluminum = 930 K (1680 R)

- Eq. (22.2) for SI units: Um = 3.33(10-6)Tm2 	Um = 3.33 x 10-6 (930)2 = 2.88 J/mm3

- Eq. (22.2) for USCS units: Um = 1.467(10-5)Tm2     Um = 1.467 x 10-5 (1680)2 = 41.4 Btu/in3

- (b) From Table 22.2, Tm for plain low carbon steel = 1760 K (3160 R)

- Eq. (22.2) for SI units: Um = 3.33(10-6)Tm2	Um = 3.33 x 10-6 (1760)2 = 10.32 J/mm3

- Eq. (22.2) for USCS units: Um = 1.467(10-5)Tm2     Um = 1.467 x 10-5 (3160)2 = 146.5 Btu/in3

- Compute the unit energy for melting for the following metals: (a) copper and (b) titanium.

- Solution: (a) From Table 22.2, Tm for copper = 1350 K (2440 R)

- Eq. (22.2) for SI units: Um = 3.33(10-6)Tm2	Um = 3.33 x 10-6 (1350)2 = 6.07 J/mm3

- Eq. (22.2) for USCS units: Um = 1.467(10-5)Tm2     Um = 1.467 x 10-5 (2440)2 = 87.3 Btu/in3

- (b) From Table 22.2, Tm for titanium = 2070 K (3730 R)

- Eq. (22.2) for SI units: Um = 3.33(10-6)Tm2	Um = 3.33 x 10-6 (2070)2 = 14.27 J/mm3

- Eq. (22.2) for USCS units: Um = 1.467(10-5)Tm2     Um = 1.467 x 10-5 (3730)2 = 204.1 Btu/in3

- A fillet weld has a cross-sectional area of 25.0 mm2 and is 300 mm long. (a) What quantity of heat (in joules) is required to accomplish the weld, if the metal to be welded is low carbon steel? (b) How much heat must be generated at the welding source, if the heat transfer factor is 0.75 and the melting factor = 0.63?

- Solution: (a) Eq. (22.2) for SI units: Um = 3.33 x 10-6 Tm2

- From Table 22.2, Tm for low carbon steel = 1760° K

- Um = 3.33 x 10-6 (1760)2 = 10.32 J/mm3

- Volume of metal melted V = 25(300) = 7500 mm3

- Hw = 10.32(7500) = 77,360 J at weld

- (b) Given f1 = 0.75 and f2 = 0.63, H = 77,360/(0.75 x 0.63) = 163,700 J at source.

- A groove weld has a cross-sectional area = 0.045 in2 and is 10 inches long. (a) What quantity of heat (in Btu) is required to accomplish the weld, if the metal to be welded is medium carbon steel? (b) How much heat must be generated at the welding source, if the heat transfer factor = 0.9 and the melting factor = 0.7?

- Solution: (a) Eq. (22.2) for USCS units: Um = 1.467 x 10-5 Tm2

- From Table 22.2, Tm for medium carbon steel = 3060 R

- Um = 1.467 x 10-5 (3060)2 = 137.4 Btu/in3

- Volume of metal melted V = 0.045(10) = 0.45 in3

- Hw = 137.4(0.45) = 61.8 Btu at weld

- (b) Given f1 = 0.9 and f2 = 0.7. 		H = 61.8/(0.9 x 0.7) = 98.1 Btu at source.

- Solve the previous problem, except that the metal to be welded is aluminum, and the corresponding melting factor is half the value for steel.

- Solution: (a) Eq. (22.2) for USCS units: Um = 1.467 x 10-5 Tm2

- From Table 22.2, Tm for aluminum = 1680 R

- Um = 1.467 x 10-5 (1680)2 = 41.4 Btu/in3

- Volume of metal melted V = 0.045(10) = 0.45 in3

- Hw = 41.4(0.45) = 18.6 Btu at weld

- (b) Given f1 = 0.9 and f2 = 0.35. 		H = 18.6/(0.9 x 0.35) = 59.1 Btu at source.

- The welding power generated in a particular arc-welding operation = 3000 W. This is transferred to the work surface with a heat transfer factor = 0.9. The metal to be welded is copper whose melting point is given in Table 22.2. Assume that the melting factor = 0.25. A continuous fillet weld is to be made with a cross-sectional area = 15.0 mm2. Determine the travel speed at which the welding operation can be accomplished.

- Solution: From Table 22.2, Tm = 1350K for copper.

- Um = 3.33 x 10-6(1350)2 = 6.07 J/mm3

- v = f1 f2 RH/UmAw = 0.9(0.25)(3000)/(6.07 x 15) = 7.4 mm/s.

- Solve the previous problem except that the metal to be welded is high carbon steel, the cross-sectional area of the weld = 25.0 mm2, and the melting factor = 0.6.

- Solution: From Table 22.2, Tm = 1650K for high carbon steel.

- Um = 3.33 x 10-6(1650)2 = 9.07 J/mm3

- v = f1 f2 RH /UmAw = 0.9(0.6)(3000)/(9.07 x 25) = 7.15 mm/s.

- A welding operation on an aluminum alloy makes a groove weld. The cross-sectional area of the weld is 30.0 mm2. The welding velocity is 4.0 mm/sec. The heat transfer factor is 0.92 and the melting factor is 0.48. The melting temperature of the aluminum alloy is 650C. Determine the rate of heat generation required at the welding source to accomplish this weld.

- Solution: Um = 3.33 x 10-6(650 + 273)2 = 2.84 J/mm3

- f1 f2 RH = UmAw v

- RH = Um Aw v/f1 f2 = 2.84(30)(4)/(0.92 x 0.48) = 771 J/s = 771 W.

- The power source in a particular welding operation generates 125 Btu/min, which is transferred to the work surface with heat transfer factor = 0.8. The melting point for the metal to be welded = 1800F and its melting factor = 0.5. A continuous fillet weld is to be made with a cross-sectional area = 0.04 in2. Determine the travel speed at which the welding operation can be accomplished.

- Solution: Um = 1.467 x 10-5 (1800 + 460)2 = 74.9 Btu/in3

- v = f1 f2 RH /UmAw = 0.8(0.5)(125)/(74.9 x 0.04) = 16.7 in/min

- In a certain welding operation to make a fillet weld, the cross-sectional area = 0.025 in2 and the travel speed = 15 in/min. If the heat transfer factor = 0.95 and melting factor = 0.5, and the melting point = 2000F for the metal to be welded, determine the rate of heat generation required at the heat source to accomplish this weld.

- Solution: Um = 1.467 x 10-5 (2000 + 460)2 = 88.8 Btu/in3

- v = 15 = f1 f2 RH/UmAw = 0.95(0.5)RH /(88.8 x 0.025) = 0.214 RH

- RH = 15/0.214 = 70.1 Btu/min