16 MACHINING OPERATIONS AND MACHINE TOOLS

### Review Questions

- What are the differences between rotational parts and prismatic parts in machining?

- Answer. Rotational parts are cylindrical or disk-shaped and are machined on a turning machine (e.g., a lathe); prismatic parts are block-shaped or flat and are generally produced on a milling machine, shaper, or planer.

- Distinguish between generating and forming when machining workpart geometries.

- Answer. Generating refers to the creation of work geometry due to the feed trajectory of the cutting tool; examples include straight turning, taper turning, and profile milling.  Forming involves the creation of work geometry due to the shape of the cutting tool; common examples include form turning and drilling.

- Give two examples of machining operations in which generating and forming are combined to create workpart geometry.

- Answer. The two examples given in the text are thread cutting on a lathe and slot milling.

- Describe the turning process.

- Answer. Turning is a machining process in which a single-point tool removes material from the surface of a rotating cylindrical workpiece, the tool being fed in a direction parallel to the axis of work rotation.

- What is the difference between threading and tapping?

- Answer. A threading operation is performed on a turning machine and produces an external thread, while tapping is normally performed on a drilling machine and produces an internal thread.

- How does a boring operation differ from a turning operation?

- Answer. Boring produces an internal cylindrical shape from an existing hole, while turning produces an external cylindrical shape.

- What is meant by the designation 12 x 36 inch lathe?

- Answer. A 12 x 36 lathe has a 12 inch swing (maximum work diameter that can be accommodated) and a 36 inch distance between centers (indicating the maximum work length that can be held between centers).

- Name the various ways in which a workpart can be held in a lathe.

- Answer. Methods of holding the work in a lathe include: (1) between centers, (2) chuck, (3) collet, and (4) face plate.

- What is the difference between a live center and a dead center, when these terms are used in the context of workholding in a lathe?

- Answer. A center holds the workpiece at the tailstock end of the lathe. A live center is mounted in bearings and rotates with the work, while a dead center does not rotate - the work rotates about it.

- How does a turret lathe differ from an engine lathe?

- Answer. A turret lathe has a toolholding turret in place of a tailstock; the tools in the turret can be brought to work to perform multiple cutting operations on the work without the need to change tools as in operating a conventional engine lathe.

- What is a blind hole?

- Answer. A blind hole does not exit the work; by comparison, a through hole exits the opposite side of the workpart.

- What is the distinguishing feature of a radial drill press?

- Answer. A radial drill has a long radial arm along which the drill head can be positioned to allow the drilling of large work parts. The radial arm can also be swiveled about the column to drill parts on either side of the worktable.

- What is the difference between peripheral milling and face milling?

- Answer. In peripheral milling, cutting is accomplished by the peripheral teeth of the milling cutter and the tool axis is parallel to the work surface; in face milling, cutting is accomplished by the flat face of the cutter whose axis is perpendicular to the work surface.

- Describe profile milling.

- Answer. Profile milling generally involves the milling of the outside periphery of a flat part.

- What is pocket milling?

- Answer. Pocket milling uses an end milling cutter to machine a shallow cavity (pocket) into a flat workpart.

- Describe the difference between up milling and down milling?

- Answer. In up milling, the cutter speed direction is opposite the feed direction; in down milling, the direction of cutter rotation is the same as the feed direction.

- How does a universal milling machine differ from a conventional knee-and-column machine?

- Answer. The universal milling machine has a worktable that can be rotated about a vertical axis to present the part at any specified angle to the cutter spindle.

- What is a machining center?

- Answer. A machining center is a CNC machine tool capable of performing multiple types of cutting operations involving rotating spindles (e.g., milling, drilling); the machine is typically equipped with automatic tool-changing, pallet shuttles to speed workpart changing, and automatic workpart positioning.

- What is the difference between a machining center and a turning center?

- Answer. A machining center is generally confined to rotating spindle operations (e.g., milling, drilling); while a turning center performs turning type operations, generally with single-point tools.

- What can a mill-turn center do that a conventional turning center cannot do?

- Answer. The mill-turn center has the capacity to position a rotational workpart at a specified angular location, permitting milling or drilling to be performed at a location on the periphery of the part.

- How do shaping and planing differ?

- Answer. In shaping, the work is stationary during the cut, and the speed motion is performed by the cutting tool; whereas in planing, the cutting tool is stationary, and the workpart is moved past the tool in the speed motion.

- What is the difference between internal broaching and external broaching?

- Answer. Internal broaching is accomplished on the inside surface (hole) of a workpart; while external broaching is performed on one of the outside surfaces of the part.

- Identify the three basic forms of sawing operation?

Answer. The three forms of sawing are: (1) hacksawing, (2) bandsawing, and (3) circular sawing.

- Why do costs tend to increase when better surface finish is required on a machined part?

- Answer. Costs tend to increase when better surface finish is required because additional operations such as grinding, lapping, or similar finishing processes must be included in the manufacturing sequence.

- What are the basic factors that affect surface finish in machining?

- Answer. The factors that affect surface finish are (1) geometric factors such as type of operation, feed, and tool shape (nose radius in particular); (2) work material factors such as built-up edge effects, and tearing of the work surface when machining ductile materials, which factors are affected by cutting speed; and (3) vibration and machine tool factors such as setup and workpart rigidity, and backlash in the feed mechanism.

- What are the parameters that have the greatest influence in determining the ideal surface roughness Ri in a turning operation?

- Answer. The ideal surface roughness is determined by the following geometric parameters of the machining operation: (1) tool nose radius and (2) feed. In some cases, the end cutting edge and end cutting edge angle of the single-point tool affects the feed mark pattern on the work surface.

- Name some of the steps that can be taken to reduce or eliminate vibrations in machining.

- Answer. Steps to reduce vibration in machining include (1) increase stiffness or damping in the setup; (2) operate at speeds away from the natural frequency of the machine tool system; (3) reduce forces in machining by changing feed or depth and cutter design (e.g., reduced rake angle), and (4) change the cutter design to reduce forces.

# Problems

- A cylindrical workpart 200 mm in diameter and 700 mm long is to be turned in an engine lathe. Cutting speed = 2.30 m/s, feed = 0.32 mm/rev, and depth of cut = 1.80 mm. Determine (a) cutting time, and (b) metal removal rate.

- Solution: (a) N = v/(πD) = (2.30 m/s)/0.200 = 3.66 rev/s

- fr = Nf = 6.366(.3) = 1.17 mm/s

- Tm = L/fr = 700/1.17 = 598 s = 9.96 min

- Alternative calculation using Eq. (16.5), Tm = 200(700)π/(2,300 x 0.32) = 597.6 sec = 9.96 min

- (b) RMR = vfd = (2.30 m/s)(103)(0.32 mm)(1.80 mm) = 1320 mm3/s

- In a production turning operation, the foreman has decreed that a single pass must be completed on the cylindrical workpiece in 5.0 min. The piece is 400 mm long and 150 mm in diameter. Using a feed = 0.30 mm/rev and a depth of cut = 4.0 mm, what cutting speed must be used to meet this machining time requirement?

- Solution: Starting with Eq. (16.5): Tm = DoL/vf.

- Rearranging to determine cutting speed: v = DoL/fTm

- v = (0.4)(0.15)/(0.30)(10-3)(5.0) = 0.1257(103) m/min = 125.7 m/min

- A tapered surface is to be turned on an automatic lathe. The workpiece is 750 mm long with minimum and maximum diameters of 100 mm and 200 mm at opposite ends. The automatic controls on the lathe permit the surface speed to be maintained at a constant value of 200 m/min by adjusting the rotational speed as a function of workpiece diameter. Feed = 0.25 mm/rev and depth of cut = 3.0 mm. The rough geometry of the piece has already been formed, and this operation will be the final cut. Determine (a) the time required to turn the taper and (b) the rotational speeds at the beginning and end of the cut.

- Solution: (a) RMR = vfd = (200 m/min)(103 mm/m)(0.25 mm)(3.0 mm) = 150,000 mm3/min

- Area of frustrum of cone A = (R1 + R2){h2 + (R1 – R2)2}0.5

- Given R1 = 100 mm, R2 = 50 mm, and h = 750 mm,

- A = (100 + 50){7502 + (100 – 50)2}0.5 = 150(565,000)0.5 = 354,214 mm2

- Given depth of cut d = 3.0 mm, volume cut V = Ad = (354,214 mm2)(3.0 mm) = 1,062,641 mm3

- Tm = V/RMR = (1,062,641 mm3)/(150,000 mm3/min) = 7.084 min

- (b) At beginning of cut (D1 = 100 mm), N = v/D = 200,000/100 = 636.6 rev/min

- At end of cut (D2 = 200 mm), N = 200,000/200 = 318.3 rev/min

- A cylindrical work bar with 4.5 in diameter and 52 in length is chucked in an engine lathe and supported at the opposite end using a live center. A 46.0 in portion of the length is to be turned to a diameter of 4.25 in one pass at a speed of 450 ft/min. The metal removal rate should be 6.75 in3/min. Determine (a) the required depth of cut, (b) the required feed, and (c) the cutting time.

- Solution: (a) depth d = (4.50 - 4.25)/2 = 0.125 in

(b) RMR = vfd; f = RMR/(12vd) = 6.75/(12 x 450 x 0.125) = 0.010 in

f = 0.010 in/rev

- (c) N = v/πD = 450 x 12/4.5 = 382 rev/min

- fr = 382(0.010) = 3.82 in/min

- Tm = 46/3.82 = 12.04 min

- The end of a large tubular workpart is to be faced on a NC vertical boring mill. The part has an outside diameter of 38.0 in and an inside diameter of 24.0 in. If the facing operation is performed at a rotational speed of 40.0 rev/min, feed of 0.015 in/rev, and depth of cut of 0.180 in, determine (a) the cutting time to complete the facing operation and (b) the cutting speeds and metal removal rates at the beginning and end of the cut.

- Solution: (a) Distance traveled L = (Do - Di)/2 = (38 - 24)/2 = 7.0 in

- fr = (40 rev/min)(0.015 in/rev) = 0.60 in/min

- Tm = 7.0/0.60 = 11.67 min

- (b) At Do = 38 in, N = v/πD, v = NπD = (40 rev/min)(38/12) = 398 ft/min

- RMR = vfd = (398 x 12)(0.015)(0.18) = 12.89 in3/min

- At Di = 24 in, N=v/πD, v = NπD = (40 rev/min)(24/12) = 251 ft/min

- RMR = vfd = (251 x 12)(0.015)(0.18) = 8.14 in3/min

- A drilling operation is to be performed with a 12.7 mm diameter twist drill in a steel workpart. The hole is a blind hole at a depth of 60 mm and the point angle is 118. The cutting speed is 25 m/min and the feed is 0.30 mm/rev. Determine (a) the cutting time to complete the drilling operation, and (b) metal removal rate during the operation, after the drill bit reaches full diameter.

- Solution: (a) N = v/πD = 25(103) / (12.7) = 626.6 rev/min

- fr = Nf = 626.6(0.30) = 188 mm/min

A = 0.5D tan (90 – θ/2) = 0.5(12.7)tan(90 – 118/2) = 3.82 mm

- Tm = (d + A)/fr = (60 + 3.82)/188 = 0.339 min

- (b) RMR = 0.25πD2fr = 0.25(12.7)2(188) = 23,800 mm3/min

- A gundrilling operation is used to drill a 9/64-in diameter hole to a certain depth. It takes 4.5 minutes to perform the drilling operation using high pressure fluid delivery of coolant to the drill point. The current spindle speed = 4000 rev/min, and feed = 0.0017 in/rev. In order to improve the surface finish in the hole, it has been decided to increase the speed by 20% and decrease the feed by 25%. How long will it take to perform the operation at the new cutting conditions?

- Solution: fr = Nf = 4000 rev/min (0.0017 in/rev) = 6.8 in/min

- Hole depth d = 4.5 min (6.8 in/min) = 30.6 in

- New speed v = 4000(1 + 0.20) = 4800 rev/min

- New feed f = 0.0017(1- 0.25) = 0.001275 in/min

- New feed rate fr = 4800(0.001275) = 6.12 in/min

- New drilling time Tm = 30.6/6.12 in/min = 5.0 min

- A peripheral milling operation is performed on the top surface of a rectangular workpart which is 400 mm long by 60 mm wide. The milling cutter, which is 80 mm in diameter and has five teeth, overhangs the width of the part on both sides. Cutting speed = 70 m/min, chip load = 0.25 mm/tooth, and depth of cut = 5.0 mm. Determine (a) the actual machining time to make one pass across the surface and (b) the maximum material removal rate during the cut.

- Solution: (a) N = v/πD = 70,000 mm/80 = 279 rev/min

- fr = Nntf = 279(5)(0.25) = 348 mm/min

- A = (d(D-d))0.5 = (5(80-5))0.5 = 19.4 mm

- Tm = (400 + 19.4)/348 = 1.20 min

- (b) RMR = wdfr = 60(5)(348) = 104,400 mm3/min

- A face milling operation is used to machine 6.0 mm from the top surface of a rectangular piece of aluminum 300 mm long by 125 mm wide in a single pass. The cutter follows a path that is centered over the workpiece. It has four teeth and is 150 mm in diameter. Cutting speed = 2.8 m/s, and chip load = 0.27 mm/tooth. Determine (a) the actual machining time to make the pass across the surface and (b) the maximum metal removal rate during cutting.

- Solution: (a) N = v/πD = (2800 mm/s)/150 = 5.94 rev/s

- fr = Nntf = 5.94(4)(0.27) = 6.42 mm/s

- =  = 0.5(150 – 82.9) = 33.5 mm

- Tm = (L + A)/fr = (300 + 33.5))/6.42 = 52 s = 0.87 min

- (b) RMR = wdfr = 125(6)(6.42) = 4813 mm3/s

- A slab milling operation is performed on the top surface of a steel rectangular workpiece 12.0 in long by 2.5 in wide. The helical milling cutter, which has a 3.0 in diameter and ten teeth, is set up to overhang the width of the part on both sides. Cutting speed is 125 ft/min, feed is 0.006 in/tooth, and depth of cut = 0.300 in. Determine (a) the actual machining time to make one pass across the surface and (b) the maximum metal removal rate during the cut. (c) If an additional approach distance of 0.5 in is provided at the beginning of the pass (before cutting begins), and an overtravel distance is provided at the end of the pass equal to the cutter radius plus 0.5 in, what is the duration of the feed motion.

- Solution: (a) N= v/πD = 125(12)/3 = 159.15 rev/min

- fr = Nntf = 159.15(10)(0.006) = 9.55 in/min

- A = (d(D-d))0.5 = (0.30(3.0-0.30))0.5 = 0.90 in

- Tm = (L + A)/fr = (12.0 + 0.9)/9.55 = 1.35 min

- (b) RMR = wdfr = 2.5(0.30)(9.55) = 7.16 in3/min

- (c) The cutter travels 0.5 in before making contact with the work. It moves 0.90 in before reaching full depth of cut. It then feeds the length of the work (12.0 in). The overtravel consists of the cutter radius (1.5 in) plus an additional 0.5 in. Thus,

- Tf = (0.5 + 0.9 + 12.0 + 1.5 + 0.5)/9.55 = 1.56 min

- A face milling operation is performed on the top surface of a steel rectangular workpiece 12.0 in long by 2.5 in wide. The milling cutter follows a path that is centered over the workpiece. It has five teeth and a 3.0 in diameter. Cutting speed = 250 ft/min, feed = 0.006 in/tooth, and depth of cut = 0.150 in. Determine (a) the actual cutting time to make one pass across the surface and (b) the maximum metal removal rate during the cut. (c) If an additional approach distance of 0.5 in is provided at the beginning of the pass (before cutting begins), and an overtravel distance is provided at the end of the pass equal to the cutter radius plus 0.5 in, what is the duration of the feed motion.

- Solution: (a) N = v/πD = 250(12)/3 = 318.3 rev/min

- fr = 318.3(5)(0.006) = 9.55 in/min

- =  in

- Tm = (12.0 + 0.671)/9.55 = 1.33 min

- (b) RMR = 2.5(0.150)(9.55) = 3.58 in3/min

- (c) The cutter travels 0.5 in before making contact with the work. It moves 1.50 in before its center is aligned with the starting edge of the 12.0 in workpiece. It then feeds the length of the work (12.0 in). The overtravel consists of the cutter radius (1.5 in) plus an additional 0.5 in. Thus,

- Tf = (0.5 + 1.5 + 12.0 + 1.5 + 0.5)/9.55 = 1.68 min

- Solve Problem 16.11 except that the workpiece is 5.0 in wide and the cutter is offset to one side so that the swath cut by the cutter = 1.0 in wide. This is called partial face milling, Figure 16.20(b).

- Solution: (a) N = 250(12)/3 = 318.3 rev/min

- fr = 318.3(5)(0.006) = 9.55 in/min

- A = (1(3-1)).5 = 1.414 in

- Tm = (12.0 + 1.414)/9.55 = 1.405 min

- (b) RMR = 1.0(.150)(9.55) = 1.43 in3/min

- (c) The cutter travels 0.5 in before making contact with the work. It moves 1.414 in before reaching full width of cut. It then feeds the length of the work (12.0 in). The overtravel consists of the cutter radius (1.5 in) plus an additional 0.5 in. Thus,

- Tf = (0.5 + 1.414 + 12.0 + 1.5 + 0.5)/9.55 = 1.67 min

- In a turning operation on cast iron, the nose radius on the single-point tool = 1.5 mm, feed = 0.22 mm/rev, and speed = 1.8 m/s. Compute an estimate of the surface roughness for this cut.

- Solution: Ri = f2/32NR = (0.22)2/(32 x 1.5) = 0.00101 mm. = 1.01 m.

- From Fig. 16.37, rai = 1.25

- Ra = 1.01 x 1.25 = 1.26 m.

- A turning operation uses a 2/64 in nose radius cutting tool on a free machining steel with a feed rate = 0.010 in/rev and a cutting speed = 300 ft/min. Determine the surface roughness for this cut.

- Solution: Ri = f2/32NR = (0.010)2/(32 x 2/64) = 0.0001 in = 100 in

- From Fig. 16.37, rai = 1.02

- Ra = 1.02 x 100 = 102 in

- A single-point HSS tool with a 3/64 in nose radius is used in a shaping operation on a ductile steel workpart. The cutting speed is 120 ft/min. The feed is 0.014 in/stroke and depth of cut is 0.135 in. Determine the surface roughness for this operation.

- Solution: Ri = f2/32NR = (0.014)2/(32 x 3/64) = 0.000131 in = 131 in

- From Fig. 16.37, rai = 1.8

- Ra = 1.8 x 131 = 235 in

- A part to be turned in an engine lathe must have a surface finish of 1.6 m. The part is made of a free-machining aluminum alloy. Cutting speed = 150 m/min, and depth of cut = 4.0 mm. The nose radius on the tool = 0.75 mm. Determine the feed that will achieve the specified surface finish.

- Solution: For free-machining aluminum at 150 m/min, from Figure 16.37 ratio rai = 1.0 in Eq. (16.22), so Ra = Ri

- Ra = Ri = f2/32NR

- Rearranging, f2 = Ri(32NR) = 1.6(10-6)(32)(0.75)(10-3) = 38.4(10-9) = 3.84(10-8) m2

- f = (3.84(10-8) m2)0.5 = 1.96(10-4) m = 0.196 mm (mm is interpreted mm/rev)

- Solve previous Problem 16.16 except that the part is made of cast iron instead of aluminum and the cutting speed is reduced to 100 m/min.

- Solution: For cast iron at 150 m/min, extrapolating Figure 16.37 ratio rai = 1.2 in Eq. (16.22),

- so Ra = 1.2 Ri = 1.2f2/32NR

- Rearranging, f2 = Ri(32NR)/1.2 = 1.6(10-6)(32)(0.75)(10-3)/1.2 = 31.96(10-9) = 3.196(10-8) m2

- f = 3.196(10-8) m2)0.5 = 1.79(10-4) m = 0.179 mm (mm is interpreted mm/rev)

- A face milling operation is to be performed on a cast iron part to finish the surface to 36 -in. The cutter uses four inserts and its diameter is 3.0 in. The cutter rotates at 475 rev/min. To obtain the best possible finish, a type of carbide insert with 4/64 in nose radius is to be used. Determine the required feed rate (in/min) that will achieve the 36 -in finish.

Solution: v = πDN = π(3/12)(475) = 373 ft/min

For cast iron at 373 ft/min, from Figure 16.2 ratio rai = 1.26, so Ra = 1.26 Ri

Ri = Ra/1.26 = 36/1.26 = 28.6 in

Ri = f2/32 NR

Rearranging, f2 = 32Ra(NR) = 32(28.6 x 10-6)(4/64) = 57.1 x 10-6 in2

f = (57.1 x 10-6).5 = 7.56 x 10-3 = 0.00756 in/tooth.

fr = Nntf = 475(4)(0.00756) = 14.4 in/min

- A face milling operation is not yielding the required surface finish on the work. The cutter is a four-tooth insert type face milling cutter. The machine shop foreman thinks the problem is that the work material is too ductile for the job, but this property tests well within the ductility range for the material specified by the designer. Without knowing any more about the job, what changes in (a) cutting conditions and (b) tooling would you suggest to improve the surface finish?

- Solution: (a) Changes in cutting conditions: (1) decrease chip load f, (2) increase cutting speed v, (3) use cutting fluid.

- (b) Changes in tooling: (1) increase nose radius NR, (2) increase rake angle, and (3) increase relief angle. Items (2) and (3) will have a marginal effect.