9 SHAPING PROCESSES FOR RUBBER AND POLYMER MATRIX COMPOSITES

Review Questions

- How is the rubber industry organized?

- Answer. The rubber industry is organized into three parts: (1) rubber growing plantations produce natural rubber, (2) the petrochemical industry produces synthetic rubber, and (3) fabricators take the NR and SR and produce finished rubber goods.

- What is the sequence of processing steps required to produce finished rubber goods?

- Answer. The typical sequence is (1) production of the raw rubber, (2) compounding, (3) mixing, (4) shaping, and (5) vulcanization.

- What are some of the additives that are combined with rubber during compounding?

- Answer. The additives include vulcanizing chemicals, reinforcing fillers, extenders to reduce cost, antioxidants, coloring pigments, plasticizers to soften the rubber, and blowing agents to make foam rubber.

- Name the four basic categories of processes used to shape rubber.

- Answer. The categories are (1) extrusion, (2) calendering, (3) coating, and (4) molding.

- What does vulcanization do to the rubber?

- Answer. Vulcanization causes cross-linking of the rubber molecules; this strengthens and stiffens the rubber while extensibility is retained.

- Name the three basic tire constructions and briefly identify the differences in their construction.

- Answer. The three basic tire constructions are (a) diagonal ply, (b) belted bias, and (c) radial ply.  Diagonal ply and belted bias both have their carcass plys running in a diagonal direction relative to the tire circumference. Radial ply has its carcass plies running in a radial direction. Belted bias and radial ply tires use belts, which are additional plies around the outside circumference of the tire; whereas diagonal ply tires do not have these belts.

- What are the three basic steps in the manufacture of a pneumatic tire?

- Answer. The three steps are (1) preform the components, (2) building the carcass and adding the rubber for the sidewall and treads, and (3) molding and curing.

- What is the purpose of the bead coil in a pneumatic tire?

- Answer. The bead coil provides a rigid support for the tire when it is mounted onto the wheel rim.

- What is a TPE?

- Answer. TPE stands for thermoplastic elastomer; it is a thermoplastic polymer that behaves like a rubber.

- What are the principal polymers used in fiber-reinforced polymers?

- Answer. Principal polymer matrices in FRPs are unsaturated polyesters and epoxies.

- What is the difference between a roving and a yarn?

- Answer. A roving consists of untwisted filaments, while a yarn consists of twisted fibers.

- In the context of fiber reinforcement, what is a mat?

- Answer. A mat is a felt consisting of randomly oriented fibers held loosely together in a binder.

- Why are flakes considered to be members of the same basic class of reinforcing material as particles?

- Answer. Flakes are simply particles that possess very low width-to-thickness ratios.

- What is sheet molding compound (SMC)?

- Answer. SMC consists of TS polymer resin, fillers, and chopped glass fibers, all rolled into a sheet of typical thickness = 6.5 mm (0.250 in).

- How is a prepreg different from a molding compound?

- Answer. Prepregs have continuous fibers rather than chopped fibers as in molding compounds.

- Why are laminated FRP products made by the spray-up method not as strong as similar products made by hand lay-up?

- Answer. Because in hand lay-up, orientation of the fibers is controlled; whereas in spray-up, the fibers in each layer are randomly oriented.

- What is an autoclave?

- Answer. An autoclave is an enclosed chamber which can supply heat and/or pressure at controlled levels.

- What are some of the advantages of the closed mold processes for PMCs relative to open mold processes?

- Answer. The advantages of a closed mold are (1) good finish on all part surfaces, (2) higher production rates, (3) closer control over tolerances, and (4) more complex three-dimensional shapes are possible.

- Identify some of the different forms of polymer matrix composite molding compounds.

- Answer. PMC molding compounds include sheet molding compounds, thick molding compounds (a.k.a. dough molding compounds), and bulk molding compounds.

- What is preform molding?

- Answer. Preform molding is a compression molding process in which a precut mat is placed into the lower half of a mold together with a charge of thermosetting resin; the materials are then pressed between heated molds to cure the resin and produce a fiber-reinforced molding.

- Describe reinforced reaction injection molding (RRIM).

- Answer. RRIM involves the injection of resins that cure by chemical reaction together with reinforcing fibers into a closed mold. The resulting part is a fiber-reinforced (usually glass fiber) plastic molding.

- What is filament winding?

- Answer. Filament winding is a process in which resin-impregnated continuous fibers are wrapped around a rotating mandrel with the internal shape of the FRP product; the resin is cured and the mandrel is removed.

- Describe the pultrusion process.

- Answer. Pultrusion is a process in which continuous fibers are dipped into a resin and pulled through a shaping die (somewhat like an extrusion die) where the resin cures.  The resulting sections are similar to extruded parts except that they are reinforced with continuous fibers.

- How does pulforming differ from pultrusion?

- Answer. Pulforming is pultrusion with the added operation of a shape change in the length (straight length becomes curved) and cross section (different cross sections throughout the length).

- How are FRPs cut?

Answer. Uncured FRPs are cut by methods that include knives, scissors, power shears, steel-rule blanking dies, laser beam cutting, and water jet cutting. Cured FRPs are cut by cemented carbides and HSS cutting tools, diamond cutting tools, and water jet cutting.