6 METAL CASTING PROCESSES

# Review Questions

- Name the two basic categories of casting processes.

- Answer. The two categories are (1) expendable mold processes, and (2) permanent mold processes.

- There are various types of patterns used in sand casting. What is the difference between a split pattern and a match-plate pattern?

- Answer. A split pattern is a pattern that consists of two pieces; a match-plate pattern consists of the two split patterns attached to opposite sides of a plate.

- What is a chaplet?

- Answer. Chaplets are metal supports of various designs used to hold the core in place in the sand mold.

- What properties determine the quality of a sand mold for sand casting?

- Answer. The usual properties are (1) strength - ability to maintain shape in the face of the flowing metal, (2) permeability - ability of the mold to allow hot air and gases to escape from the cavity, (3) thermal stability - ability to resist cracking and buckling when in contact with the molten metal, (4) collapsibility - ability of the mold to give way during shrinkage of the solidified casting, and (5) reusability - can the sand be reused to make other molds?

- What is the Antioch process?

- Answer. The Antioch process refers to the making of the mold.  The mold is 50% sand and 50% plaster heated in an autoclave and then dried.  This mold has greater permeability than a plaster mold.

- What are the most common metals used in die casting?

- Answer. Common die-casting metals include zinc, tin, lead, aluminum, brass, and magnesium.

- Which die-casting machines usually have a higher production rate, cold-chamber or hot-chamber, and why?

- Answer. Hot-chamber machines are faster because cold-chamber die casting machines require molten metal to be ladled into the chamber from an external source. Ladling takes more time than injecting the molten metal into the die as in the hot-chamber operation.

- What is flash in die casting?

- Answer. Flash is a thin portion of metal at the exterior of a casting that results from molten metal being squeezed into the spaces between the die halves of the mold at the parting line, or into the clearances around the cores and ejector pins.

- What is a cupola?

- Answer. A cupola is a vertical cylindrical furnace equipped with a tapping spout near its base.  Cupolas are used for melting cast irons.

- What are some of the operations required in sand casting after the casting is removed from the mold?

- Answer. The operations include (1) trimming, in which the sprues, runners, risers, and flash are removed, (2) core removal, (3) surface cleaning, (4) inspection, (5) repair if needed, (6) heat treatment, and (7) machining.

- What are some of the general defects encountered in casting processes? Name and briefly describe three.

Answer. General defects include: (1) misruns, in which the casting solidifies before filling the mold cavity; (2) cold shuts, in which two portions of metal flow together but there is lack of fusion at the joint; (3) cold shots, where solid globules of cast metal become entrapped in the casting; (4) shrinkage cavity, which is a depression on the casting surface or an internal void in the casting caused by solidification shrinkage; (5) microporosity, which is a network of small voids throughout the casting caused by localized solidification shrinkage; and (6) hot tearing, which is a crack in the casting caused by a mold that does not yield to the metal during the early stages of solidification shrinkage.

# Problems

- A horizontal true centrifugal casting operation will be used to make copper tubing. The lengths will be 1.5 m with outside diameter = 15.0 cm, and inside diameter = 12.5 cm. If the rotational speed of the pipe = 1000 rev/min, determine the G-factor.

- Solution: From Eq. (6.3), GF = R(N/30)2/g = 7.5((1000)/30)2/981 = 83.8

- A true centrifugal casting operation is performed in a horizontal configuration to make cast iron pipe sections. The sections will have a length = 42.0 in, outside diameter = 8.0 in, and wall thickness = 0.50 in. If the rotational speed of the pipe = 500 rev/min, determine the G-factor. Is the operation likely to be successful?

- Solution: Using outside wall of casting, R = 0.5(8)/12 = 0.333 ft.

- v = RN/30 = (0.333)(500)/30 = 17.45 ft/sec.

- GF = v2/Rg = (17.45)2/(0.333 x 32.2) = 28.38

- Since the G-factor is less than 60, the rotational speed is not sufficient, and the operation is likely to be unsuccessful.

- A horizontal true centrifugal casting process is used to make brass bushings with the following dimensions: length = 10 cm, outside diameter = 15 cm, and inside diameter = 12 cm. (a) Determine the required rotational speed in order to obtain a G-factor of 70. (b) When operating at this speed, what is the centrifugal force per square meter (Pa) imposed by the molten metal on the inside wall of the mold? The density of brass is 8.62 g/cm3.

- Solution: (a) Using the outside wall diameter of the casting, which is equal to the inside wall diameter of the mold, D = 15 cm

- N = (30/)(2g x 70/15).5 = 913.7 rev/min.

- (b) Use 1.0 cm of mold wall length as basis of area calculations.

- Area of this length of mold wall A = DoL = (15 cm)(1 cm) = 15 cm2 = 15(10-4) m2

- Volume of cast metal V = (Ro2 - Ri2)(1.0) = ((7.5)2 - (6)2)(1.0) = 63.62 cm3

- Mass m = (8.62 g/cm3)(63.62 cm3) = 548.4 g = 0.5484 kg

- v = RN/30	Use mean radius R = (7.5 + 6.0)/2 = 6.75 cm

- v = (6.75)(913.7)/30 = 645.86 cm/s = 6.4585 m/s

- Centrifugal force per square meter on mold wall = Fc/A where Fc = mv2/R

- Fc = (0.5484 kg)(6.4586 m/s)2/(6.75 x 10-2 m) = 338.9 kg-m/s2

- Given that 1 N = 9.81 kg-m/s2, Fc = 338.9/9.81 = 34.55 N

- Fc/A = (34.55 N)/(15 x 10-4 m2) = 0.7331(104) N/m2 = 7331 Pa

- True centrifugal casting is performed horizontally to make large diameter copper tube sections. The tubes have a length = 1.0 m, diameter = 0.25 m, and wall thickness = 15 mm. (a) If the rotational speed of the pipe = 700 rev/min, determine the G-factor on the molten metal. (b) Is the rotational speed sufficient to avoid "rain?" (c) What volume of molten metal must be poured into the mold to make the casting if solidification shrinkage and contraction after solidification are considered? Solidification shrinkage for copper = 4.5%, and solid thermal contraction = 7.5%.

- Solution: (a) GF = v2/Rg		g = 9.8 m/s2

- v = RN/30 = (.125)(700)/30 = 9.163 m/s

- GF = (9.163)2/(0.125 x 9.8) = 68.54

- (b) G-factor is sufficient for a successful casting operation.

- (c) Volume of final product after solidification and cooling is

- V = (0.252 - (0.25-.03)2) x 1.0/4 = 0.25(0.252 - 0.222) = 0.011074 m3

- Given: solidification shrinkage = 4.5% and solid thermal contraction = 7.5% for copper. Taking these factors into account,

- Volume of molten metal V = 0.011074/(1 - 0.045)(1 - 0.075) = 0.01254 m3

- If a true centrifugal casting operation were to be performed in a space station circling the Earth, how would weightlessness affect the process?

- Solution: The mass of molten metal would be unaffected by the absence of gravity, but its weight would be zero. Thus, in the G-factor equation (GF = v2/Rg), GF would theoretically go to infinity if g = 0. Thus, it should be possible to force the metal against the walls of the mold in centrifugal casting without the nuisance of “raining” inside the cavity.  However, this all assumes that the metal is inside the mold and rotating with it. In the absence of gravity, there would be a problem in pouring the molten metal into the mold cavity and getting it to adhere to the mold wall as the mold begins to rotate. With no gravity the liquid metal would not be forced against the lower surface of the mold to initiate the centrifugal action.

- A horizontal true centrifugal casting process is used to make aluminum rings with the following dimensions: length = 5 cm, outside diameter = 65 cm, and inside diameter = 60 cm. (a) Determine the rotational speed that will provide a G-factor = 60. (b) Suppose that the ring were made out of steel instead of aluminum. If the rotational speed computed in part (a)  were used in the steel casting operation, determine the G-factor and (c) centrifugal force per square meter (Pa) on the mold wall. (d) Would this rotational speed result in a successful operation? The density of steel = 7.87 g/cm3.

- Solution: (a) Use inside diameter of mold in Eq. (6.4), D = Do = 65 cm. Use g = 981 cm/s2,

- N = 30(2g x GF/D).5/ = 30(2 x 981 x 60/65).5/ = 406.4 rev/min.

- (b) Rotational speed would be the same as in part (a) because mass does not enter the computation of rotational speed. N = 406.4 rev/min

- (c) Use 5 cm ring length as basis of area calculations.

- Area of this length of mold wall A = DoL = (65 cm)(5 cm) = 1021 cm2 = 0.1021 m2

- Volume of cast metal V = (Ro2 - Ri2)(L) = ((65/2)2 - (60/2)2)(5.0) = 2454.4 cm3

- Density of steel  = 7.87 g/cm3

- Mass m = (7.87g/cm3)(2454.4 cm3) = 19,315.9 g = 19.316 kg

- v = RN/30	Use mean radius R = (65 + 60)/4 = 31.25 cm = 0.3125 m

- v = (31.25)(406.4)/30 = 1329.9 cm/s = 13.299 m/s

- Centrifugal force per square meter on mold wall = Fc/A where Fc = mv2/R

- Fc = (19.316 kg)(13.299 m/s)2/(0.3125 m) = 10,932.1 kg-m/s2

- Given that 1 N = 9.81 kg-m/s2, Fc = 10,932.1/9.81 = 1114.4 N

- Fc/A = (1114.4 N)/(0.1021 m2) = 10,914.7 N/m2 = 10,914.7 Pa

- (d) The G-factor of 60 would probably result in a successful casting operation.

- For the steel ring of preceding Problem 6.10(b), determine the volume of molten metal that must be poured into the mold, given that the liquid shrinkage is 0.5%, solidification shrinkage = 3%, and solid contraction after freezing = 7.2%.

- Solution: Volume of final casting V = (Ro2 - Ri2)L = (32.52 - 302)(5) = 2454.4 cm3

- Given that the molten metal shrinkage = 0.5%, and from Table 10.1, the solidification shrinkage for steel = 3% and the solid contraction during cooling = 7.2%, the total volumetric contraction is

- (1-0.005)(1-0.03)(1-0.072) = 0.8957

- The required starting volume of molten metal V = 2454.4/(0.8957) = 2740.2 cm3

- A horizontal true centrifugal casting process is used to make lead pipe for chemical plants. The pipe has length = 0.5 m, outside diameter = 70 mm, and wall thickness = 6.0 mm. Determine the rotational speed that will provide a G-factor = 60.

- Solution: D = 70 mm = 0.07 m.  g = 9.8 m/s2

- N = 30(2g x GF/D).5/ = 30(2 x 9.8 x 60/.07).5/ = 1237.7 rev/min.

- The housing for a certain machinery product is made of two components, both aluminum castings. The larger component has the shape of a dish sink, and the second component is a flat cover that is attached to the first component to create an enclosed space for the machinery parts. Sand casting is used to produce the two castings, both of which are plagued by defects in the form of misruns and cold shuts. The foreman complains that the parts are too thin, and that is the reason for the defects. However, it is known that the same components are cast successfully in other foundries. What other explanation can be given for the defects?

- Solution: Misruns and cold shuts result from low fluidity. One possible reason for the defects in this case is that the thickness of the casting cross sections is too small. However, given that the casting of these parts is successfully accomplished at other foundries, two other possible explanations are (1) the pouring temperature is too low, and (2) the pouring operation is performed too slowly.

- A large steel sand casting shows the characteristic signs of penetration defect: a surface consisting of a mixture of sand and metal. (a) What steps can be taken to correct the defect? (b) What other possible defects might result from taking each of these steps?

Solution: (a) What are the possible corrective steps? (1) Reduce pouring temperature. (2) Increase the packing of the mold sand to resist penetration. (3) Treat the mold cavity surface to make it harder.

(b) What possible defects might result from each of these steps? In the case of step (1), the risk is for cold shuts and misruns. Steps (2) and (3) would reduce permeability of the sand, thus increasing the risk of sand blows and pin holes.